## Slide 1: Booster QCM update
Anna Solopova, Mike Drury
Updated 09-01-2020

## Slide 2: QCM commissioning preliminary results
 | Cavity 1 (2-cell) | Cavity 2 (7- cell)
QextFPC | 6.2E+06 | 9.7E+06
QextFP | 2.4E+12 | 3.0E+12
Emax (MV/m) | 15.1 | 15.2
Emaxop (MV/m) (1 Hour run) | 14.5 | ~14.0
Limit | Quench | Maxed out RF drive
FE onset (MV/m) | 11.5 | 16.0
RF heat load at typical operating gradients | 9.5E+09 (< 1W at 6 MV/m) | 1.2E+10 (~12 W at 6 MV/m)
Static heat load | 20 W |