CHAPTER

Photocathodes

Wei Liu1,2,3, Matt Poelker3, John Smedley4, Romain Ganter5

1Institute of Modern physics, Chinese Academy of Sciences, 509 Nanchang Rd., Lanzhou, 730000, China

2University of Chinese Academy of Sciences,19A Yuquan Rd., Beijing, 100049, China

3Thomas Jefferson National Accelerator facility, 12000 Jefferson Avenue, Newport News, Virginia, 23606, USA

4 Affiliation of John ????

5Paul Scherrer Institut, 5232 Villigen PSI, Switzerland

Abstract

Photocathodes were at the heart of quantum physics development in the early twentieth century and are still used in high technologies devices like night-vision goggles, photomultiplier tubes and particle accelerators. The simplest form of photocathode is a metallic surface, negatively biased, from which electrons are extracted by energetic photons. After a brief description of the photocathode preparation, this chapter will present the latest developments and limitations of metallic and semi-conductor photocathodes.

Contents

1	Introduction to photoemission	3

1.1	One-Step and Three-Step Models of Photoemission	3

1.2	Comparison between metal and semi-conductor photoemission processes based on the three steps model	4

2	Metallic Photocathodes:	6

2.1	Introduction:	6

2.2	Practical approach of photoemission from metals	6

2.3	QE performances of metals	8

2.4	Limitations and potential of metallic photocathodes	12

2.4.1	Cathode preparation: bulk material choice, polishing and cleaning techniques	12

2.4.2	Incident photons	17

2.4.3	Surface Electric Field:	18

3	PEA Semiconductors	19

3.1	Introduction	19

3.2	Preparation and performances of Cs2Te photocathodes:	20

3.2.1	Preparation methods	20

3.2.2	QE values of Alkali based cathodes - Cs2Te:	22

3.3	Sensitivity to vacuum	23

3.4	Alkali-Antimonide photocathodes:	24

3.4.1	Preparation methods and film properties	24

4	NEA Semiconductors: GaAs photocathodes for polarized electron beams	25

4.1	Overview GaAs	25

4.2	Theory: Spin relaxation mechanisms	28

4.3	Recent Measurements	30

4.3.1	Bulk GaAs Polarization Study - Temperature and Zn dopant dependence	30

4.3.2	High Polarization Strained-Superlattice Photocathode with Distributed Bragg Reflector	32

4.3.3	Ion Bombardment – Cleave Plane Dependence	36

5	References	43

# Introduction to photoemission

## One-Step and Three-Step Models of Photoemission

Photoemission has a long and storied history in physics, beginning with Einstein’s explanation of the photoelectric effect in 1905. Today photoemission spectroscopy, both in the UV and X-ray regime (UPS/XPS), is used to characterized materials, determine chemical bonding and measure electronic band structures of materials.  Two prevailing theoretical frameworks exist for describing photoemission, the one-step quantum mechanical model [J1], and the three-step model [J2,1] described in detail below. The one-step model relies on a “sudden” approximation, where electrons are excited from a bound state within a material to a free state outside of it, in a transition that can be described by a quantum mechanical matrix element. This model is widely used in UPS analysis to understand material band structure; it considers electrons to conserve both energy and momentum upon emission. While powerful, this model is in general not widely applicable to practical photocathodes, as it generally assumes well defined crystalline initial states, and ignores electron scattering within the material.

The Three-Step Model was developed to deal with photoemission in practical photocathodes, and had found great success in predicting the behavior of both metals and semiconductors in the near-threshold regime that dominates practical applications.  In this model, the process is broken into:

- absorption and excitation

- transport to surface

- escape over or through the surface barrier

Step 1 accounts for loss of incident light due to reflection, and the excitation of electrons from filled states in the material valence band to excited states in the material conduction band. Most treatments of the model neglect momentum as a conserved quantity, reasoning that phonon scattering and the polycrystalline initial state will randomize the electron momentum state while leaving its energy largely unaffected. The electronic Density of States (DOS) is considered, so conservation of energy is accounted for. In this way, the model accounts for unproductive absorption (photons which excite electrons to conduction band states with energy below the vacuum level, so that they cannot escape).

Step 2 accounts for loss due to the various scattering processes which occur during the transport to the surface.  Here the photon absorption length is compared to the electron mean free path, to determine the fraction of electrons lost to scattering. For metals, the dominant scattering mechanism is electron-electron scattering, and a single scattering event is considered to be a loss mechanism.  For semiconductors, as will be discussed in detail later, electron-electron scattering is often forbidden and other scattering mechanisms take over.

Step 3 accounts for the direction of travel within the material as the electron approaches the surface. Although we often think of the work function as a limit on the energy required to escape the material, it is actually a limit on required momentum perpendicular to the material surface. Thus the electron direction of travel must be within a cone defined by the energy in excess of the emission threshold to escape.  For metals, failure to meet this criterion is considered a loss mechanism, as the electron will reflect off the surface and be lost to subsequent e-e scattering. For semiconductors, a monte carlo treatment is required, as the electrons may have their direction of travel randomized again via phonon scattering.

Each step represents a probability of photon/electron survival. The product of these probabilities produces an energy distribution curve (EDC: relative yield as a function of electron energy), and the integration of these EDCs over all energies capable of escape provides the QE.

## Comparison between metal and semi-conductor photoemission processes based on the three steps model

Metal photocathodes are used for some low average current accelerator applications, especially where prompt response time is required. However, most new accelerator applications and virtually all photodetector applications use semiconductor cathodes. The reason for this is that semiconductor cathodes offer far superior quantum efficiency performance, and can be sensitive to visible or infrared radiation. The photoemission mechanism for both metals and semi-conductors can be described by the three step model outlined above [1]. However, there are two fundamental differences – the extent of unproductive absorption and the type of collisions that photoexcited electrons experience during their travel to the surface.

In metals, photons can in general be absorbed throughout the conduction band, resulting in a large number of photons being “used” to excite electrons to states which lack sufficient energy to escape. In addition, photoexcited electrons may collide with electrons from the conduction band. In such scattering, the photoexcited electrons lose energy such that they can no longer escape (Fig. 1.2.1) and thus will not contribute to the QE. In consequence, only electrons within one electron mean free path λe-e below the surface can possibly escape. In metals, the value of λe-e is much smaller than the laser penetration depth so that only a small fraction of the photoexcited electrons can be emitted (the violet area in Fig. 1.2.1) making the QE of metals low.

In semiconductors, the bandgap performs two functions. First, it limits unproductive absorption, as no electrons are excited into the bandgap due to the absence of a final allowed state. The lack of states in the band gap also has a consequence on scattering – electron-electron collisions are not allowed if the final energy of electrons falls into this gap (Fig. 1.2.1). As a consequence, λe-e can be even larger than the laser penetration depth and all photoexcited electrons could potentially reach the surface. This makes the QE of semiconductors much larger than the QE of metals [2] since the reservoir of electrons eligible for photoemission is much larger than for metals. For example, the forbidden gap of Cs2Te photocathodes is 3.3 eV wide. Only the electrons excited above an energy of 6.6 eV will be able to scatter with an electron from the valence band. With laser light at 266 nm (that is to say a photon energy of 4.6 eV), photoexcited electrons will not interact with the other electrons from the conduction band during their travel to the surface. Other scattering processes, such as grain boundary scattering and scattering with lattice phonons still occur, however electrons in these interactions tend to lose only a small fraction of their energy [3]. Scattering of electrons with the lattice can even be beneficial, as the interaction randomizes the electron momentum with minimal loss of energy. This allows electrons that are initially moving away from the surface to be redirected, potentially allowing emission. In this way, semiconductor cathodes can have a QE over 50% (CsI, for example). Interaction with the lattice can also cool the electrons, which is beneficial for certain accelerator photoinjector applications, as it reduces the initial kinetic energy of the photoemitted electrons (Ekin) and thus also the intrinsic emittance.

Figure 1.2.1: The 3 steps model can be used both for metals and semiconductors, here parameters of copper and Cs2Te are compared. λe-e and λe-p correspond to the electron mean free path between electron – electron and electron – phonon scattering events; τ is the electron extraction time (colored figure).

!!! @ John:  As discussed in the meeting, you can add something about the importance of density of states, the particularity of superconducting metals … .

# Metallic Photocathodes:

## Introduction:

The metals discussed in this chapter are the most common metals that occur freely in nature. One of the most important parameters which characterize a photocathode is quantum efficiency (QE), that is to say, the ratio of emitted electrons to the number of incident photons. The goal of many studies aims at increasing the QE of cathodes. In practice, the QE parameter is not the only parameter to look at since the QE value obtained in the ideal condition of a laboratory might not be reproducible in all photocathode applications. Indeed, many other constraints like the vacuum level, the wavelength of incident photons, the applied electric field amplitude, and the mechanical assembly where the cathode sits, will determine the type of cathode material to choose and consequently the QE which can be expected. In the following paragraphs we will review the most important parameters which determine the performance of a photocathode material.

## Practical approach of photoemission from metals

The QE depends on three fundamental parameters (for a given illumination wavelength): the photo-cathode reflectivity, the material work function and the applied electric field (see eq. 2.2.1). Metallic photocathodes are often used in applications where the cathode surface has to be exposed to air. Indeed metallic surfaces will not lose much QE after brief exposure to air, although long exposure to humid air can be problematic. Among metallic photocathodes, a well-known and studied example is the copper photocathode. In the following paragraphs we will look into more detail the behavior of copper photocathodes.

Since photoemission is a process taking place in the first tens of nanometers below the surface, it highly depends on the quality of the surface which is, unfortunately, also changing with time. For example, the work function of a material depends on the presence of contaminants but these contaminants might also migrate across the surface over time. Surface contamination like oxidation changes the reflectivity of the surface and thus the QE. The electric field applied on the cathode surface will be enhanced depending on the roughness of the surface, which can change with photocathode use. This electric field enhancement will also affect the QE locally, through a reduction (or increase) of the Schottky effect. The schematic of Fig. 2.2.1 illustrates this link between fundamental parameters driving the QE and practical aspects of photocathode.

Fig 2.2.1: Schematic representation of the link between the theoretical parameters controlling the QE of copper and macroscopic properties as well as ways to act on these properties.

The time varying nature of photocathode QE can be problematic.  A photocathode with decreasing QE can mean a photogun cannot meet the beam current requirements of the accelerator.  But sometimes photocathode QE increases [4], as illustrated in Fig. 2.2.2, where photocathode QE increased by more than an order of magnitude during 4 days of operation. The change in the surface state was probably due to a cleaning/removal of the contaminants by the illuminating laser. Such QE variation corresponds to only 0.06 eV drop in the surface work function when using the QE expression of Eq. 2.2.1 from [5]

Based on the 3 step model and a step-like Fermi-Dirac distribution for the energy density of states in metals, Dowell et. al. [5] derived a simple expression for the QE of metals which accurately reproduces the experimental data of copper:

eq. 2.2.1

where R corresponds to the reflectivity, λopt is the laser penetration depth, λe-e is the mean free path of electrons between two consecutives electron-electron scattering event; hω is the photon energy, Em is the energy of electrons above the Fermi Level for which λe-e has been measured; Фeff is the effective work function  already reduced by the Schottky effect, and EF is the Fermi level.

It is interesting to note in the measurements of Fig. 2.2.2, that increasing the electric field from 10 MV/m to 20 MV/m results in a QE increase of a factor 10. Such a doubling of the electric field can easily happen locally, due to mechanical protruding defects which will enhance the electric field (tip effect) on the microscopic scale. This illustrates the importance of the Schottky effect (potential barrier reduction due to the applied electric field) in the value of the QE for photocathode application.

Fig. 2.2.2: QE of a copper photocathode versus the applied electric field during 4 days of operation. Laser pulses at 266 nm with 6 μJ per pulse energy at 10 Hz repetition rate were used to illuminate the copper cathode. The copper cathode (inset) was diamond turned with an average roughness of a few nanometers. The theoretical curve corresponds to the QE expression of eq. 2.2.1 taken from [5].

Any change of the surface state will modify the three fundamental parameters (reflection, work function and local electric field) at the same time. Changes in the method of polishing the surface will change the microstructures profile and thus the local electric field but it will also change the reflectivity of the surface and might also change the density of contaminants which in turns modifies the local work function.

## QE performances of metals

Because of the technical difficulty of having atomically clean samples, free of contaminants, the QE of a polycrystalline metal can easily vary from one sample to another. In table 2.3.1, typical values of QE measured for different transition metals are presented. These values were obtained by laser illumination at different wavelengths on polycrystalline metals. Most of Table 2.3.1 comes from Suberlucq [6] and augmented with some recent results. The work function data was compiled by Michaelson [7]. These values correspond to the most reasonable work function values for polycrystalline metals used in practice: the so called preferred work function. Since the work function depends on the crystal orientation distribution, the vacuum quality and the surface cleanliness, one can reasonably expect a variation of 0.1 – 0.2 eV from one sample to another. This is the reason why QE values differ from one measurement to another in table 2.3.1.

|  [nm] | 193 | 213/209 | 248 | 262-266 | 308 | 355 | s | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E [eV] | 6.4 | 5.8 / 5.9 | 5 | 4.7 | 4 | 3.5 | eV |  |
| Al |  | 8.4*10-4 |  | 3.2*10-5 |  | 3.4*10-7 | 4.3 | [8] [9] |
| Ag (a) |  |  |  | 2*10-5 |  |  | 4.3 | [10] |
| Ag (b), (g) |  |  |  | 8.4*10-5 |  |  | 5.06 | [11] |
| Au (a) |  |  |  | 4.7*10-5 |  |  | 5.1 | [10] |
| Au |  | 4*10-4 |  | 1.310-5 |  |  | 5.1 | [8] |
| Ca |  |  | 4*10-5 |  |  |  | 2.9 | [12] |
| Cu | 2.0*10-4 | 1.5*10-4 |  | 2.2*10-6 | 1.6*10-7 | 8*10-9 | 4.6 | [8] |
| Cu (b) | 1.5*10-3 | 4.2*10-4 |  |  |  |  | 4.6 | [8] |
| Cu (a) (g) |  |  |  | 1.4*10-4 |  |  | 4.6 | [10] & [13] [14] |
| Cu |  |  | 5*10-5 |  |  |  |  | [15] [16] |
| Mg |  |  |  | 5.1*10-5 |  |  | 3.7 | [8] |
| Mg |  |  |  | 2.7*10-4 |  |  | 3.7 | [8] |
| Mg (d) |  |  |  | 5*10-4 |  |  | 3.7 | [17] |
| Mg (b) |  |  |  | 1.7*10-3 |  |  | 3.7 | [11] |
| Mo |  |  |  | <7*10-7 |  |  | 4.6 | [8] |
| Mo (b) |  |  |  | 2.5*10-6 |  |  | 4.6 | [9] [11] |
| Nb | 4.5*10-4 |  | 3.2*10-6 |  |  |  | 4.3 | [[18] |
| Nb |  |  |  | 3.*10-6 |  |  | 4.3 | [9] |
| Nb (b) |  |  |  | 1.9*10-4 |  |  | 4.3 | [11] |
| Nb (b), (g) |  |  |  | 2.6*10-4 |  |  |  | [14] |
| Ni (a) |  |  |  | 2.5 10-5 |  |  | 5.2 | [10] |
| Pb | 5.4*10-3 | 2.7*10-3 |  |  |  |  | 3.88 | [19] |
| Pb (b) |  |  |  | 2.2*10-4 |  |  | 3.88 | [11] |
| Pd (a) |  |  |  | 1.2*10-5 |  |  | 5.1 | [10] |
| Ac 316 LN |  | 9*10-5 |  | 1.6*10-6 |  |  | ? | [8] |
| Sm |  |  |  |  | 1.6*10-6 |  | 2.7 | [8] |
| Sm (a) |  |  |  | 7.3*10-4 |  |  | 2.7 | [10] |
| Ta (a) |  |  |  | 10-5 |  |  | 4.3 | [10] |
| Tb (a) |  |  |  | 2.3*10-4 |  |  | 3 | [10] |
| Ti |  |  |  | 6.*10-6 |  |  | 4.33 | [9] |
| Ti (b) |  |  |  | 3.3*10-4 |  |  |  | [11] |
| V (b), (g) |  |  |  | 10-5 |  |  |  | [11] |
| W (111)(e) |  |  |  |  |  | 2*10-5 | 4.5 | [20] |
| WK+ (b), (f) |  |  |  |  | 1.2*10-5 |  | 2.8 | [8] |
| Y |  |  |  | 5*10-4 |  |  | 3.1 | [10] |
| Y |  |  |  | 2.7*10-6 | 1.1*10-6 |  | 3.1 | [8] |
| Y (b) |  |  |  | 1.8*10-4 |  |  | 3.1 | [8] |
| Y (a) |  |  |  | 5*10-4 |  |  | 3.1 | [10] |
| Zn (a) |  |  |  | 1.4*10-5 |  |  | 4.3 | [10] |
| Zr (a) |  |  |  | 10-5 |  |  | 4.1 | [10] |
| Zr (b) |  |  |  | 2.9*10-4 |  |  |  | [11] |
| Фs = work function from [7]. (a) = Surface preparation and activation under vacuum, from [10]. (b) = Cleaning by Argon ion bombardment [21] (d) = ATF (BNL) measurements at 70 MV/m without surface treatment (e) = Photoemission assisted by high electric field, E = 3 GV/m (f) = Potassium ions implanted in tungsten substratum (150 keV implantation energy, ion density 1.3x1017 ions / cm2 at the surface) (g)= Annealing procedure at 250 deg. C |  |  |  |  |  |  |  |  |

Table 2.3.1: Quantum Efficiency of polycrystalline metallic photocathodes (main source: [6])

If no special in-vacuum treatment is applied to a metallic photocathode surface, QE will be dominated by the contamination on the surface. Reaction of the cathode surface with air leads to surface chemistry like oxidation which will increase the work function. The QE can then become much smaller than the values listed in Table 2.3.1. Fig 2.3.1 illustrates QE measurements taken in a diode-geometry gun where the cathode was illuminated with laser pulses at 266 nm. The metal samples were exposed to air for several weeks before being installed in the diode gun. Under such conditions the QE always stayed below 1e-4 and the ordering of the metal becomes much different from that of work function revealing more the reactivity of the metal with ambient air.

Fig.2.3.1: Quantum efficiency from various metal measured in a diode gun (350 kV and variable gap) using laser pulses of 6 ps rms pulses length at 266 nm, 10 Hz. Cathode samples were exposed to air without any in vacuum cleaning treatment [9] .

For an atomically clean surface, the crystal orientation can change the work function by several tenths of eVs leading to important variation of QE. Table 2.3.2 gives an example of the work function variation for different crystal orientations of copper which extends from 4.48 to 4.94 eV, that is to say 0.46 eV variations. The dependence of the QE with the work function is plotted in Fig. 2.3.2 which corresponds to the Eq. 2.2.1 for the case of copper illuminated by 253 nm photons. Taking into account the Schottky reduction (~ 0.3 eV), the effective work function ranges between 4.18 eV and 4.64 eV which corresponds to a QE variation of one order of magnitude.

Crystal Orientation; Work function (eV). Cu Polycrystalline; 4.65 +/- 0.2. Cu (100); 4.59 +/- 0.03. Cu (110); 4.48 +/- 0.03. Cu (112); 4.53 +/- 0.03. Cu (111); 4.94 +/- 0.03.

Table 2.3.2: Work function for four crystal orientations of copper from  [7].

Fig. 2.3.2: Variation of QE versus work function in case of 253 nm wavelength illuminating copper.

Figure 2.3.3 shows two micrographs of a polycrystalline copper photocathode from an RF photo-injector. The grain boundaries between different facet orientations are clearly visible on the picture and the cathode surface appears as a highly non-uniform surface. In practice, it is difficult to observe a spatial variation of QE on a polycrystalline metal surface (see for example QE map of Fig. 2.4.3) Most probably because the effective spatial distribution of work function is dominated by contaminants on the surface. A single crystal photocathode would have the advantage of a much better uniformity. If the typical grain size is however larger than the illuminating spot size, one could also obtained photoemission from a single crystal. In the RF photoinjector of the LCLS free electron laser at Stanford, a polycrystalline copper photocathode is used as an electron source. During the preparation of the cathode, the copper is fired to very high temperature (above 800 degree C) such that the grain sizes are growing to become almost larger than the laser spot size illuminating the cathode (mm). By picking up a sufficiently large grain they can obtain photoemission from a single crystal [15].

Fig. 2.3.3: Micrographs of a copper photocathode under white light illumination [13].

As illustrated in table 2.3.1, the QE also decreases with the illuminating photon energy, simply because the amount of electrons in the conduction band eligible for excitation above the vacuum barrier gets reduced (see Fig. 1.2.1). On the other hand, this means also that photo-emitted electrons have energies just above the top of the barrier of potential. That is to say they have very low initial kinetic energy at emission which can be beneficial for applications where the thermal agitation of extracted electrons (intrinsic emittance) is a concern. For example, in accelerator physics one aim to produce electron bunches that occupies a very small volume in phase space. This is the case if all electrons are following parallel trajectories at cathode exit without random thermal agitation. The drawback is that the QE becomes very low when the photon energy becomes close to the barrier height.

Figure 2.3.4 from Vicario et al. [22] illustrates quite well the dependence of the QE on the illuminating photon wavelength. To fit the data they used a similar relation to eq. 2.2.1 for copper.

Fig. 2.3.4: Quantum efficiency of a copper photocathode versus the illuminating wavelength from [22].

## Limitations and potential of metallic photocathodes

### Cathode preparation: bulk material choice, polishing and cleaning techniques

As mentioned in the previous section, the cathode surface preparation before installation in vacuum but also after being installed in vacuum is extremely important to get QE values as expected from theory. All metallic photocathodes produced from bulk metals in air, will have several layers of adsorbed contaminants on the surface. These contaminants can come from the ambient air (H2O, CO, CO2, N2, H2, …) or are organic films, chemical compounds of the base metal formed during the machining and manipulation of the photocathode.

Out of vacuum cleaning:

A common technique to clean metals for ultra-high vacuum is to start with a hot ultra-sound washing with detergent followed by a careful rinsing. Alkaline cleaners like tetrapotassium pyrophosphate are efficient detergent to clean metallic surfaces [23] [24]. In a second step, ultra-sound cleaning with solvent like acetone and alcohol is a good way to remove remaining grease or organic films from the surface. The photocathode should then be dried with dry air and be installed as soon as possible under vacuum. Detergent and solvent are however not removing oxide layer and should be applied as a last step just before installation in vacuum.

To remove the oxide layer, more aggressive techniques are needed like the mechanical polishing (discussed below) which will remove a layer of several micrometers thickness or an acid treatment (nitric, sulfuric, hydrochloric and phosphoric acid). In the case of mechanical polishing cleaning processes as mentioned above are required afterwards. For both techniques, it is important to put the photocathode as soon as possible after the treatment under vacuum. Indeed after, the oxide layer has been removed the surface is very reactive and depending on the metal type an oxide layer could build up again very rapidly. All metals do not react at the same rate with molecules. For example oxidation of copper is much faster and never stops in contrary to aluminum.

In vacuum cleaning:

To remove molecules adsorbed in the surface, one efficient way is to heat up the photocathode under vacuum. If the annealing exceeds 250 degree Celsius than most of the water, hydrogen and carbon based molecules will be desorbed from the surface. Figure 2.4.1 illustrates the effect of annealing a copper photocathode to about 250 deg C for 10 hours. The QE was increased by a factor 5 to 30 [25] after the thermal cycle for three different samples. Such annealing procedure insures that the initial QE of a copper photocathodes stays around 10-4, that is to say close to the theoretical expectation of polycrystalline copper [13].

Fig. 2.4.1: Effect of the annealing of a copper photocathode on QE: QE versus time (top) and temperature cycle versus time (bottom) for three samples Cu_17, Cu_20 and Cu_20b (source: [25]).

Once the cathode surface has been atomically cleaned under vacuum then the only contamination which would appear again comes from the residual gas present in the vacuum chamber. Typical contaminants in vacuum systems are residual molecules from air like H2O, CO, CO2, N2, H2, O2, … . Assuming that all striking molecules from residual gas would stick to the surface, it takes only one hour to cover the surface by one monolayer at a pressure of 10-9 torr [26]. Luckily the partial pressure and sticking coefficient of residual gas such as CO and H2O is much smaller. But it explains why the QE of a cathode can evolve in time by quite some large amount as in Fig. 2.4.2. In some condition the illuminating light can help to clean the surface but it can also crack the molecules so that they stick even more to the surface as illustrated by the nice QE hole in Fig. 2.4.3 which is exactly at the laser spot position. In any case, a regular annealing procedure after some time of operation will desorb most of the accumulated contaminants and bring back the QE close to its initial value. Another important mechanism responsible for QE variation and which can lead to definitive damage of the surface is the ion back bombardment. Residual gas atoms and molecules can be ionized near the cathode by the photoelectrons and will then be accelerated towards the cathode. This mechanism can be a major issue in an anode cathode configuration with DC voltage. The negatively biased photocathode acts like an ion pump which ionizes residual gas in the beam path and collects them on the photocathode.

Fig. 2.4.2: Evolution of the QE of copper photocathode samples over several weeks of operation under pulsed laser illumination (parameters in inset) in a vacuum of 10-9 mbar.

Several other techniques do exists to clean metallic photocathodes in vacuum. A common technique consists in using a laser that is focused close to the ablation threshold and then to scan the laser spot other the cathode surface [16]: the so-called laser cleaning technique. In order to avoid too large craters on the surface, a careful monitoring of the vacuum pressure during laser cleaning is required [27,28]. Ozone cleaning has also been successfully used to desorb molecules from metallic surface [29].

Fig 2.4.3.: QE map revealing the effect of laser illumination on QE degradation. Long term illumination has the effect of cracking organic molecules which then are bind to the surface (source: [25]) (Colored Figure).

Figure 2.4.3 is a QE map of a copper photocathode which has been used in the electron gun of an accelerator. The QE map is obtained by focusing a UV laser to a small spot (below 100 um) and by scanning this spot over the full cathode surface. One can clearly distinguish a round area where the QE is smaller. This area corresponds to the region which was exposed to the full laser beam during normal operation of the electron gun. Long UV laser exposition seems to induce surface chemistry which then lowers the QE. Some labs are using laser ablation to clean the surface and retrieve the original QE of the bulk photocathode material. Such ablation process is however delicate if one want to preserve the highly polished surface [30].

In addition to the contaminants coming from the residual gas, the cathode material crystal can also contain impurities. Metallic cathodes made out of bulk materials can usually reach purities above 99.99% that is to say about 10 ppm of different impurities like O2, C, P, …. are still present in the crystal. Metals do also contain inclusions, bubbles which could potentially degas molecules once being in vacuum. Metals that are forged or even better produced by hot isostatic pressure (HIP) methods have larger grain sizes and have less inclusions and defects than cast metals such that they are a better choice for photocathode applications.

Fig. 2.4.4: Top: Surface profilometry of a diamond turned copper sample 2.7 mm * 1.5 mm (forged copper). Bottom: Transverse profile along the line cut of the top figure; Grain size: 300 µm; Ra ~3 nm; Height Peak to Valley ~ 30 nm (source: [13]) (Colored figure)

Metallic cathodes made out of bulk material in opposition to those produced by thin film deposition needs to be polished. Diamond turning of the surface with “state of the art” ultra-precision machine lead to average roughness (Ra) of less than 5 nm. Fig 2.4.4 represents an interferometer micrograph of a copper surface which has been diamond turned. The measured roughness is about 3 nm with peak to valley maximum height going up to 30 nm. The parallel diagonal lines seen in the background come from the machining tool. Diamond turning still leaves the waviness of the machine tool on the surface but it still gives better roughness than manual polishing with diamond paste. Indeed, the latest has the drawback to leave small inclusions in the metal, especially for soft metals like copper. The grain boundaries are also visible in Fig. 2.4.4 and have a typical size of a few hundred micrometers. Fig. 2.4.5 shows a 5 by 5 micrometers area of an aluminum sample which was also diamond turned. The average roughness of this sample is about 1.3 nm but the atomic force microscope reveals some local tips which can be as high as 37 nm. The electric field applied to the photocathode will be amplified locally by such tip. This tip effect will lower locally the work function such that non uniformities in the photoemission transverse distribution could appear. These non-uniformities of the emission can then be revealed by electron-imaging of the cathode surface that is to say in a QE map.

Fig. 2.4.5: Atomic force microscope picture of diamond turned aluminum samples. The rms roughness is equal to 1.2 nm for this sample despite some local tip as high as 37 nm.

Metal photocathodes can also be produced by growing thin films on a substrate. Pulsed laser depositions of thin films of Mg and Y have been deposited on a copper substrate [31] and exhibited QE similar to bulk cathode. The uniformity and roughness of the obtained films remain however difficult to control. Magnetron sputtering of Cu and Nb thin films deposited on Si substrate exhibited QE values similar to those obtained with bulk materials [14].

### Incident photons

The QE performance of a photocathode is related to the illuminating light through three parameters present in eq. 2.2.1:

- the wavelength which determines the energy of the incoming photons

- the reflectivity coefficient R

- the electric field component of the incident electromagnetic wave (in the case of large power density with a strong electric field component)

The dependence of the QE on incident photon energy is illustrated in Fig. 2.3.4. QE is increasing with the photon energy because electrons from energy states deeper below the maximum of the conduction band can then be excited above the barrier of potential.

If the power density of the incident photon beam is sufficiently large (~ 1W/m2) like with strongly focused laser beam or ultra-short pulses, two or more photons can be absorbed at the same time by the same atom: multi-photon photoemission. In such process, photoemission of electrons with photon energy smaller than the work function becomes possible. The dependence of the extracted charge versus the illuminating power will deviate from a linear behavior in case of multi-photon photoemission. For two photon absorption the extracted charge is proportional to the square of the laser power density and for n-photon photoemission the charge goes with the illuminating intensity at the power n [32]. Multi-photon photoemission can even become more efficient than single photon emission to extract a given charge if one considers the necessary laser power needed for frequency doubling or tripling.

The quantum efficiency changes with the polarization of the incident light: the vectorial photoelectric effect [33]. QE can vary by several factors with the incidence angle of p polarized photons as it is almost constant for s polarized photons [34]. Evidence of QE enhancement using z polarized laser light (electric field component in the direction of propagation) were also demonstrated [35]. In such scheme, it is the electric field applied to the cathode which is enhanced by the z component of the incident light.

Photoemission can always be enhanced by using the electric field component of the illuminating wave in order to lower the work function. This is the so called optical field emission. This can be illustrated with experiments were quasi half cycle THz pulses have been used to extract charge from a cathode surface [36]. In Fig. 2.4.6, a THz half cycle with sufficiently high peak electric field (hundreds of MV/m [37]) could trigger field emission of electrons with a charge close to one pC [38].

Fig. 2.4.6: A quasi half cycle THz pulse is used to trigger the field emission from a ZrC tip. The current pulse time structure is limited by the scope bandwidth but should in principle follow the THz half cycle.

### Surface Electric Field:

The electric field applied to the cathode surface is an important parameter for the photoemission process since it lowers the barrier of potential that electrons have to cross to be emitted. This barrier lowering is known as the Schottky reduction ΔФ. This effect becomes significant for electric field above a few tens of MV/m which lowers the barrier by a few tenths of eV.  The reduction of the barrier of potential can be expressed by the following expression:

∆Ф=e3F4πε0	(eq. 2.4.3.1)

with e the elementary charge, F the local electric field on the surface and ε0 the electric constant.

The local electric field F can be higher than the applied electric field because of enhancement effect due to the morphological imperfections on the surface (see Fig. 2.4.5). In extreme case where the electric field is also enhanced by geometric effect above a few GV/m, field emission can take place. Indeed when the barrier of potential is sufficiently low and then also thin, the electrons from the conduction band can start to tunnel through the barrier.

It exists an intermediate state where the barrier still prevent too strong field emission but where almost all incident photons will lead to electron emission, that is to say when the QE is equal to 1 or above. This was observed when sharp tips were illuminated by UV laser pulses while high voltage was applied to the tip as illustrated in Fig. 2.4.3.1.

Fig 2.4.3.1: Top: Emitted current pulse when only a nanosecond long voltage pulse is applied (pure field emission); Bottom: Current pulse when a voltage pulse (ns) and a laser pulse (ps) are simultaneously applied. The cathode is here a ZrC tip. [39]

This so called photo-assisted field emission or photo-field emission can be unstable since the local electric field at the apex of the tip is close to the field emission threshold and thus close to the electric field beyond which electrical breakdown occurs. One way to prevent arcs consists in using very short voltage pulses applied to the cathode and short laser pulses to trigger short pulses of photoemission superposed to the field emission pulse. If the voltage pulses are short enough (nanosecond range) the joule effect related to the electron emission is limited and the risk of arcs is limited. In the experiment of Fig. 2.4.3.1, voltage pulses of about 2 ns FWHM and 50 kV amplitude where applied to a ZrC tip having an apex radius of curvature of a few micrometers.

High applied electric field is also desired in photocathode system to overcome space charge screening effect near the cathode. Indeed, the photocathode current can be limited by the quantum efficiency of the cathode but also by a too weak extracting electric field. The electric field under which the electron emission starts to saturate is equal to the beam surface charge density σ over the vacuum permittivity: ESC=σ/ε0. For example, for a short electron emission pulse of 6 ps duration the maximum current which can be extracted from one square millimeter with 50 MV/m is about 70 A.

@John: Maybe here you could add a section 2.4.4 on Superconducting metal photocathodes unless you feel that what is in the theoretical part is enough.

# PEA Semiconductors

## Introduction

Alkali metals are very reactive metals that do not occur freely in nature. These metals have only one electron in their outer shell. Therefore, they are ready to lose that one electron in ionic bonding with other elements. Telluride is a metalloid (quasi-metals) which will react with alkali metals to form a most stable compound. Among the alkali photocathodes, Cs2Te is one of the most widely used compounds because of its relatively long lifetime (up to years) and high QE compared to other semiconductor photocathodes.

There are more than 20 different semi-conductor materials that have been developed, especially for the photo-multiplier technologies, in order to cover the largest bandwidth of the spectrum (Fig. 3.1.1). In this section we will focus on Cs2Te photocathodes.

Fig. 3.1.1: Overview of semi-conductor photocathodes QE values versus the wavelength of the illuminating photons (source: Hamamatsu [40]).

## Preparation and performances of Cs2Te photocathodes:

### Preparation methods

Semi-conductor photo-cathodes are produced by the deposition of thin-films on a massive substrate. For Cs2Te photocathodes, the thin films are usually obtained by thermal evaporation of tellurium Te and cesium Cs [8]. The substrate (Al, Au, Cu, Mg, Mo, Stainless Steel, …) has an influence on the performance of the photocathode since bulk materials atoms can diffuse in the thin film. For example Cu atoms will diffuse much deeper in tellurium than would do molybdenum [41]. As a consequence, betterQE results and longer lifetime were obtained with molybdenum substrates.

The thickness of the evaporated Cs2Te layer varies between a few nm and a few hundreds of nm. The evaporation can be either done in two steps by first evaporating a layer of Te and then a layer of Cs. The Te comes first since it will stick better to the substrate as would do the Cs. The Cs will then react with the deposited Te atoms to form various compounds (Cs2Te, Cs2Te5, Cs3Te2, Cs2Te3, Cs4Te) [42]. This successive evaporation lead typically to QE values around a few percent [43,44] in comparison to almost 20 % when the Te and Cs are co-evaporated [45]. The co-evaporation technique consists in evaporating the Te and Cs simultaneously so that Cs2Te molecules form in the gas phase before deposition on the cathode surface. This technique requires a careful monitoring of the QE together with a control of the Cs flow to reach the best stoichiometry. Figure 3.2.1 illustrates the evolution of the cesium source evaporation current while monitoring the photocurrent (which here corresponds to the QE) and for a quasi-constant tellurium evaporation rate of 0.03 A/s. The Cs evaporation rate is constantly adjusted to maximize the photocurrent rise. The deposition is stopped when the photocurrent starts to decrease.

Fig. 3.2.1: Evolution of the Cs evaporation current (related to the deposition rate) and collected photocurrent under constant illumination at 266 nm and while Te is deposited at 0.03 Å/s. Pressure rises to 10-8 mbar during deposition.

The tellurium growing process onto the substrate follows a Stransky-Krastanov [46] scheme. First Te atoms get deposited layer by layer up to a few monolayers and then isolated islands will start to growth until the coalescence of these adsorbate 'islands' takes place. This results in an almost smooth surface. The Cs growing process is a pure island type of growth where some nucleation sites are growing independently. The overlap of Cs on a Te layer produces a layer with a complex granularity which is a mix of the two processes described above: island and quasi smooth surface. The roughness is definitively larger than the one from the initial substrate.  In the case of the co-evaporation technique the roughness should be smaller than with the sequential technique [47]. This can have important consequences on the beam quality (uniformity, emittance).

Due to the very high reactivity of Cs with oxygen [41], the newly formed thin film of Cs2Te cannot be exposed to air and has to be stored in vacuum with pressure below, at least, 10-10 mbar. For this reason the semiconductor photocathode has to be transported in a vacuum suitcase and inserted to its final location via a load-lock chamber. The design of the vacuum system to produce and transport semiconductor photocathodes is extremely important and is usually the main cost driving factor in cathode production system.

One way to improve the uniformity of the produced layer is to heat the cathode sample during the deposition [48] to about 100 - 150 degree Celsius. Most probably the warm sample helps the spreading of the growing islands on the cathode surface. It also helps to keep the substrate clean since water is then desorbed from the surface and longer lifetime have been observed with such warm recipe [49].

### QE values of Alkali based cathodes - Cs2Te:

The absolute value of QE reachable with Cs2Te has to be discussed together with lifetime since the very high values (above 10 % at 260 nm) reported in the literature usually last only for a few hours of operation.

Table 3.2.2.1 summarizes the QE values obtained with alkali metal cathodes tested in similar conditions in different laboratories. QE values as high as 20% were reached but the decay time is exponential with a lifetime constant T1/τ of only a few hours, after that the decay is still exponential but with a much longer time constant. Then for most of the reference the Cs2Te photocathode could hold a QE above 1 % for at least several months depending on the level of vacuum and the amount of charge extracted.

| Material | Substrate | QE at λ | Lifetime | Field (MV/m) | Operating vacuum (mbar) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| CsI-Ge |  | 0.73 % at 213 nm 0.13% at 266 nm | T1/τ > 1 year | 70 |  | [8] |
|  |  | 2% at 209 nm | T1/τ > 150 h |  | 10-10 -10-9 | [50] |
| Cs3Sb | Cu | 7.5% at 532 nm | > 1% over 30 h | 7 | 10-10 | [6,45,51] |
|  | Cu | 4.9% at 532 nm | > 1% over 30 h | 85 | 10-10 | [51] |
|  |  | 4 % at 527 nm | T1/τ < 4 h | 20 | 10-10 -10-9 | [50] |
| K3Sb |  | 1.6 % at 266 nm |  |  |  | [8] |
|  |  | 0.3% at 541 nm |  |  |  | [52] |
|  |  | 1-3 % at 262 nm |  |  |  | [8] |
| K2CsSb |  | 8 % at 527 nm | T1/τ < 4 h | 20 | 10-10 -10-9 | [53] |
|  |  | 1.2 % at 541 nm | T1/τ < 24 h |  |  | [52] |
| Cs2Te | Cu - Au | 16 % at 262 nm | 450 h above 1.5 % | 100 | 1 -5.10-9 | [54] |
|  | Cu -Au | 2 – 8 % at 262 nm | Few weeks > 1.5 % | 120 | 1 -5.10-9 | [45] |
|  | Cu | 20% at 266 nm | 300 h above 3% | 120 | 10-9 | [45] |
|  | Mo | 20% at 262 nm | 200 days above 4% | 35 - 40 | 10-10 | [55] |
|  |  | 15.5 % at 263 nm | 1 month above 1 % |  | 5*10-8 | [56] |
|  | Mo | 16-18 % at 251 nm 8 -12 % at 263 nm | > 1% over 100 h | 20 - 25 | 10-10 | [50] |
|  |  | 15- 20 % at 266 nm |  |  | 10-9 | [57] |
|  |  | 8 - 15% at 266 nm | > 1% over 420 days |  | 10-9 | [58,59] |

Table 3.2.2.1: Overview of QE of alkaline metals measured in different laboratories with slightly different conditions based on the table from [60] updated with some more recent results.

In comparison to the typical QE of metallic photocathodes, even a QE of 0.1 % remains a large value. And if such QE can be maintained over many months of operation, then it becomes an interesting candidate for many applications [61]. Figure 3.2.2 summarized the time evolution of the QE for several copper and Cs2Te photocathode samples operated all in the same RF photoinjector (same experimental conditions). Both photocathodes material undergo a degradation of the QE with time but in average Cs2Te has QE one order of magnitude larger than copper for at least 100 days. The total amount of extracted charge for the sample Cs2Te_17 was 3 mC without major sign of degradation.

Fig. 3.2.2: Evolution of the QE with time of various copper and Cs2Te samples operated in the same conditions: Extracting field: 52 MV/m; 262 nm; laser pulses of 4 ps rms at 10 Hz repetition rate, 10-9 mbar.

## Sensitivity to vacuum

As already mentioned above, the main drawback of semiconductor photocathodes over metallic ones is their high sensitivity to oxygen [41]. The poisoning of the cathode surface can affect the lifetime of the cathode but also the uniformity of the photoemission. A current way to measure the uniformity of the emission consists in scanning a small laser spot over the entire emitting area and record the QE at each position, to obtain a QE map.

The QE maps of Cs2Te photocathodes can present non uniformities as shown in Fig. 3.2.3. Such non-uniformities are not good for the beam quality and might be related to the deposition procedure.

Fig. 3.2.3: QE map of a Cs2Te cathode measured in the gun by scanning small laser spots with constant energy.

The lifetime is always an important criteria for semiconductor photocathodes. The degradation comes mainly from O2 and CO2 [41,62].

!!!!@ John: Here you may want to add your figure on the Oxygene pollution effect … .

Fig. 3.2.4: Typical lifetime of a Cs2Te photocathodes used in an RF photoinjector: Illumination: Trains of 2400 laser pulses of ps duration in 800 μs at 10 Hz, 262 nm; 40 MV/m, 700 pC / pulses (source: [55])

Figure 3.2.6 shows the typical lifetime of Cs2Te photocathodes in the operating conditions of an RF photoinjector at the Free Electron Laser (FEL) FLASH in Germany. A cathode is lasting typically between one and six months depending on the operating pressure and produces up to 10 μC / s continuously and up to 1 C in six months [63].

## Alkali-Antimonide photocathodes:

The most common photocathodes in vacuum emissive devices come from the alkali antimonide family. This includes most image intensifiers (night-vision), and low light detectors (photomultiplier tubes). These materials typically consist of 3 alkali and one antinomy per molecule, and some cathodes (such as the S-20) use multiple layers of differing composition. Commonly used cathodes of this family include Cs3Sb, K2CsSb, Na2KSb, and (Cs) Na2KSb (S20), though others are used as well. For accelerators, this class of materials holds the average current record for both DC and RF photoinjectors [J3,J4]

### Preparation methods and film properties

Several sources have been used to provide alkali materials for growth, including thermal evaporation from sealed sources [J3], chromates [J5], alkali azides [J6], pure alkali metal effusion sources. In most of these cases, antimony is provided via thermal evaporation, either from Sb pellets in a crucible or from Sb (or PtSb alloy) wire sources. Recently sputter growth of C3Sb and K2CsSb has also been demonstrated [J7]. Vacuum is critical in alkali antimonide growth – these materials degrade quickly in a partial pressure of water over 0.1 nTorr. However, the cathodes are relatively insensitive to most other gasses – alkali antimonide cathodes are routinely operated in gas electron multiplier-based detectors at ambient pressure of Ar & CH4.

The structure of an alkali antimonide film is a strong function of whether the growth is sequential (Sb-K-Cs, for example), or via co-deposition/sputtering. Traditional growth has involved sequential deposition of Sb, followed by the weakly bonded alkali, followed by the strongly bonded alkali (typically Cs). This results in a good QE, but the lattice mismatch between crystalline Sb [J8] and the cubic alkali antimonides results in significant roughening of the surface (up to 25 nm RMS for a 50 nm thick film [J9]).

Co-evaporation of Sb and the alkalis avoids this recrystallization, and results in a far smoother film [J10,J11]. It has also been shown to dramatically improve the lifetime of cathodes for detector applications [J12]. It is, however, significantly more difficult to control. These methods have resulted in surfaces with RMS roughness of under 1 nm.

Sputter growth produces films that are largely amorphous but very smooth (RMS ~0.5 nm for a 50 nm film). These films have lower QE (typically 16-20% peak, and 4% in the green, as compared to 30% and 8% for sequential and co-evaporated cathodes), but are easy to produce over large areas.

For many applications, the roughness of the cathode is not an important parameter, but for accelerators it has a dramatic impact on the source emittance and achievable brightness [J13]. It is also important for detector applications which use high electric fields.

# NEA Semiconductors: GaAs based photocathodes for polarized electron beams

## Overview GaAs

Polarized electron beams play a critical role in nuclear and high energy physics research, including parity-violating electron scattering experiments and the measurement of nucleon spin structure functions [ref].  And as recently demonstrated, spin-polarized electron beams can be used for magnetization-sensitive imaging [ref]. The first polarized electron source for an accelerator, based on photo-ionization of state-selected 6Li atoms, was developed at Yale University in the early 1970s for use at the Stanford Linear Accelerator (SLAC) [3].  Later, a polarized electron source based on the Fano effect in Rb was developed for the Bonn synchrotron [4].  Other polarized sources were developed or proposed during the 1970s, including an improved version of the Li photo-ionization source [5], a source based on the chemi-ionization of metastable He atoms [6], and sources using the Fano effect in Cs [7].  None of these latter sources were ever developed to the point of being operational at accelerators.  Following the 1974 demonstration of polarized photoemission from GaAs [8] at low voltage, a high voltage source was constructed at SLAC [9] to conduct the seminal parity violation experiment E122 [10] that verified predictions by Wienberg and Salam and thereby helped to establish the Standard Model of electro-weak physics.  Shortly thereafter, polarized electron sources using GaAs photocathodes with an NEA surface condition were constructed at MIT-Bates [ref], the Mainz Microtron [ref], Bonn-ELSA [ref], Nagoya University [ref] and CEBAF-Jefferson Lab [ref].

Photocathode QE and electron spin polarization (ESP) are important characteristics of GaAs photocathodes.  For decades, photocathode experts have worked to increase these quantities.  The QE of GaAs photocathodes is affected by many factors including cathode material quality, the wavelength of the incident light, the thickness of the photocathode, dopant density, the temperature of the photocathode, surface contamination, the negative-electron affinity condition on the photocathode surface, the power density of the laser light, the bias voltage (i.e., Schottky Effect) and the vacuum pressure under which photo-extracted beam is produced. These factors also affect ESP via spin relaxation/depolarization mechanisms that influence conduction-band electrons migrating toward the surface of the photocathode, and then emitted into vacuum.  This section provides an overview of polarization and ion bombardment, which is the chief lifetime-limiting factor of the NEA GaAs photocathode inside a high voltage photogun.

GaAs is a direct-transition III-V semiconductor with zincblende crystal structure [18, 19].  It can absorb laser light across the broad visible spectrum but only illumination with near-IR wavelengths provides polarized photoemission.  This can be understood by looking at detailed and simplified representations of the energy level diagrams of GaAs (Figure X).  Electron spin-orbit coupling splits the P1/2 and P3/2 energy levels of the valence band into two states separated by 0.33eV, which is large enough to avoid optical pumping from the lower energy P1/2 state.  Polarized photoemission takes advantage of the quantum mechanical selection rules, noting that for circularly polarized laser light, conservation of angular momentum requires an electron’s spin-angular momentum quantum number to change by one unit, mj = +/- 1.  Furthermore, some transitions are more favorable than others as indicated by the transition probabilities shown in Fig.1 (right).  By using circularly polarized laser light with near-bandgap energy, the conduction band can be preferentially populated with a particular spin state. Polarization is defined as P=N↑ -N↓N↑ +N↓  where N refers to the number of electrons in the conduction band of each spin state, “up” or “down”.  For bulk GaAs, the theoretical maximum polarization is 50%, corresponding to three electrons of the desired spin state for every one electron with opposite spin.

Figure 4.1.1: (left) Energy level diagram of GaAs at the center of the Brillouin zone: a “close-up” view near the valance band maxima/conduction band minima, and (right) simplified view showing the optical transitions between sublevels for right circularly polarized light (solid lines) and left circularly polarized light (dashed lines),  with relative transition strengths given by circled numbers

As discussed previously for other photocathodes, the emission of electrons from GaAs can be described as a three-step process [31] involving absorption of light, diffusion of electrons to the surface of the photocathode, and emission of the electrons into the gun vacuum chamber. However, it is worth mentioning two aspects of efficient photoemission that are unique to GaAs.  Namely, efficient photoemission from GaAs requires that the material be p-doped [8], which serves to lower the Fermi level throughout the material.  The p-doping also serves to lower the conduction band at the surface of the photocathode, which in turn lowers the electron affinity (EAeff in Figure 3b).  Secondly, no significant photoemission is obtained until the potential barrier is reduced further and this is accomplished by adding a ~ mono-layer of cesium and oxidant (Figure 3c).  The process of adding cesium and oxidant to the photocathode surface to create the desired NEA condition is called “activation”.

Figure 4.1.2: Energy level diagrams describing the formation of the negative electron affinity (NEA) condition on GaAs.  Ecb, EF, Evb, and E∞ describe the conduction band energy, the fermi level, the valance band energy and the vacuum energy level, respectively.  EA and EAeff  refer to the electron affinity which is related to the surface work function.  Vdipole is the decrease of vacuum level caused by activation layer (CsF)  (a) Intrinsic GaAs (b) p-type dopant lowers the Fermi level which leads to band bending at the surface (c) adding a CsF layer lowers the surface potential barrier and leads to further band bending, and the desired NEA condition.

At room temperature, highly doped bulk GaAs photocathodes typically provide ESP of the order ~ 30%, a value considerably less than the theoretical maximum value of 50%.  The investigation of spin relaxation and depolarization has a long history dating back to the 1950s [64][65][66].  Literature describes two main spin relaxation mechanisms for p-type III-V semiconductors: 1) the lack of inversion symmetry in III-V semiconductor leads to a spin splitting of the conduction band, called the D’yakonov-Perel (DP) mechanism, [67] and 2) the exchange interaction between electrons and holes, called the Bir-Aronov-Pikus (BAP) mechanism. [68] As described below, for p-type GaAs, the BAP mechanism dominates with the DP mechanism playing a role at high temperature and low dopant concentration [69][70]. There are other depolarization processes, but these are typically considered to have little consequence and are frequently ignored.  These include the Elliot-Yafet (EY) mechanism [71][72] in which the spin–orbit interaction generates non–pure spin states in the conduction band, and radiation trapping, in which ESP is diluted by supplemental photoemission that results from the absorption of linearly polarized recombination light. There is a wealth of literature describing polarization studies using bulk GaAs, as a function of temperature [73][74][75], dopant concentration [74][73][75], electron (and hole) density [76], and thickness of the photocathode [64].  In sections below, recent measurements are summarized describing ESP sensitivity to sample temperature and Zn dopant density, which have a significant impact on ESP.  In general, ESP can be increased at the expense of QE.

## Theory: Spin relaxation mechanisms

Electrons in the conduction band will arrive at an equilibrium polarization when the photocathode reaches a steady-state condition defined as, dP/dt=P0/τ-P/τ-P/τ0=0. The term P0/τ is the rate of polarization creation using circularly polarized light, P/τ describes polarization loss due to electron recombination to the valence band, and P/τ0 is the rate at which polarization disappears due to spin relaxation effects. So the equilibrium polarization is given by:

P=P011+ττs			           				(1)

where P0 is the initial polarization determined by the quantum mechanical selection rules (as mentioned above, P0=50% for bulk GaAs), τ and τs describe the electron lifetime and spin relaxation time for electrons at the bottom of the conduction band, respectively. The electron lifetime τ of GaAs is of the order 10-9 to 10-10 s, with the exact value dependent on the temperature and doping concentration of the sample. The cumulative spin relaxation time is composed of individual spin relaxation mechanisms given by, 1τs=1τsDP+1τsBAP+1τsEY+ 1τsrad, where the superscripts represent the different spin relaxation mechanisms mentioned above.  For p-type GaAs, the terms related to the EY mechanism and radiation trapping can be neglected.

The lack of inversion symmetry in GaAs is due to the presence of two distinct atoms in the Bravais lattice, such that the momentum states of the spin-up and spin-down electrons are not degenerate: Ek↑≠Ek↓. The resulting energy difference plays the role of an effective magnetic field and results in spin precession during the time between collisions, which contributes to spin relaxation because the magnitude and direction of k changes in an uncontrolled way. This is the so called DP mechanism, and the spin relaxation rate is given by [67,77] :

1τsDP=Qτpα02kBT3ℏ2Eg						(2)

where Q is a dimensionless factor and ranges from 0.8 to 2.7 depending on the dominant momentum scattering mechanism, τp is the momentum relaxation time, α0 is a dimensionless parameter specifying the strength of the spin-orbit interaction (α0=4∆memevEg+∆3Eg+2∆12, here meis the effective mass of the electron, mev is a constant close in magnitude to the mass of the free electron[74]) and Eg is the bandgap of GaAs. The temperature dependence of the spin relaxation rate is 1/τsDP~T3τp~T9/2. [74]  xi

In p-type GaAs, spin relaxation can result from the spin exchange interaction between electrons and holes. This is the so-called BAP mechanism, and the spin relaxation rate is given by two terms. [68][77] In case of exchange with nondegenerate holes:

1τsBAP=2τ0NAaB3vkvBNhNAψ(0)4+53NA-NhNA				(3)

where τ0 is an exchange splitting parameter given by 1τ0=3π64Δex2ℏEB (with Δex is the exchange splitting of the excitonic ground state and EB=ℏ22meaB2 is the Bohr exciton energy), aB=ℏ2ϵe2me is the Bohr exciton radius, vk is the electron velocity, vB=ℏmeaB is the Bohr exciton velocity, Nh is the density of free holes, and ψ(0)2 is the Sommerfeld’s factor.

In the case of exchange with degenerate holes and when the electron velocity  vk is greater than the Fermi velocity of the holes, the spin relaxation rate is given by: [77]

1τsBAP=3τ0NhaB3vkvBkBTEf						(4)

where Ef is the hole Fermi energy. If the electrons are thermalized, vk needs to be replaced by the thermal velocity ve=3kBTme1/2.

The temperature dependence of τsBAP is dominated by the temperature of ψ(0)2 as well as by the density of free holes Nh. The dependence on the acceptor density is essentially 1/τsBAP~NA for nondegenerate holes from Eq. (3) and 1/τsBAP~NA1/3 for degenerate holes from Eq. (4). In between these regimes, 1/τsBAP is only weakly dependent on NA.  In this paper, measurements of ESP as a function of sample temperature and dopant density serve to validate these assumptions.

The formulas cited above (Eqs. 2, 3 and 4) were used to calculate the spin relaxation rate as a function of temperature for bulk GaAs with dopant concentrations 1×1019 cm-3 and 5×1017 cm-3, as shown in Figure 3. The BAP mechanism clearly dominates over the DP mechanism, which contributes appreciably only at higher temperature.  The clear message from this plot is that low spin relaxation rates - and therefore higher ESP – will be obtained at lower dopant densities and temperatures.

Figure 4.2.1: Temperature dependence of the spin relaxation rate for the DP mechanism, BAP mechanism and the total value in bulk GaAs.

## Recent Measurements with GaAs NEA Photocathodes

### Bulk GaAs Polarization Study - Temperature and Zn dopant dependence

In a recent work [ref], three bulk GaAs photocathodes, each with 100 surface cleave plane but with dopant densities spanning roughly 1.5 orders of magnitude, were activated at room temperature and evaluated using a retarding field Mott-polarimeter apparatus [ref].  Photocathode QE and ESP were measured as a function of illumination wavelength, first at room temperature and then with a sample holder filled with dry ice (195 K) and LN2 (77 K). The QE and ESP spectral scans presented in Figure 4 exhibit the typical shape for bulk GaAs, namely ESP increases while QE decreases as the energy (wavelength) of the illumination light is decreased (increased), with the highest polarization obtained when the energy of the light is equal to the semiconductor bandgap ensuring that only electrons from the P3/2 ground state are excited to the conduction band.  More interesting is the effect of dopant density on QE and ESP.  Higher dopant concentrations serve to increase band bending, which lowers the surface work function, which increases the electron escape probability and leads to higher QE, however at the expense of polarization.  For the commonly used dopant density of 1019 cm-3, photocathode QE at room temperature reached ~ 6.9% but provided a maximum ESP of only ~ 30%.  Polarization increased to ~ 41% for the low-doped sample but provided QE of only ~ 1.5%.  This behavior is consistent with predictions of the BAP mechanism that describes the spin relaxation rate proportional to the dopant concentration.  Higher dopant concentration leads to greater spin relaxation rate, and thus lower ESP.

Cooling the samples to 77K modifies the crystal lattice structure and shifts the bandgap energy [78].  This bandgap shift means peak polarization occurs at higher photon energies. The bandgap energy for GaAs can be calculated using EgT=1.519-5.41×10-4T2T+204, which yields bandgaps of 1.51 and 1.42 eV for samples at 77 and 300 K, respectively.  Only the 77 K bandgap “knee” is visible in the QE spectral plot of Figure 4 (top right).  More noteworthy is the significant increase in ESP observed for all three samples cooled to 77 K.  The ESP for the highly-doped sample increased from ~30 to 41%, and from ~ 40 to 52% for the low-doped sample. This behavior is consistent with Figure 3 which predicts smaller spin relaxation rates for both mechanisms (BAP and DP) at lower temperature.  For the low-doped sample at 77 K, measured polarization exceeds the theoretical maximum value of 50%.  This could point to an inaccurate effective Sherman Function used in the Mott polarimeter analysis, with this measurement serving to identify the magnitude of systematic error relevant to the entire study, or perhaps an indication of interesting physics phenomenon, e.g., the creation of strain within the sample at cryogenic temperature, which serves to eliminate the energy level degeneracy of the P3/2 ground state.

Figure 4.3.1.1: The QE and ESP of bulk GaAs (100 cleave plane) with different Zn dopant densities, and measured at 300 K (left) and 77 K (right).  Error bars are statistical. Axes ranges were kept identical to highlight the measurement variations observed between conditions. The bandgap energy Eg could be discerned for samples at 77K (note arrow).

The temperature and dopant density studies are summarized in Figure 5, which shows ESP versus temperature for the three samples with different dopant concentrations. Overall, lower temperature leads to lower spin relaxation rate, and therefore higher ESP.  Fits were applied to the data sets using the sum of Equations 2 and 4, which describe the DP and BAP spin relaxation mechanisms, respectively. The fit to the high dopant sample set is quite good, and less so for the lower dopant density results, although the fits still support the basic predicted trend.

Figure 4.3.1.2: Maximum ESP versus sample temperature and dopant density (the wavelength of illumination was allowed to vary to provide peak polarization). Fits were applied using the sum of Equations 2 and 4 which describe the DP and BAP spin relaxation mechanisms, respectively. Vertical error bars are statistical. Horizontal error bars are attributed to uncertainty in sample temperature.

### High Polarization Strained-Superlattice Photocathode with Distributed Bragg Reflector

GaAs photocathodes grown on a crystal structure with a different lattice constant can provide beam polarization exceeding 50% because of induced uniaxial strain that eliminates the degeneracy of the P3/2 valence band.  The first demonstrations of this technique were reported in 1991 using photocathodes grown with a single strained layer [TN1991, TM1991]. Throughout the 1990s, single-strained-layer GaAs/GaAsP photocathodes [Bandwidth, Japan and Russia] were used at electron accelerators throughout the world [SLC, CEBAF, MIT-Bates, Bonn ELSA, Mainz Microtron, NIKHEV] providing polarization 75%-80% and maximum QE ~ 0.3% or less. But beam delivery using single-strained-layer photocathodes made apparent the delicate competing balance between maintaining the required strain, and growing a layer thick enough to provide sufficient QE.  In the following decade, higher polarization and notably higher QE were obtained using strained superlattice structures consisting of very thin quantum-well active layers and alternating lattice-mismatched barrier layers. The superlattice structure maintained the required degree of strain to produce high polarization and also provided sufficient active layer thickness to obtain higher QE. The first demonstration of beam production from a strained GaAs/In0.15GaAs superlattice photocathode in 1994 achieved polarization of 82.7% but QE of just 0.015% [TO1994] however, continued development eventually resulted in photocathodes with QE ~ 1%.  The strained GaAs/GaAsP0.36 superlattice structure reported in ref. TM2004 provided QE of 1.2% with polarization of 86% and is available commercially [SVT]. Strained superlattice photocathodes fabricated at other facilities have also demonstrated very high polarization but no higher QE [YA2006, YA2008, XJ2013, XJ2014].

Some new accelerator applications require very high average current polarized beams [PEPPo, and eRHIC].  A photocathode with a QE of only 1% would require ~ 8 W of laser light (with RF structure) to generate the desired 50 mA average beam current for the eRHIC proposal21 and even more light when QE decays during operation due to ion-bombardment22. In the standard strained superlattice design, most of the incident laser light simply heats the photocathode instead of promoting electron ejection, which can degrade QE due to evaporation of the chemicals used to reduce the surface work function.23  Methods to cool the photocathode during beam delivery are complicated because the photocathode floats at high voltage.  Developing photocathodes with enhanced QE could simplify the photogun design, reduce the drive-laser power requirements and prolong the effective operating lifetime of the photogun.

A photocathode with a distributed Bragg reflector (DBR) was first proposed in 199324 and reported in following years25,26 as a means to enhance photocathode QE. The DBR serves to create a Fabry-Perot cavity formed by the front surface of photocathode and a DBR region existing beneath the superlattice active layer.  Instead of a single pass in the standard design, laser light of a particular wavelength reflects repeatedly within the Fabry-Perot cavity which increases the beneficial absorption of the incident photons, and in principle, leads to enhanced QE.  From past work, it was clear that the wavelength of peak reflectivity of the DBR was very sensitive to the refractive indices and thickness of each DBR layer constituent, and that the peak of resonant absorption was very sensitive to the thickness of the photocathode, especially the spacer layer between the DBR and the superlattice photocathode structures.  Accurate control of the thickness of each layer and of the composition of each constituent chemical within the photocathode structure represents a significant challenge.

A recent DBR study [ref] benefited from past work that resulted in the fabrication of the strained GaAs/GaAsP superlattice photocathode described in ref. 15, which represents the basis for polarization and QE comparison.  See ref. 15 for a complete description of the design criteria and optimization of this photocathode structure.  A schematic layout of the strained GaAs/GaAsP superlattice photocathodes with and without DBR structure is shown in Figure 1.

FIG. 1. Schematic structure of the photocathodes: without DBR (left) and with DBR (right).

The DBR was composed of multiple layers of alternating high and low index of refraction.  A natural choice for high index of refraction layer was GaAsP which provides a good lattice match to the graded buffer layer. Though a challenge for growth, we chose AlAs1-yPy for the low index of refraction layer for maximum refractive index contrast and minimum DBR thickness. The thickness of each layer follows the quarter wavelength condition:24 nHλDBRdH=λDBR4=nL(λDBR)dL. The bandwidth for which the DBR exhibits high reflectivity is given by the formula:

∆λDBR=4λDBRπsin-1(nH(λDBR)-nL(λDBR)nH(λDBR)+nL(λDBR))                                                          (1)

The Fabry-Perot cavity is formed by the vacuum/GaAs cap layer interface and the DBR.  Proper thickness of a GaAsP spacer layer between GaAs/GaAsP superlattice and the DBR ensures the maximum absorption in superlattice active layer coincide with the central reflective wavelength of the DBR. To design the structure, the refractive index of these layers can be estimated using the simplified interband transition model as a function of photon energy28:

n(E)2=AfX0+12E0E0+∆032fXso+B					(2)

with fX=X-2(2-1+X-1-X), X0=EE0, and Xso=EE0+∆0. Here, A represents the strength parameter of the E/(E0+∆0) terms and B represents the nondispersive contribution arising from the higher-lying band gap terms (E1,E1+∆1,E2,etc.) for each layer. The quantities E0 and ∆0 are the band-gap energy and spin-orbit splitting, respectively, given by Vegard’s Law for GaAs1-xPx29,30.

The desired wavelength of peak reflectivity was λDBR ~ 780 nm, compatible with CEBAF drive lasers.  Setting the phosphorus fractions in the GaAs1-xPx and AlAs1-yPy layers to 0.35 and 0.4, respectively, provided refractive indices of nH780nm=3.4506 and nL780nm=2.9443. From these parameters, the design values for the thickness of the GaAsP0.35 and AlAsP0.4 layers were 56.5 nm and 66.5 nm, respectively. Actual layer thicknesses were very close to these design values, 54 nm and 64 nm, which set the wavelength of peak reflectivity to λDBR of 755 nm, and the reflectivity bandwidth  ∆λDBR ~79 nm. This implies the DBR can achieve a high reflectivity > 90% for wavelengths between 715 and 795 nm.

The transfer matrix method 32,33 was used to calculate the reflection, transmission and absorption of incident light through the complete multilayer thin-film structure including the GaAs substrate. Calculated values of surface reflectivity (R), transmittance (T) into the GaAs substrate, absorption (A), and the absorption enhancement factor as a function of wavelength, are shown in Figure 2. There are two resonant absorption peaks within the optical cavity for the DBR photocathode at wavelengths 726 nm and 776 nm.  Absorption by the substrate is not plotted as this process does not contribute to the polarized electron emission.  The resonant peak at 776 nm is just 4 nm from the desired value 780 nm. At 776 nm, the absorption is 21.03%, surface reflectivity is 50.14%, and transmittance into GaAs substrate is 28.83% for the DBR photocathode, corresponding to maximum electron spin polarization. The full-width half-maximum of the Fabry-Perot resonance is about 10 nm at 776nm. The absorption enhancement factor is 7.4 at this wavelength.

To estimate the quantum efficiency of photocathode, one can solve the one-dimensional diffusion equations, based on Spicer’s three-step model:34,35

QEλ=PLFLA1+1αλLL+PΓexp⁡[k(-11.42-λ1240)]A1+1αλLΓ[FΓ+FLLΓαλFL(LΓ+LL)(1+1αλLL)]			(3)

where PΓ and PL are the surface electron escape probabilities for the Γ and L minima, respectively, which are independent of the incident photon energy, FΓ is the remaining fraction of excited electrons, FL is the fraction of electrons that is excited to energies greater than the L minima, A is the absorption of photocathode, LΓ and LL are the electron diffusion length for the Γ and L minima, respectively, αλ is the absorption coefficient of the photocathode, and k is a coefficient (k≥0). The calculated QE for the DBR photocathode, together with the QE enhancement factor as a function of wavelength, are shown in Figure 2.

Fig. 4.3.2.1. Calculated values of absorption, reflectivity and transmittance of the DBR photocathode, as a function of wavelength. Also shown, calculated QE and the QE enhancement factor compared to the photocathode without the DBR.

Measured values of QE and polarization as a function of wavelength, for photocathodes with and without DBR, are shown in Figure 3a.  For the non-DBR photocathode, results are consistent with past work15 indicating peak polarization of 90% and QE of 0.89% at a wavelength ~ 780 nm.   In stark contrast, the QE of the DBR photocathode shows the telltale prominent oscillatory behavior indicative of resonant absorption. Measured reflectivity and QE enhancement (i.e., the ratio of QE values of photocathodes with and without DBR) are shown in Figure 3b. The two dips in the reflectivity spectrum are clearly correlated with wavelength locations of QE maxima. At the wavelength of interest, 776 nm, the QE was 6.4% and polarization ~ 84%.  The measured QE enhancement of ~ 7.2 is very close to the predicted value of ~7.4.

Fig. 4.3.2.2. (a) The QE and electron-spin polarization (ESP) for the strained GaAs/GaAsP superlattice photocathodes with and without DBR as a function of the wavelength; (b) Reflectivity and QE enhancement factor of DBR photocathode as a function of the wavelength. The dash line indicates the resonant position.

### Ion Bombardment – Cleave Plane Dependence

Ion back-bombardment represents the dominant lifetime-limiting mechanism of modern DC high voltage photoguns that rely on delicate NEA GaAs photocathodes.7,8 Ion back-bombardment is the process whereby residual gas within the cathode/anode gap is ionized by the extracted electron beam and attracted to the negatively-biased photocathode. Photogun experts speculate that ions strike the photocathode surface sputtering away the chemicals used to create the NEA condition, or they become implanted within the photocathode material knocking out atoms from the crystal structure and altering the energy band structure, or they serve as interstitial defects that reduce the electron diffusion length. All of these possibilities are problematic because the net result is reduced QE, which results in reduced operating lifetime of the photogun. Improving the vacuum within the photogun is the best way to reduce ion back-bombardment and thereby prolong the operating lifetime of the photogun, but modern DC high voltage photoguns are already operating in the 10-11 Torr pressure range, or lower, so improving the photogun vacuum further is thus very challenging.

To understand ion back-bombardment inside a photogun, it is important to note that the energy spectrum of the extracted photoemitted electron beam within the cathode/anode gap is broad, with electrons leaving the cathode electrode at zero velocity, and then gaining energy until reaching the anode.  For a typical DC high voltage photogun, the photocathode is biased at voltages between -100 and -350 kV.  Hydrogen is the dominant gas species inside a modern photogun, and the peak ionization cross section occurs at ~ 100 V and drops by more than two orders of magnitude at 100 kV8,13 (Figure 1). So under typical photogun operation, the surface of the photocathode is bombarded by significantly more low energy ions than high energy ions.

Fig. 4.3.2.3. Electron impact ionization cross section for hydrogen molecules - the dominant gas species inside modern DC high voltage photoguns - as a function of electron kinetic energy.

The software program SRIM (Stopping Range of Ions in Matter)18 can be used to estimate the penetration depth of the hydrogen ions into the material and the number of vacancies created within the material when ions collide with gallium and arsenic atoms and knock them out of their positions within the crystal lattice. In the simulation, the hydrogen ions were injected into GaAs at normal incidence and the ion injection energy was varied from 100 to 10,000 V while keeping the ion dose constant for each simulation.  The stopping depth of implanted hydrogen ions and the distribution of knock-out vacancies for different ion energies are shown in Figure 3.  Unsurprisingly, higher energy ions penetrate deeper into the material and do more damage to the crystal structure compared to lower energy ions.  The penetration depth (defined as the depth at which the dose falls to 1/e of its original value) is 69 Å and 1690 Å for 100 V and 10,000 V hydrogen ions, respectively, while gallium and arsenic atoms begin to be knocked out from their lattice positions at ion energies greater than ~ 500 V.  It is an interesting question, which ions are most problematic for NEA GaAs photocathodes inside a photogun, many low energy ions or fewer high energy ions?

Fig. 4.3.2.4. (left) Hydrogen ion distribution and (right) vacancy distribution within GaAs for different hydrogen ion energies. All simulations preformed using the same hydrogen ion dose of 8.1×105 nA∙s.  Plots obtained using SRIM.18

Channeling [ref] is the process whereby positively charged ions follow the direction between two neighboring crystal planes, which leads to deeper penetration of the positive ions in the material.  Figure 2 shows the relative spacing of atoms in the GaAs crystal structure for the three surface cleave planes studied, viewed at normal incidence.  The red boxes in Figure 2 denote the recurring geometric cells used for calculating the atomic number density which is a measure of the “open space” between atoms. The atomic number densities for the (100), (110) and (111A) GaAs cleave planes were calculated to be 8/a2, 42/a2, and 43/a2, respectively, where a is the GaAs lattice constant (5.6535 Å).  Measurements were performed to investigate if channeling would be enhanced for the (110) cleave plane which possesses the smallest atomic number density (i.e., the most open space between atoms).  If so, a photocathode with (110) surface cleave plane would therefore be the most insensitive to ion bombardment.

Fig. 4.3.2.5. Schematic representations of the GaAs crystal for three surface cleave planes, looking normal to the surface – from left to right, (100), (110) and (111). The red boxes denote the recurring geometric cells used for calculating the atomic number density for each cleave plane and a is the GaAs lattice constant.

To quantify the effects of ion energy, and to investigate whether crystal orientation plays a role in QE degradation, GaAs samples with different surface cleave planes were implanted with hydrogen ions at 100 and 10,000V.  Prior to implantation, each photocathode sample was heated, cooled and activated.  The QE was measured as a function of laser wavelength and the results are presented in Figure 6.  Quantum efficiency was calculated using the expression QE = 124IPλ,26 where I is the measured photocurrent in μA, P is the laser power in mW, and λ is the wavelength of the laser light in nm.  The cleave planes (100) and (110) provided the highest QE, approximately 21% at the laser wavelength 532 nm.  Cleave plane sample (111A) provided the lowest QE, approximately 19% at 532 nm.  Although these values are lower than reported in ref. 16, the relative trend between samples is consistent (i.e., QE100 > QE 110 > QE111A).

Fig. 4.3.2.6. Photocathode QE versus laser wavelength for commercial bulk GaAs samples with different surface cleave planes, prior to ion implantation.

After determining that each sample provided high QE, samples were heated to 250 °C for 20 minutes to remove the activation layer of Cs and NF3.  Samples were then cooled to room temperature and implanted with hydrogen ions at the chosen energy and for the prescribed dose. The vacuum was allowed to recover overnight.  Photocathode samples were then repeatedly heated and activated following different heating protocols (temperature and duration).  Following each activation, the photocathode QE was measured at 532nm and compared to the pre-implantation value.  In this manner, the sample’s sensitivity to ion damage was evaluated.   Figure 7 shows typical QE maps for samples implanted with 100 and 10,000 V hydrogen ions (the caption provides specific details of the cleave plane surface and heating protocol).  For 100 V ions, QE degradation was uniformly distributed across the sample.  But for 10,000 V hydrogen ions, the QE degradation was localized to a specific region of the sample, consistent with an electrostatic simulation that predicted significant focusing.

Fig. 4.3.2.7. Typical QE maps of the photocathode obtained by scanning a focused low power green laser beam across the photocathode following activation. These maps show the bulk GaAs (111A) sample. Left: after the third activation following implantation with 100 V hydrogen ions. Right: after the third activation following implantation with 10,000 V hydrogen ions.  The 2-dimensional plots help to illustrate ion implantation uniformity: 100 V hydrogen ions were uniformly distributed across the entire sample but 10,000 V hydrogen ions were focused to a region denoted by the red circle, consistent with the particle tracking code simulations.

Figure 8 summarizes the results of the experiment, with QE at 532nm plotted as a function of repeated activation following a variety of heating protocols described within the caption, for samples implanted with 100 and 10,000 V hydrogen ions, and for samples that were not implanted with ions.   When samples were repeatedly heated and activated – but not subjected to hydrogen ion implantation – the QE at 532 nm remained constant to within 5%.  This speaks to the quality of the vacuum within the apparatus, which was dominated by chemically inert gas species like H2, CH4, CO and CO2. The QE of each sample did not degrade following repeated heating and activation, due to adverse chemical reactions that might take place under degraded vacuum conditions, especially when samples were hot.

The next observation evident in Figure 8 is that both 100 and 10,000 V hydrogen ions served to degrade the sample QE, however the QE degradation associated with 10,000 V ions was significantly greater than that caused by 100 V ions.   In general, for both ion energies, heating the sample to higher temperature and for longer time served to restore QE.  For implantation with 100 V hydrogen ions, the QE could be completely restored by heating the sample. But for implantation with 10,000 V hydrogen ions, only a fraction of the QE could be restored.  It should be noted that data points presented in Figure 8 were obtained by averaging the QE measurements over a specific region of the photocathode sample surface. For 100 V ion implantation, QE measurements were averaged over the entire sample.   For the 10,000 V ions, QE values were averaged only in the region where the ions were focused, as indicated by the red circle shown in Figure 7 (right).

Fig. 4.3.2.8. QE versus heat cycle for bulk GaAs with three different surface cleave planes. Black Square: no implantation; Red Circle: implantation with 100 V hydrogen ions; Blue Triangle: implantation with 10,000 V hydrogen ions; Error bars represent the standard deviation in QE values averaged over the entire sample for “no implantation”: and 100 V results, and over the small region denoted by the red circle in Figure 7 (right) for the 10,000 V results.  Error bars are smaller than the data point symbols for “no implantation” and 100 V results because QE was very uniform across sample. Heat cycle number 1: 250°C for 20 minutes; 2: 370°C for 30 minutes; 3: 490°C for 1 hour; 4 and 5: 550°C for 1hour.

To determine if a specific surface cleave plane provided enhanced ion channeling, the QE results from the 10,000 V ion implantation studies were divided by the non-implantation QE results (Figure 9).  Per supposition, when ions penetrate deeper into the material, they pass beyond the surface region that contributes to photoemission and therefore provide less QE degradation.  When comparing QE values of implanted and non-implanted samples, those with the highest QE ratio would correspond to samples with enhanced ion channeling. The simple picture presented in Figure 2 suggests samples would be ordered (110), (111A) and (100), in terms of samples supporting the highest level of channeling to the least amount of channeling.  This simple picture is consistent with results presented in Figure 9, at least for samples that were heated sufficiently long and at a relatively high temperature (see results for heat cycles 4 and 5 in Figure 9).  The (110) GaAs cleave plane - i.e., the sample with the most “open space” between atoms, and therefore the sample supporting the highest level of ion channeling - exhibited the highest QE ratio.  Whereas the cleave plane (100) - i.e., the sample with the least “open space” between atoms, and therefore the sample supporting the lowest level of ion channeling - exhibited  the lowest QE ratio.  If one assumes a strict QE dependence on atomic number density, the QE of (110) and (111A) cleave planes following ion implantation should be greater than sample (100) by roughly 41 and 15%, respectively. In comparison, looking at Figure 9 heat cycle 5 values, the measured QE of (110) and (111A) cleave planes following ion implantation are greater than sample (100) by 33 and 30%, respectively, however there is fairly good agreement between measurements and predictions when error bars are taken into account.

Fig. 4.3.2.9. QE ratio - samples implanted with 10,000 V hydrogen ions to samples that were not exposed to hydrogen ions - as a function of heat cycle, for bulk GaAs with three different surface cleave planes. Heat cycle numbers: 1: 250°C for 20 minutes; 2: 370°C for 30 minutes; 3: 490°C for 1 hour; 4 and 5: 550°C for 1 hour

In conclusion, implantation of the photocathode with either low or high energy hydrogen ions served to reduce photocathode QE, but the QE degradation caused by 100 V hydrogen ions was modest and QE could easily be recovered following sample heating.  In sharp contrast, the QE degradation caused by 10,000 V hydrogen ions was severe and QE could not be fully recovered with heat. These observations suggest that low energy ions penetrate the surface, stopping at locations between atoms and creating interstitial defects that likely reduce the diffusion length of the electrons within the material, reducing the number of available electrons that reach the photocathode surface that can contribute to photoemission.  During sample heating, the interstitial defects diffuse throughout the material, restoring the electron diffusion length and the photocathode QE. Whereas high energy ions likely generate knock-out vacancies within the crystal structure that permanently adversely alter the band structure of the semiconductor.  As noted above, inside a DC high voltage photogun, the photocathode will be bombarded by considerably more low voltage ions than high voltage ions.  This is fortuitous and explains why the photocathode QE can be routinely restored following simple heating and reactivation, except at the electrostatic center of the photocathode, where the highest energy ions are directed8, 27.

In addition, the data support the simple picture that channeling is enhanced for the sample with the most “open space” between atoms. More “open space” leads to enhanced channeling which means high energy ions create fewer vacancies that lead to reduced and unrecoverable QE. Surface cleave plane (110) has the most “open space” and cleave plane (100) the least “open space”. As such, surface cleave plane (110) was the least sensitive to ion bombardment and cleave plane (100) the most sensitive. Considering all the results in total, the best choice for a photogun using bulk GaAs would be surface cleave plane (110), providing the highest QE and least sensitivity to ion bombardment.  It’s true that modern high-current accelerator applications now prefer alkali-antimonide photocathodes over GaAs photocathodes, because alkali-antimonide photocathodes offer similarly high QE but with longer operating lifetime.  However, spin-polarized accelerator applications may be forced to use bulk GaAs as the only practical means to generate milliampere-levels of spin-polarized beam. 28

# References

[J1]	Wolfgang Schattke, Progress in Surface Science 54, 211 (1997)

[J2]	C.N. Berglund and W.E. Spicer Phys. Rev. 136, A1030 (1964)

[1]	W. E. Spicer, Phys. Rev. 112, 114 (1958).

[2]	W. E. Spicer and A. Herrera-Gomez, Modern Theory and Applications of Photocathodes, Report No. SLAC-PUB-6306

SLAC/SSRL-0042, 1993

[3]	G. Ferrini et al., Solid State Communications 106, 21 (1998).

[4]	D. H. Dowell et al., in FEL'07, Novosibirsk, Russia (2007).

[5]	D. H. Dowell et al., Phys. Rev. ST Accel. Beams 9, 063502 (2006).

[6]	G. Suberlucq, Developpement et production de photocathodes, Report No. CLIC-NOTE-299, 1996.

[7]	H. B. Michaelson, J. Appl. Phys. 48 (1977).

[8]	E. Chevallay et al., Nuclear Instruments and Methods in Physics Research A 340 (1994).

[9]	F. L. Pimpec et al., in IPAC'10, (2010).

[10]	T. Srinivasan-Rao et al., J. Appl. Phys. 69, 3291 (1991).

[11]	R. Valizadeh et al., in IPAC2014, Dresden, Germany (2014).

[12]	P. Schoessow et al., The Argonne Wakefield Accelerator High Current Photocathode Gun and Drive Linac, Report No. ANL-HEP-CP-95-34, 1995.

[13]	J. Bossert et al., in 36th international Free Electron Laser Conference FEL14, Basel, Switzerland (2014).

[14]	S. Mistry et al., in IPAC2015, Richmond, VA, USA (2015).

[15]	A. Brachmann et al., in IPAC2011, San Sebastian, Spain (2011).

[16]	F. Zhou et al., Phys. Rev. ST Accel. Beams 15 (2012).

[17]	X. J. Wang et al., in LINAC1994, (1994).

[18]	L. N. Hand and U. Happek, Nuclear Instruments and Methods in Physics Research A 372, 335 (1996).

[19]	J. Smedley et al., Phys. Rev. ST Accel. Beams 11, 013502 (2008).

[20]	Y. Gao and R. Reifenberger, Phys. Rev. B 35 (1987).

[21]	M. Wurgel, Nettoyage ionique sous vide des photocathodes, 1991.

[22]	C. Vicario et al., in FEL 2013, New York, USA (2013).

[23]	R. J. Reid, Cleaning for vacuum service, Report No. OPEN-2000-276, 1999.

[24]	J. D. Herbert and R. J. Reid, Vacuum 47, 693 (1996).

[25]	R. Ganter et al., in FEL 2013, New York (USA) (2013).

[26]	P. H. Holloway and G. E. McGuire, Handbook of compound semiconductors (Noyes Publication.

[27]	H. Qian et al., in PAC2009, Vancouver, Canada (2009).

[28]	H. Qian et al., in PAC09, Vancouver, Canada (2009).

[29]	G. Penco et al., in IPAC'10, Kyoto, Japan (2010).

[30]	F. Zhou et al., in FEL'14, Basel, Switzerland (2014).

[31]	A. Lorusso et al., Phys. Rev. ST Accel. Beams 14, 090401 (2011).

[32]	P. Musumeci et al., Phys. Rev. Lett. 104, 084801 (2010).

[33]	H. E. Ives, Phys. Rev. 38, 1209 (1931).

[34]	E. Pedersoli et al., Appl. Phys. Lett. 87, 081112 (2005).

[35]	H. Tomizawa et al., in LINAC2012, Tel-Aviv, Israel (2012).

[36]	L. Wimmer et al., nature Physics 10, 432 (2014).

[37]	C. Vicario et al., Optics express 23, 4573 (2015).

[38]	R. Ganter et al., 2014).

[39]	R. Ganter et al., Phys. Rev. Letters 100, 064801 (2008).

[40]	Photocathode technology, http://www.hamamatsu.com/jp/en/technology/innovation/photocathode/index.html.

[41]	A. D. Bona et al., J. Appl. Phys. 80 (1996).

[42]	H. Trautner, Clic project at CERN, Switzerland, 2000.

[43]	E. Chevallay, edited by P. Communication2013).

[44]	E. Chevallay et al., in 19th International Linear Accelerator Conference, Chicago, USA (1998).

[45]	E. Chevallay, Experimental results at the CERN photoemission laboratory with co-deposition photocathodes in the frame of the CLIC studies, Report No. CTF3-Note-104, 2012.

[46]	A. Baskaran and P. Smereka, J. Appl. Phys. 111, 044321 (2012).

[47]	Z. Ding et al., J. Appl. Phys. 121, 055305 (2017).

[48]	P. Michelato, in EPAC, Sitges, Spain (1996).

[49]	P. Michelato, Nuclear Instruments and Methods in Physics Research A 393, 464 (1997).

[50]	S. H. Kong et al., J. Appl. Phys. 77, 6031 (1995).

[51]	C. Hessler et al., in IPAC15, Dresden, Germany (2015).

[52]	B. M. v. Oerle and G. J. Ernst, Nuclear Instruments and Methods in Physics Research A 358, 287 (1995).

[53]	S. H. Kong et al., Nuclear Instruments and Methods in Physics Research A 358, 272 (1995).

[54]	E. Chevallay et al., Production of a high average current electron beam with Cs2Te photocathode, Report No. CTF3 Note 020, 2001.

[55]	S. Lederer et al., in FEL2011, Shanghai, China (2011).

[56]	A. Fry et al., in XIX International Linac Conference, Chicago, Illinois (1998).

[57]	P. J. M. v. d. Slot et al., in FEL 2008, Gyeongju, Korea (2008).

[58]	R. Xiang et al., in IPAC2012, New Orleans, Louisiana, USA (2012).

[59]	R. Xiang et al., Phys. Rev. ST Accel. Beams 13, 043501 (2010).

[60]	J. Teichert et al., Report on photcathodes, Report No. CARE/JRA-PHIN July 2004, 2004.

[61]	E. Prat et al., in FEL14, Basel, Swistzerland (2014).

[62]	D. Sertore et al., Nuclear Instruments and Methods in Physics Research A 445, 422 (2000).

[63]	S. Lederer et al., in IPAC'10, (2010).

[64]	T. Maruyama et al., Appl. Phys. Lett. 55, 1686 (1989).

[65]	R. Alley et al., Nuclear Instruments and Methods in Physics Research A 1, 365 (1995).

[66]	P. J. Saez, Stanford University, 1997.

[67]	M. I. D’yakonov and V. I. Perel, Zh. Eksp. Teor. Fiz. (Sov. Phys. JETP)33, 1053) 60, 1954 (1971).

[68]	G. L. Bir et al., Zh. Eksp. Teor. Fiz. (Sov. Phys. JETP 42, 705) 69, 1382 (1975).

[69]	F. Meier and B. P. Zakharchenya, North-Holland Physics, Netherlands, 108 (1984).

[70]	P. H. Song and K. W. Kim, Phys. Rev. B 66 (2002).

[71]	R. J. Elliot, Phys. Rev. 96 (1954).

[72]	Y. Yafet, Solid State Physics (Academic, New York, 1963), Vol. 14,  p.^pp. 1-98.

[73]	A. G. Aronov et al., Sov. Phys. JETP 57, 680 (1983).

[74]	G. Fishman and G. Lampel, Phys. Rev. B 16, 820 (1977).

[75]	K. Zerrouati et al., Phys. Rev. B 37, 1334 (1988).

[76]	J. H. Jiang and M. W. Wu, Phys. Rev. B 79, 125206 (2009).

[77]	I. Zutic et al., Rev. Mod. Phys. 76, 323 (2004).

[78]	B. V. Zeghbroeck, Principles of semiconductor devices 2011).