## Slide 1
Injector R&D
The Problems with Photoguns
M. Poelker
BNL, August 8, 2018

## Slide 2: New Photoguns
CEBAF Injector Full-Energy Upgrade
  Replace 130 kV gun with 200 kV gun
  New baked beamline, Wien filters at proper locations
  New Quarter Cryomodule
Upgraded Injector Test Facility
  Help commission the re-designed HDIce target
  Verify the new QCM functions properly
  Pockels cell studies to support PV experiments
  Bubble Chamber astrophysics measurement
  Prepare polarized solid targets
  Polarized positron source
  Test coated SRF cavities
JLab Electron Ion Collider
  Very high average current un-polarized beams for cooling ions – magnetized cooling
  Exploring two options: DC high voltage photogun and rf-pulsed thermionic gun
Notes: Interior Page Design 2

## Slide 3
Always Tweaking the Design
The endless quest for perfection
1
2
3
4
Lifetime increased from 10s to 100s of Coulombs
Notes: Interior Page Design 1

## Slide 4: Key Features of a Polarized Photogun
Photocathode
  High Polarization
  High QE (photoemission yield)
  Long Lifetime
Vacuum
  Static Vacuum
  Dynamic Vacuum
High Voltage
  Must eliminate field emission
  No breakdowns, insulator failure
Drive Laser
  Reliable, phase locked to machine
  Adequate Power
  Wavelength Tunable
Notes: Interior Page Design 2

## Slide 5: The CEBAF Inverted Gun
Our “Load-locked” GaAs photogun:
Gun Vacuum ~ 10-12 Torr
Beamline vacuum could be improved…
NEG pumps
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 6
Recent CEBAF Polarized Source Performance
Fall 2016 – Spring 2017
  Strained Superlattice GaAs/GaAsP #5756-4
  Good Polarization 85-87% (measured at Mott)
  Good QE > 1% after activation => 6 mA/Watt/% @ 780 nm
  Lifetime about 200 C (s4D ~ 1mm) at currents < 200 uA

## Slide 7: Improving Lifetime with Larger Laser Size
J. Grames, et al., Phys. Rev. ST Accel. Beams 14 043501 (2011)
GaAs @ 532nm

## Slide 8: Lifetime Studies at mA Beam Current
Polarized positrons for CEBAF, and discussions with BNL related to high current eRHIC EIC, prompted experiments at CEBAF to characterize lifetime vs. laser spot size using high-polarization photocathodes
CEBAF 130kV polarized “inverted gun” with load lock
Make beam here
(-130kV, 0-1.5mA, 0-3pC)
Deliver it here
(Faraday cup)
Vary the laser beam size
(f=499 MHz, st ~ 50 ps)
Monitor vacuum and radiation levels along beam line
Work of Joe Grames, PSTP2017

## Slide 9: Lifetime Studies at mA Beam Current
1mA
Required laser power to maintain current, slope proportional to QE decay
Increasing laser size reduces QE decay proportionally
Adjust beam size to decrease x-ray level

## Slide 10: First Results: GaAs/GaAsP at mA Current
  CEBAF charge lifetime improves with larger laser spot size, as expected, but eventually beam size becomes “too large”
  Laser diameters greater than ~4 mm (4 sigma) will require properly designed cathode/anode electrodes, to ensure 100% transmission, to maintain excellent vacuum, to minimize ion bombardment
1 mA for 4.7 days
1mA(2007)
4mA(2011)
CEBAF

## Slide 11
Vacuum vs. Lifetime
Vacuum levels vs. lifetime are not as highly correlated with radiation levels
Still gun vacuum remains (sensibly) the greatest correlation with lifetime

## Slide 12
Radiation Level vs. Lifetime
Generally, charge lifetime improves with decreasing x-ray levels
Levels away from apertures (<10 Hz) more revealing than apertures (>250 Hz)

## Slide 13
Sensitivity of x-ray detectors for beam loss
Always use ion pumps as beam loss monitors, but in this study, beamline pressure appeared constant
X-ray monitors detect low level beam loss, sensitive to ~ 60 pA loss (typ. 1-5 nA), an array of GM tubes can pinpoint loss
loss
x-ray
loss
vacuum

## Slide 14: Polarization Studies at mA Beam Current
First measurement of beam polarization at JLab from superlattice (GaAs/GaAsP photocathode at milli-Ampere current
CEBAF 5 MeV Mott polarimeter: on-going effort to ascribe sub-percent accuracy (collaborators D. Moser, X. Roca-Maza, Charles Sinclair, M.J. McHugh, and Tim Gay)
CEBAF 5 MeV Mott Polarimeter
Chart: Polarization (%)
| 1.67 | 10.4 | 50.5 | 100.5 | 250.5 | 504 | 755 | 1011 | 1.06
 | 85.6704 | 84.5218 | 84.3896 | 85.3479 | 84.9536 | 86.116 | 84.7714 | 85.9647 | 87.1486
Work of Joe Grames, PSTP2017

## Slide 15: JLEIC High Energy Electron Cooler
High Energy Electron Cooler
ion beam
cooling solenoid (B>0)
Magnetization flip
cooling solenoid (B<0)
injector
beam dump
linac
fast extraction kicker
fast injection kicker
dechirper
rechirper
circulating bunches
extracted bunches
injected bunches
exchange
septum
vertical
bend
into ERL
vertical
bend
to CCR
ion beam
Circulator Cooler Ring
ERL Ring

## Slide 16: Magnetized Cooling Schematics
Electron beam suffers an azimuthal kick at entrance of cooling solenoid. But this kick can be cancelled by an earlier kick at exit of photogun. That is purpose of cathode solenoid
Upon exit of Cathode Solenoid
Upon entering Cooling Solenoid
re= 0.7 mm
Bcool = 1 T
Electrons born in strong uniform Bz
= Rlaser = 3.14 mm
Bz = 0.5 kG
= 36 µm
V
B
V
B
B
V
B
V

## Slide 17: JLEIC Magnetized Source Requirements
Bunch length | 60 ps (2 cm)
Repetition rate | 43.3 MHz
Bunch charge | 3.2 nC
Peak current | 33.3 A
Average current | 120 mA
Transverse normalized emittance | <19 microns
Cathode spot radius – Flat-top () | 3.14 mm
Solenoid field at cathode (Bz) | 0.5 kG
Bunch length | 60 ps (2 cm)
Repetition rate | 43.3 MHz
Bunch charge | 3.2 nC
Peak current | 33.3 A
Average current | 120 mA
Transverse normalized emittance | <19 microns
 | 3.14 mm
Solenoid field at cathode (Bz) | 0.5 kG
Cornell University demonstrated 65 mA and 2 nC, but not at same time, and non-magnetized
Fermilab Magnetized Photoinjector Laboratory:
Pulsed NCRF gun with Cs2Te photocathode and UV laser (λ=263 nm)
Bunch charge: 0.5 nC and bunch length: 3 ps
0.5% duty factor (average current: 7.5 μA)
  Bunch frequency: 3 MHz
  Macropulse duration: 1 ms
  Number of bunches per macropulse: 3000
  Macropulse frequency: 5 Hz

## Slide 18: Magnetized Source Schematics
Beamline
Gun Solenoid
Photocathode
Preparation
Chamber
Gun HV Chamber
Slit
Viewer Screen
Shield Tube
Viewer 3 Screen
Beam Dump
Use slit and viewscreens to measure mechanical angular momentum:
: solenoid field at photocathode
: laser rms size
φ: rotation (sheering) angle

## Slide 19: Building a 500 kV (?) Gun
C. Hernandez-Garcia, M. Poelker, and J. Hansknecht, “High Voltage Studies of Inverted-geometry Ceramic Insulators for a 350kV dc Polarized Electron Gun,” IEEE Transactions on Dielectrics and Electrical Insulation, Vol. 23, No. 1; February 2016
Start with “dummy” electrode (no photocathode) and test different insulators and cathode screening electrodes

## Slide 20: The Reality of HV Breakdown
The first test with R30 pure alumina ceramic suffered breakdown at ~315kV with subsequent puncture at 330kV.
A second test with a new R30 pure alumina suffered breakdown at ~315 kV.
* M. BastaniNejad, A. A. Elmustafa, E. Forman, J. Clark, S. Covert, J. Grames, J. Hansknecht, C. Hernandez-Garcia, M. Poelker and R. Suleiman, “Improving the performance of stainless-steel DC high voltage photoelectron gun cathode electrodes via gas conditioning with helium or krypton,” Nucl. Instr. and Meth. in Phys. Res. A, Vol. 762, pp. 135–141, 2014
Field emission managed via krypton-processing*, i.e., voltage was applied with ~10-5 Torr krypton added to gun chamber

## Slide 21: Careful design of triple-junction-shield
Gradients shown for 350 kV
Simulationsby Y. Wang
Ceramic
HV plug
Design overall shape for low gradient here !!

## Slide 22: In Lieu of Segmented Insulator
<10 MV/m
> 100 MV/m
Besides reducing field strength, the triple-point-junction shield “linearizes” the potential drop along insulator

## Slide 23: 500 kV Gun?
Notes: Interior Page Design 2

## Slide 24: 500 kV Gun? No
Notes: Interior Page Design 2

## Slide 25: Gun High Voltage Conditioning
Chart: HV conditioning time (hours)
Reached
360 kV
Vacuum and radiation levels
indistinguishable from bkgd at 350kV
Work by Carlos Hernandez-Garcia
Notes: Interior Page Design 2

## Slide 26: Barrel-Polished Electrodes
Gun electrodes traditionally polished using sand paper and diamond paste
Tedious process, takes about 30 days to complete
Now performed in 1 day using SRF barrel polishing machine
  From machine shop
30 minutes with plastic cones
30 minutes with corncob
Work by Don Bullard
Notes: Interior Page Design 2

## Slide 27: 300 kV Inverted Gun and CsK2Sb Photocathode
Slide 27
27
8 MV/m
11 MV/m
First insulator conditioned to 325 kV, then rebuilt gun with optimized triple-junction shield
1mA
Learning how to use the new photocathode
QE drop

## Slide 28: Charge Lifetime of High Current Beam
Chart: Gun HV=300 kV
| 0 | 200 | 300 | 400
3 mA | 1085 | 162 | 2583 | 343
4 mA | 195 | 167 | 214 | 309
4.5 mA | 294 | 143 | 275
Chart: Run Sequence
| 4 | 5 | 2 | 8 | 7 | 9 | 6 | 3
3 mA | 1085 | 10000 | 377 | 2583 | 512 | 343 | 5000 | 162
4 mA | 183 | 214 | 309 | 167 | 195
4.5 mA | 275 | 210 | 143 | 294
Chart: Beam Current=3 mA
| 200 | 250 | 300
0 A | 10000 | 10000 | 1085
200 A | 377 | 162
300 A | 512 | 2583
400 A | 343
CsxKySb photocathodes on GaAs substrates
No apparent Lifetime dependence on gun HV, magnetization effect, or run sequence
Only 3 incidents of QE drop due to arcing, and this happened only with non-magnetized beam
Strong focusing of gun solenoid might help keep ions away from e-beam
Work of Md. Mamun, Y. Wang

## Slide 29: Molybdenum Puck, Biased anode, Precipitators
Slide 29
29
Periodic vacuum bursts,
sometimes accompanied by step decrease in QE
Biased anode
Two beamline precipitators
Uninterrupted Operation

## Slide 30: Good lifetime using GaAs Substrates (sometimes)
Slide 30
30
Thick antimony layer
Thin antimony layer
work of Md. A. Mamun and Y. Wang, very preliminary
Lifetime runs using biased anode and beamline precipitators

## Slide 31: Alkali-Antimonide Photocathode Lifetime
Slide 31
31
CsxKySb photocathode studies
Factors that effect photocathode lifetime:
HV micro-discharges
Field emission?
Beamline ions
laser heating
Recipe variations and chemistry
photocathode/substrate interface
work of Md. A. Mamun and Y. Wang, very preliminary

## Slide 32: Improved lifetime at CEBAF with Wien “precipitator”
Slide 32
32
Vert. Wien ON and set to rotate polarization 50 degrees

## Slide 33: Parity Table
Upgrading the CEBAF Injector will help us conduct PREx, CREx and proposed parity violation experiments that are even more demanding
Notes: Interior Page Design 2

## Slide 34
Injector Upgrade
Increase gun voltage, modify Wien filters for 200kV operation
Improve baked beam line vacuum so gun does not pump on beam line
Locate H-Wien (energy filter) upstream of pre-buncher cavity
New SRF booster eliminates warm capture, RF deflection and x/y coupling
Our new “1/4 cryomodule”, or QCM:
2 cell capture section + 7 cell cavity,
should provide 10 MeV beam and introduce no x/y coupling, allow better matching, more adiabatic damping
200 kV

## Slide 35: CEBAF Photogun at 200 kV
Deemed too aggressive
Notes: Interior Page Design 2

## Slide 36: Plan A
< 10 MV/m, demonstrated performance at 300 kV,
a “sure thing” at 200 kV
CEBAF 130 kV, used since 2010
Notes: Interior Page Design 2

## Slide 37: Upgraded Injector Test Facility - UITF
TEST NEW PHOTOGUNS
COMMISSION NEW QUARTER CRYOMODULE
TEST 200 kV WIEN FILTER
TEST HDIce
37

## Slide 38: Upgraded Injector Test Facility

## Slide 39
Homemade NEG coating
“It’s going to be the best polarized photogun ever”
anonymous
Work of P. Adderley

## Slide 40
Homemade NEG coating

## Slide 41: But wait…..
41
Gun vented at 229 kV
Field emission and excessive voltage–induced gas bursts
Voltage-induce gas bursts are normal, but not at this level
Neon, used for NEG coating, liberated by high voltage

## Slide 42: Plan B
Smaller R28 insulator, with optimized triple point shield and mildly conductive insulator
CEBAF 130 kV, used since 2010
Only two R30 insulators left, need them for LDRD magnetized beam
Notes: Interior Page Design 2

## Slide 43: Plan B
Field maps by G. Palacios
Notes: Interior Page Design 2

## Slide 44: Beam Deflection and Astigmatism
Original CEBAF cathode electrode
New cathode electrode
Some Progress:
Beam delivery 180 kV
New power supply attached to PSS
But…
Beam deflection
Astigmatic beam harder to transport
Reaped no rewards for stiffer beam
Notes: Interior Page Design 2

## Slide 45: Summary
Polarized beam - How much beam loss is bad? Good evidence that even a part in 106 is problematic
Radiation monitoring, now an essential tool for polarized beam operations
Scaling the laser beam size to ~ 1cm should be possible if gun electrodes are designed properly
Why don’t we bias the anode at CEBAF? Precipitators are exciting development
CEBAF gun group finally starting to perform realistic and useful modeling, but so far, I don’t think modeling has solved a problem BEFORE cutting metal
Students have been key to recent progress, and bringing projects to semi-conclusion
Alkali-antimonide lifetime studies very interesting. Similar/different compared to GaAs - ions, laser heating, chemistry variations, photocathode/substrate interface

## Slide 46: Summary
Fixing one problem can create another – NEG coating seems to have resulted in insulator failure, a result of gas load liberated from coating during HV processing
High Voltage: no explosions, no field emission, uniform field in the cathode/anode gap
High voltage R&D is expensive and takes a long time to complete
The inverted insulator design seems perfect for guns biased to 200 kV, but temperamental at voltage 300+ kV, although we did operate at 300 kV for > 1000 hours
Some JLab locations can’t accommodate a tall photogun
Segmented insulator, wonderful for pinning the voltage drop across the insulator, I wish there was a way to implement for inverted insulator
The best way to make progress is to keep the test apparatus ON every day

## Slide 47: Gun Group
P. Adderley, B. Bullard, M. Poelker, J. Grames, J. Hansknecht,
C. Hernandez-Garcia, M. Poelker, R. Suleiman, M. Stutzman, and S. Zhang
Postdoc: M. A. Mamun
Graduate Students: G. Palacios, Y. Wang, S. Wijiethunga, J. Yoskovitz, M. Stefani
Frequently work with others: F. Hannon, R. Kazimi, A. Hofler

## Slide 48: Supplemental Material

## Slide 49
Ion Bombardment

## Slide 50: Improving charge lifetime with GaAs/GaAsP
Indeed, we enhanced the Charge Lifetime for QWeak by a factor of four when doubling the laser spot size from 0.5 mm to 1.0 mm (diameter)
but milliampere applications require kiloCoulomb charge lifetime to provide uninterrupted operation of reasonable duration

## Slide 51: Parity Violation Experiments
Increasing precision
Decreasing Physics Asymmetry
Notes: Interior Page Design 2

## Slide 52: Benefits of Distributed Bragg Reflector
Enhanced absorption occurs only at specific laser wavelengths
non-DBR Photocathode : absorption in the GaAs/GaAsP superlattice < 5%
  Most light passes into the substrate leading to unwanted heating
DBR photocathode : absorption in the GaAs/GaAsP superlattice > 20%
  Less light required to make required beam, less light means less heat
Great for high current initiatives like polarized positrons at CEBAF and EIC
Non-DBR photocathode
DBR photocathode
Photocathode without DBR
Photocathode with DBR
(57 layers!)

## Slide 53: World Record QE from High Polarization Photocathode
Others have tried…but very difficult to obtain QE enhancement at the laser wavelength that also provides high polarization, CEBAF lasers operate at ~ 776 nm (doubled-telecom lasers)
Standard strained-superlattice
  QE = 0.89%
  Polarization = 92%
DBR
  QE = 6.4%
  Polarization = 84%
The highest reported QE of any high polarization photocathode
Excellent candidate for mA operations, will test at CEBAF this shutdown
SBIR partnership
W. Liu, S. Zhang, M. Stutzman, M. Poelker, Y. Chen, W. Lu, and A. Moy, Appl. Phys. Lett. 109, 252104 (2016)

## Slide 54: Magnetized Bunched-Beam Electron Cooling
Ion beam cooling in presence of magnetic field is much more efficient than cooling in a drift (no magnetic field):
  Electron beam helical motion in strong magnetic field increases electron-ion interaction time, thereby significantly improving cooling efficiency
  Electron-ion collisions that occur over many cyclotron oscillations and at distances larger than cyclotron radius are insensitive to electrons transverse velocity
Long cooling solenoid provides desired cooling effect:
  Counteracting emittance degradation induced by intra-beam scattering
  Maintaining ion beam emittance during collisions and extending luminosity lifetime
  Suppressing electron-ion recombination
  but putting the electron beam into the cooling solenoid represents a challenge

## Slide 55: Measuring Electron Beam Magnetization
Use slit and viewscreens to measure mechanical angular momentum:
: solenoid field at photocathode
: laser rms size
φ: rotation (sheering) angle

## Slide 56: Slit and Viewscreen Measurement
0 G at photocathode
1511 G at photocathode
Beamlet observed on downstream viewer

## Slide 57: Beam Size Oscillation
Gun solenoid magnetizes beam but also focuses beam
Rotation angle influenced by Larmor oscillation in gun solenoid
Three curves correspond to measurements at three beamline viewers
Chart: B@cathode, Gauss
| 0 | 3.6259999999999999 | 7.2519999999999998 | 10.878 | 14.504 | 18.13 | 21.756 | 25.381999999999998 | 29.007999999999999 | 32.634 | 36.26 | 54.39 | 72.52 | 90.649999999999991 | 108.78 | 126.91 | 145.04 | 163.16999999999999 | 181.29999999999998 | 217.56 | 253.82 | 271.95 | 290.08 | 326.33999999999997 | 362.59999999999997 | 398.86 | 435.12 | 453.25 | 471.38 | 507.64 | 543.9 | 580.16 | 616.41999999999996 | 634.54999999999995 | 652.67999999999995 | 688.93999999999994 | 725.19999999999993 | 743.32999999999993 | 761.45999999999992 | 779.59 | 797.72 | 815.85 | 833.98 | 852.11 | 870.24 | 888.37 | 906.5 | 942.76 | 979.02 | 997.15 | 1015.28 | 1051.54 | 1087.8 | 1178.45 | 1269.0999999999999 | 1359.75 | 1450.3999999999999
σ (V1), mm | 1.7714 | 1.7775 | 1.7704 | 1.7626 | 1.7071 | 1.6955 | 1.6802 | 1.6048 | 1.5353 | 1.5437 | 1.4785 | 1.1003 | 0.659 | 0.25374 | 0.43979 | 0.84338 | 1.1792 | 1.4508 | 1.4479 | 1.1094 | 0.38868 | 0.42047 | 0.74867 | 1.1531 | 1.0345 | 0.54079 | 0.45355 | 0.58938 | 0.65869 | 0.55215 | 0.32189 | 0.49159 | 0.68473 | 0.86909 | 1.0323 | 1.0938 | 0.47539 | 0.49614 | 0.54158 | 0.63396 | 0.79357 | 0.91425 | 1.0069 | 1.045 | 1.0617 | 1.064 | 1.1167 | 1.4647 | 1.7154 | 1.7361 | 1.6907 | 1.7376 | 1.8783 | 2.1166 | 2.1719 | 2.0662 | 1.6395
σ (V2), mm | 2.512 | 2.5214 | 2.4852 | 2.501 | 2.3915 | 2.4324 | 2.3315 | 2.2628 | 2.1948 | 2.1285 | 2.0618 | 1.4907 | 0.84295 | 0.30379 | 0.74431 | 1.3821 | 1.8817 | 2.1799 | 2.1251 | 1.4858 | 0.4832 | 0.66359 | 1.1624 | 1.6893 | 1.3976 | 0.6512 | 0.66781 | 0.83871 | 0.8802 | 0.59449 | 0.33823 | 1.0636 | 1.5427 | 1.8953 | 2.1284 | 2.0612 | 1.015 | 1.0405 | 1.1641 | 1.4012 | 1.7081 | 1.9142 | 2.0253 | 2.073 | 2.0148 | 2.0095 | 2.0716 | 2.7165 | 3.0553 | 3.051 | 3.0442 | 2.9717 | 3.1391 | 3.5575 | 3.2997 | 2.898 | 1.976
σ (V3), mm | 4.5603 | 4.5053 | 4.5845 | 4.4949 | 4.2199 | 4.3547 | 4.1896 | 4.1675 | 3.8947 | 3.8464 | 3.6761 | 2.5948 | 1.3284 | 0.73223 | 1.7584 | 2.9284 | 3.8168 | 4.2198 | 3.9432 | 2.7106 | 1.0129 | 1.5291 | 2.3939 | 3.1948 | 2.3791 | 1.1964 | 1.3656 | 1.6045 | 1.5054 | 0.9969 | 0.9037 | 2.8517 | 3.8007 | 4.7607 | 5.2883 | 4.776 | 2.7389 | 2.891 | 3.2476 | 3.7624 | 4.4183 | 5.0525 | 5.1443 | 5.1709 | 4.9779 | 4.9099 | 5.0629 | 6.5887 | 6.9666 | 6.8697 | 6.8314 | 6.4947 | 7.1683 | 7.2243 | 6.0779 | 4.8546 | 2.3456
Chart: B@cathode, Gauss
| 0 | 3.6259999999999999 | 7.2519999999999998 | 10.878 | 14.504 | 18.13 | 21.756 | 25.381999999999998 | 29.007999999999999 | 32.634 | 36.26 | 54.39 | 72.52 | 90.649999999999991 | 108.78 | 126.91 | 145.04 | 163.16999999999999 | 181.29999999999998 | 217.56 | 253.82 | 271.95 | 290.08 | 326.33999999999997 | 362.59999999999997 | 398.86 | 435.12 | 453.25 | 471.38 | 507.64 | 543.9 | 580.16 | 616.41999999999996 | 634.54999999999995 | 652.67999999999995 | 688.93999999999994 | 725.19999999999993 | 743.32999999999993 | 761.45999999999992 | 779.59 | 797.72 | 815.85 | 833.98 | 852.11 | 870.24 | 888.37 | 906.5 | 942.76 | 979.02 | 997.15 | 1015.28 | 1051.54 | 1087.8 | 1178.45 | 1269.0999999999999 | 1359.75 | 1450.3999999999999
Slit1-V2 | 0 | -0.017189 | -0.22918 | -0.040107 | -0.022918 | -0.13178 | 0.034377 | -0.057296 | -0.16043 | -0.2521 | 0.017189 | -0.18908 | -1.1746 | 4.8759 | 0.77349 | -0.3495 | -0.69901 | -1.5871 | -1.2261 | -1.3636 | 5.1681 | 5.953 | 0.080214 | -1.9538 | -2.1142 | 3.008 | 8.1704 | 1.0199 | -0.20626 | 3.3346 | 45.2637 | 4.5378 | -0.13751 | -1.9996 | -3.0768 | -3.6898 | 6.0734 | 4.8759 | 3.2544 | 0.80787 | -0.6589 | -1.8621 | -2.9049 | -2.9106 | -3.2716 | -3.9763 | -4.1253 | -5.2368 | -6.5661 | -7.0531 | -7.0818 | -7.3797 | -7.586 | -8.5657 | -9.8434 | -9.3106 | -10.1528
Slit1-V3 | 0 | -3.7529 | -3.4779 | -3.008 | -3.4091 | -3.2945 | -3.3575 | -3.0711 | -3.3976 | -3.008 | -2.8075 | -2.8762 | -3.3461 | 17.332 | 1.3923 | -2.6986 | -4.3258 | -6.0504 | -5.2254 | -4.4519 | 10.7659 | 10.6456 | -1.9996 | -6.7036 | -7.5 | 6.3713 | 13.8083 | 3.6555 | 0.028648 | -5.9702 | 27.4619 | 6.7552 | -4.2857 | -7.5344 | -8.7892 | -8.3996 | 8.709 | 9.4366 | 7.4255 | -1.8048 | -4.7842 | -7.0245 | -8.9324 | -8.3709 | -8.6287 | -11.1498 | -7.8209 | -12.7082 | -15.8251 | -16.547 | -17.8591 | -18.0253 | -17.67 | -21.3083 | -23.5142 | -17.0741 | -33.0138
Mamun’s work

## Slide 58: New Steel Photocathode Holders
New steel holders (pucks) to enhance field to 2.0 kG at photocathode. Two types:
  Molybdenum and carbon steel hybrid puck
  Carbon steel puck
Molybdenum
Steel
Steel

## Slide 59: Photocathode Preparation Chamber
K2CsSb grown with a mask – limit photocathode active area (3 mm diameter) to reduce beam halo, minimize vacuum excursions and high voltage arcing, prolong photogun operating lifetime
Active area can be offset from electrostatic center
5 mm active area available, Entire photocathode can be activated too
Consistently growing photocathodes with 5-7% QE

## Slide 60: Gun Solenoid
Using spare CEBAF Dogleg magnet power supply (500 A, 80 V)
Learned that gun solenoid can influence field emission
First trials with gun at high voltage and solenoid ON resulted in new field emission and vacuum activity
Procedure to energize solenoid without exciting new field emitters
Size | 11.811" ID, 27.559" OD, 6.242" Z
Conductor | L=500 m, A=0.53 cm2 16 layers by 20 turns
Coil Weight | 254 kg (560 lbs)
Resistance | 0.198 Ω
Field at Photocathode | 1.5 kG
Voltage | 79 V
Current | 400 A
Chart: z, m

## Slide 61: ASTRA Simulation
Bz, T
Lens 1
Lens 2
Viewer 1
At 400 A
Sajini’s work
Beam size on viewers depends on the initial beam size and the angular momentum at the exit of the solenoid field.

## Slide 62: Beam Sizes at Viewer 1
Sajini’s work
Making good progress in modeling our apparatus and beam magnetization
Chart: Bz at Cathode, G
| 0 | 7.5549999999999997 | 18.887499999999999 | 30.22 | 37.774999999999999 | 56.662499999999994 | 75.55 | 94.4375 | 113.32499999999999 | 151.1 | 169.98749999999998 | 188.875 | 226.64999999999998 | 264.42500000000001 | 302.2 | 339.97499999999997 | 377.75 | 415.52499999999998 | 453.29999999999995 | 491.07499999999999 | 528.85 | 566.625 | 604.4 | 642.17499999999995 | 661.0625 | 679.94999999999993 | 717.72500000000002 | 755.5 | 774.38749999999993 | 793.27499999999998 | 812.16250000000002 | 831.05 | 849.9375 | 868.82499999999993 | 887.71249999999998 | 906.59999999999991 | 925.48749999999995 | 944.375 | 982.15 | 1019.925 | 1038.8125 | 1057.7 | 1095.4749999999999 | 1133.25 | 1152.1375 | 1171.0249999999999 | 1227.6875 | 1265.4624999999999 | 1303.2375 | 1322.125 | 1416.5625 | 1454.3374999999999 | 1473.2249999999999 | 1511
ASTRA Simulation | 1.6532 | 1.6693 | 1.6067 | 1.4516 | 1.3119 | 0.9273 | 0.6127 | 0.3718 | 0.3403 | 1.0491 | 1.2304 | 1.2373 | 1.1061 | 0.6862 | 0.504 | 0.9325 | 1.1574 | 0.9383 | 0.487 | 0.5337 | 0.7188 | 0.5724 | 0.312 | 0.3028 | 0.3299 | 0.3271 | 0.3338 | 0.5161 | 0.5871 | 0.6366 | 0.6752 | 0.7266 | 0.8224 | 0.965 | 1.1182 | 1.2459 | 1.3372 | 1.3919 | 1.4166 | 1.5431 | 1.6897 | 1.8631 | 2.168 | 2.2133 | 2.1621 | 2.1313 | 2.3903 | 2.5546 | 2.4551 | 2.3667 | 1.9521 | 1.6206 | 1.4428 | 1.06
Viewer 1 Measured Size | 1.7714 | 1.7775 | 1.7704 | 1.7626 | 1.7071 | 1.6955 | 1.6802 | 1.6048 | 1.5353 | 1.5437 | 1.4785 | 1.1003 | 0.659 | 0.25374 | 0.43979 | 0.84338 | 1.1792 | 1.4508 | 1.4479 | 1.1094 | 0.38868 | 0.42047 | 0.74867 | 1.1531 | 1.0345 | 0.54079 | 0.45355 | 0.58938 | 0.65869 | 0.55215 | 0.32189 | 0.49159 | 0.68473 | 0.86909 | 1.0323 | 1.0938 | 0.47539 | 0.49614 | 0.54158 | 0.63396 | 0.79357 | 0.91425 | 1.0069 | 1.045 | 1.0617 | 1.064 | 1.1167 | 1.4647 | 1.7154 | 1.7361 | 1.6907 | 1.7376 | 1.8783 | 2.1166 | 2.1719 | 2.0662 | 1.6395

## Slide 63
CEBAF Polarized Inverted Load Lock Gun (Spring 2017)
  CEBAF Load Lock Photogun (-130kV)
1 mA 86 C/day
5 mA 432 C/day
10 mA 860 C/day
50 mA 4320 C/day

## Slide 64: Inverted-Insulator Photoguns
(At 350 kV, beam is sufficiently relativistic, don’t need a “capture” section )
CEBAF 130 kV, used since 2010
350 kV gun for GTS and UITF
Longer “R30” insulator
Spherical electrode
Notes: Interior Page Design 2

## Slide 65: Inverted-Insulator Photoguns
CEBAF 200 kV Gun
350 kV gun for GTS and UITF
with optimized triple point shields and mildly conductive insulators
Both designs, maximum field strength < 10 MV/m
Notes: Interior Page Design 2

## Slide 66: Optimizing the Electrode Design
Pure alumina insulator replaced with doped alumina for higher voltage stand-off and robust operations
Electrode ‘shed’ (triple junction shield) re-designed to lower gradient from 12 MV/m to 10 MV/m at 350kV
Pure alumina insulator
Doped alumina insulator

## Slide 67: 3 photoguns with barrel polished electrodes
CEBAF 200 kV
Installed June 2018
Commissioning now.
UITF 350 kV
Polarized Gun
Under assembly
GTS 350 kV
In operation since Nov. 2016 with CsK2Sb photocathode:
500 uA magnetized beam
4.5 mA non-magnetized