## Slide 1: DC sputtered NEG coatings for non-uniformly shaped chambers Philip A. Adderley, Marcy L. Stutzman, Matthew Poelker
Notes: Title Page Design 3

## Slide 2: Thomas Jefferson National Accelerator Facility
12 GeV electron accelerator for Nuclear Physics (US DOE)
Mission: To understand the transition from hadronic (protons and neutrons) to partonic (quarks and gluons) physics.
Electron beam, with polarization ~ 90%, current to 200 μA
1.4 km racetrack design accelerator
Hall A
Hall B
Hall C
Hall D
Source
Polarized source
Notes: Cut way back here if I am short on time.

## Slide 3: DC Photoemission Source
-130kV
130 kV DC bias, RF pulsed laser
x-ray standard “inverted” insulator
Base pressure approaching XHV ≡ P < 1x10-12 mbar
Pumps with NEG modules and SEM style ion pump
light in
electrons out
Ionized, accelerated residual gas damages photocathode
Upgrades require higher voltage, larger electron gun
Future accelerators (e-RHIC, CLIC) require higher currents (10 mA)

## Slide 4: Introduction
Outgassing measurements:
  heat treatment, a-Si, TiN
NEG coating
  Gun exit beampipe
  Gun chamber
  Atomic physics chambers
Conclusions

## Slide 5: Motivation for outgassing rate studies
TiN
  Does low outgassing found in literature correspond to low pressure?
Heat treatments
  How much can we improve pressure with medium temperature bakes
a-Si (Silco-tek) fast pumpdown time unbaked, how does it work baked
Restek / SilcoTek data with
Bruce Kendall

## Slide 6: Outgassing rates vs. heat processing and coatings
Identical 304L chambers
Bare steel
TiN coating (9 µm, cathodic arc PVD)
a-Si (SilcoGuard-1000® ~900 nm, CVD)
Outgassing rates
Spinning Rotor Gauge
Accumulation technique
Multiple bakes
Q(Troom) after each bake

## Slide 7: Outgassing rate vs. room temperature after each bakeout
Factor of 20 reduction in outgassing after 400°C heat treatment
Linearity on Arrhenius plot:
Temperature dependent diffusion activation energy
Bake temperatures, in order
Effect of heat treatments and coatings on the outgassing rate of stainless steel chambers, M.A.Mamun et al., J. Vac. Sci. Technol. A 32, 021604 (2014)
Outgassing rate temperature sensitive:
Factor of 5 variation between 15 and 30°C

## Slide 8: Outgassing rates: bare and coated chambers
Chart: Outgassing Rate (Torr L s-1 cm-2)
| First Bake 90°C, 30h | Second Bake 150°C, 30h | Third Bake 250°C, 30h | Fourth Bake 400°C, 100h | Fifth Bake 150°C, 30h | Sixth Bake 250°C, 30h | Seventh Bake 150°C, 30h | Eighth Bake 360°C, 150h
TiN | 6.44e-13 | 3.7e-15 | 2.4e-16
SilcoII | 1e-12 | 1.3e-13 | 1.5e-13
SS | 4e-12 | 1.7e-13 | 1e-13 | 2.8e-13 | 2.2e-13 | 9.9e-14
Silco | 2.4e-12 | 2.1e-12 | 1.6e-12 | 3.6e-12 | 2.8e-12 | 1.9e-12
All data at Troom = 20°C
Notes: Steel:
Expected reduction
with 400°C heat
treatment
Silco:
Little variation with
heat treatment
Silco on heated SS:
Retains prior
outgassing rate
TiN coating:
Very low outgassing
rates, consistent with
literature, elemental
Ti pumping?

## Slide 9: Coated chambers with NEG & ion pumps Measured vs. calculated pressures
Chart: Pressure (x10-12 Torr)
| bare | silco | TiN
3BG | 0.93916 | 1.6567 | 1.0143
Calculated | 0.85997 | 0.45897 | 0.00073435
Notes: Preliminary conclusions: is the sensitivity correct? Were the outgassing measurements correct? (no for TiN) was the pump speed constant through the three. Work on error bars until the extractor error is more believable. Poor signal to noise on the extractor gauge makes it difficult to use?

## Slide 10: Coated chambers with NEG & ion pumps Measured vs. calculated pressures
Chart: Pressure (x10-12 Torr)
| bare | silco | TiN
3BG | 0.93916 | 1.6567 | 1.0143
Calculated | 0.85997 | 0.45897 | 0.00073435
Measure pressure:
Watanabe Bent Belt Beam Gauge
Notes: Preliminary conclusions: is the sensitivity correct? Were the outgassing measurements correct? (no for TiN) was the pump speed constant through the three. Work on error bars until the extractor error is more believable. Poor signal to noise on the extractor gauge makes it difficult to use?

## Slide 11: TiN results in disagreement?
Cathodic arc PVD (commercial vendor)
Thick (9 um)
Ti:N ratio ~ 1:1, but inhomogeneous (EDS)
Ti:N ranges from 0.58:1 through 1.17:1
How to reconcile discrepancy?
Any pumping in system during accumulation measurement affects apparent outgassing rate

## Slide 12: TiN to reduce outgassing?
TiN pumps poorly (0.003 L/s for entire chamber ~1x10-6 L/s/cm2)
Ultimate pressure in chamber as expected for heat treated steel (~1x10-12 Torr)
Measured outgassing ≠> predicted pressure
Can we deposit a good pump on surface?
  Try TiZrV coatings on full chambers

## Slide 13: Initial JLab TiZrV coating: ~1998
6 cm diameter, 1.3m long beamline at gun exit
1 mm Ti, Zr and V wires
Bake 150°C, 12 hours
Argon gas
Glow discharge clean: +HV on wire, 1 hour
DC sputter, no magnet
Characterization of the Characterization of the CEBAF 100 kV DC GaAs photoelectron gun vacuum system, M.L. Stutzman et al., NIMA 574, (2007)p. 213.
NEG tube

## Slide 14
Drytel Pump
Kr or Ar gas
window
with
ground grid
bakable gas manifold
with pumpout port
variable leak valve
beampipe
HV feedthrough,
Re-entrant insulator
HV feedthrough
bellows
Thompson
rail support
Springs
for tension
coupon holder
Ion pump
RGA
Convectron Gauge
Convectron Gauge
Right angle valve
Heat at ~100°C during sputtering
Ion pump power supply
(no indep. current/voltage control)
  ~10 mA, ~600V
  Pressure ~200 mTorr
Sputter for 36-72 hours

## Slide 15: Pump Speed Measurement
Modified Flowmeter
M.H.Hablanian Recommend Procedure for measuring pump speeds, JVSTA, 1987
Orifice Method
Leak valve
RGA
Extractor
Ion pump
orifice
Test chamber/tube
extractor
Bake pump
RGA

## Slide 16: Coating properties
Pump speed ~30 L/s for tube
0.015 L/s/cm2
EDS analysis:
  25% Ti
  50% V
  25% Zr
Low pump speed vs. commercial
Net pump rather than gas load
NEG coated gun exit at JLab over 15 yrs

## Slide 17: Extrapolation to cylindrical chambers
First: aluminum supports for array of wires
  Sputtering yield from support frame dominates
Second: Self supporting frame, TiZrV twisted wires, tied at joints with Ti wires
  Attempt to maintain 3 cm distance from wall to wire used in tube sputtering

## Slide 18: Chamber coating setup
25 cm diameter chamber “cage”
Cage for 30 cm diameter

## Slide 19: Chamber sputtering parameters
Bake 48 hours, 150°C
Glow discharge clean, 2 hours, 550 V, 25 mTorr, 90°C
Sputter, 100 hours, 80 mTorr, 90°C
~50 mTorr, ~160 mA, 700-1000V
0.012 g/cm2 , 0.12 mg/cm2/hour, ~24 g total
Pump speed: 220 L/s for chamber = 0.02 L/s/cm2 (throughput method)

## Slide 20: Discharge during sputtering
10” diameter chamber (25 cm)
12” diameter chamber (30 cm)

## Slide 21: Problems: Flaking
Coating tends to flake on edges
and ends of chamber,
particularly corners

## Slide 22: Coating and modules: First Load Locked gun

## Slide 23: SEM morphology
Columnar structure
Inhomogeneous

## Slide 24: Problems in NEG coated chamber
First Load Locked High voltage Gun
100 kV
Injector test cave
  Lifetime 200 Coulomb at
  250 A and 1 mA
Vent, move to CEBAF tunnel, install, bake
  Lifetime 30 Coulomb
  60 A

## Slide 25: Flake-caused field emission?
2 years at CEBAF with poor lifetime
High voltage electrode removed
Hazy spot – evidence of field emission
Correlated with flaky NEG coating?

## Slide 26: Inverted Gun: No NEG coating
Rotate NEG modules to eliminate line of sight from walls to cathode/anode gap
Add ~400°C activation during 250°C bake
Horizontal, First Load Locked gun NEG array orientation
Inverted Gun NEG array rotated
Reaches low 10-12 Torr range without full NEG activation (shorted)
Good photocathode lifetimes

## Slide 27: Coating atomic physics chambers

## Slide 28: MIT chamber
Benefits
No High voltage
  -> Flaking not important
Not vented once put in service
Drawbacks
Geometry
Time/effort
Heat treat 400°C, 100 hours
Install twisted wire “basket”
Bake 150°C, 24 hours
Coat ~100 hours
Happy scientists!

## Slide 29: JILA chamber
Atomic clock time standard
Atomic physics methods
Strontium atom transitions, optical lattice
lifetime is pressure dependent
Collaborative effort to see how coatings, work toward XHV can extend beyond accelerator physics

## Slide 30: Most recent work
Increasing gun voltage (130 kV to 350 kV)
Larger electrode
Larger chamber required (46 cm dia)
Keeping NEG strips surrounding makes chamber huge
Will NEG coating help?
Can we avoid flaking?
NOTE:
10” flange (DN200) and 18” diameter (46 cm) means “basket” can’t fit inside intact
Sputtering thus far with central twisted wire, 9” (23 cm) distance
Film very thin, well adhered, no flakes

## Slide 31: Pressure in coated chamber: coating + 45 L/s ion pump
Chart: 350 kV chamber vs. time
Heat treat 400°C
Several sputter cycles
Vent with Ar between cycles, install extractor, ion pump
Bake 48 hours, 250°C
Measure pressure with extractor gauge

## Slide 32: 350 kV chamber coating
Outgassing after 400°C, 100 hr heat treatment ~1x10-13 TorrL/s/cm2
Pressure (x-ray limit corrected, nitrogen equivalent) ~1.5x10-12 Torr
pump speed ~0.07 L/s/cm2 (extrapolated from ultimate pressure, outgassing rate)
No flaking evident
Does the thin coating and wire rather than basket help?

## Slide 33: Conclusions
TiN coating studies
  Artificially low outgassing rate due to small pump speed
a-Si coating
  similar outgassing to the chamber before the coating
JLab’s NEG coating setup (DC sputter, no magnetron)
  Low pump speeds (but net pump rather than gas load)
  Longer coating duration (working on automation)
  Issues with flaking – possible high voltage issue? (optimizing)
Non-uniform chambers can be coated and the coating + IP nearly XHV
Other fields interested in this kind of work
Lots of room for improvement

## Slide 34: Pressure measurement backgrounds
measured
minimized
measured
Chart: Repeller voltage (V)
| 85.381 | 94.900999999999996 | 105.176 | 114.982 | 124.747 | 135.21600000000001 | 145.67400000000001 | 154.90899999999999 | 165.51 | 175.01 | 184.816 | 194.85599999999999 | 205.01900000000001 | 214.85499999999999 | 225.04900000000001 | 234.93600000000001 | 245.17 | 255.44499999999999 | 265.69 | 275.29199999999997 | 285.73 | 295.57600000000002 | 305.58600000000001 | 315.31 | 325.34100000000001 | 335.09500000000003 | 345.57400000000001 | 354.78800000000001 | 364.69600000000003 | 375.42 | 384.93 | 395.12299999999999 | 405.20499999999998 | 415.68400000000003 | 425.35700000000003
10 v steps, 5 min | 20.313 | 20.445 | 21.715 | 22.557 | 23.773 | 24.596 | 28.104 | 29.26 | 31.013 | 35.232 | 36.703 | 42.438 | 42.778 | 42.53 | 42.565 | 40.863 | 40.414 | 38.585 | 35.604 | 35.173 | 31.557 | 26.468 | 23.498 | 22.187 | 19.501 | 20.027 | 18.644 | 19.714 | 19.81 | 19.364 | 19.902 | 19.082 | 19.082 | 18.923 | 21.317
background | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408
Chart: Days
Extractor:Bare Steel | 2.2e-11 | 6e-12 | 3.83e-12 | 3.52e-12 | 2.58e-12 | 2.29e-12
BBB:Bare Steel | 1.58e-11 | 4.3e-12 | 4.61e-12 | 3.86e-12 | 3.57e-12 | 2.8e-12 | 2.46e-12 | 2.5e-12 | 3.8e-12 | 4.84e-12 | 2.96e-12 | 2.5e-12 | 2.96e-12
Chart: Days
Extractor:Bare Steel | 2.2e-11 | 6e-12 | 3.83e-12 | 3.52e-12 | 2.58e-12 | 2.29e-12
BBB:Bare Steel | 1.58e-11 | 4.3e-12 | 4.61e-12 | 3.86e-12 | 3.57e-12 | 2.8e-12 | 2.46e-12 | 2.5e-12 | 3.8e-12 | 4.84e-12 | 2.96e-12 | 2.5e-12 | 2.96e-12
x-ray limit
heating
ESD

## Slide 35: XHV gauges
Extractor gauge
  available commercially for decades
  x-ray limit reduced through geometry
  x-ray limit quote: 7.5x10-13 Torr
Watanabe BBB (Bent Belt Beam) gauge
  Uses Leybold IE540 controller
  230° deflector BeCu housing
  JVSTA 28, 486 (2010)
  Quoted limit: 4x10-14 Torr
extractor
BBB

## Slide 36: x-ray limit measurement
Extractor Gauge
Chart: Repeller voltage (V)
| 85.381 | 94.900999999999996 | 105.176 | 114.982 | 124.747 | 135.21600000000001 | 145.67400000000001 | 154.90899999999999 | 165.51 | 175.01 | 184.816 | 194.85599999999999 | 205.01900000000001 | 214.85499999999999 | 225.04900000000001 | 234.93600000000001 | 245.17 | 255.44499999999999 | 265.69 | 275.29199999999997 | 285.73 | 295.57600000000002 | 305.58600000000001 | 315.31 | 325.34100000000001 | 335.09500000000003 | 345.57400000000001 | 354.78800000000001 | 364.69600000000003 | 375.42 | 384.93 | 395.12299999999999 | 405.20499999999998 | 415.68400000000003 | 425.35700000000003
10 v steps, 5 min | 20.313 | 20.445 | 21.715 | 22.557 | 23.773 | 24.596 | 28.104 | 29.26 | 31.013 | 35.232 | 36.703 | 42.438 | 42.778 | 42.53 | 42.565 | 40.863 | 40.414 | 38.585 | 35.604 | 35.173 | 31.557 | 26.468 | 23.498 | 22.187 | 19.501 | 20.027 | 18.644 | 19.714 | 19.81 | 19.364 | 19.902 | 19.082 | 19.082 | 18.923 | 21.317
background | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408 | 21.408
Bent Belt Beam Gauge
Chart: Deflector voltage (V)
| 84.983000000000004 | 89.492999999999995 | 95.216999999999999 | 99.768000000000001 | 104.86 | 110.655 | 114.982 | 120.57299999999999 | 125.634 | 130.73599999999999 | 135.328 | 140.34800000000001 | 145.64400000000001 | 150.30699999999999 | 155.184 | 160.26599999999999 | 164.77600000000001 | 169.72399999999999 | 174.59100000000001 | 180.26499999999999 | 184.816 | 189.82599999999999 | 194.815 | 199.53899999999999 | 205.15100000000001 | 209.6 | 214.83500000000001 | 220.13
3BG31July2013c | -0.896 | -0.777 | 0.593 | 0.068 | -0.372 | -0.942 | -0.56 | -0.942 | 0.959 | 3.165 | 8.951 | 22.336 | 23.51 | 26.686 | 26.598 | 27.171 | 26.82 | 24.874 | 23.827 | 23.587 | 20.655 | 18.987 | 15.92 | 12.836 | 9.892 | 8.155 | 4.943 | 3.189
1Aug2013c | -2.217 | -2.015 | -1.433 | -1.983 | -1.614 | -1.245 | -1.04 | -1.718 | -1.666 | 1.702 | 9.296 | 19.034 | 24.498 | 26.288 | 0 | 27.273 | 26.8 | 25.239 | 24.748 | 22.495 | 20.626 | 17.823 | 16.92 | 12.962 | 11.379 | 7.691 | 6.384 | 3.917 | 1.485 | 1.028 | 0.867 | 0.167 | -0.198 | -0.005 | -0.028 | -0.257 | -0.916 | -0.655 | 0.697
5-Aug | -2.141 | -0.445 | -0.616 | -0.186 | 0.531 | -1.762 | -0.492 | -0.957 | -0.018 | 2.264 | 7.857 | 19.282 | 25.038 | 28.272 | 27.187 | 27.076 | 26.488 | 25.398 | 23.501 | 23.45 | 21.717 | 20.151 | 17.646 | 14.883 | 11.377 | 7.791 | 4.666 | 3.808 | 1.375 | 1.625 | 0.108 | -0.731 | -1.928 | 0.206 | 0.195 | -0.041 | -0.112 | 1.503 | 0.405
extractor back on | -1.06 | -0.108 | 0.468 | -0.249 | -2.083 | -0.381 | -0.542 | 0.582 | -0.315 | 2.079 | 8.736 | 19.289 | 25.349 | 27.684 | 27.806 | 28.181 | 26.13 | 26.001 | 24.21 | 24.452 | 21.961 | 20.271 | 16.861 | 13.62 | 10.78 | 7 | 5.526 | 2.461 | 1.233 | 0.3 | 0.331 | 0.606 | -0.239 | -0.292 | -1.197 | -1.136 | -1.142 | -2.154 | -1.53
x-ray background
x-ray background