## Slide 1
Milliampere beam studies using high polarization photocathodes at the CEBAF Photoinjector
Joe Grames, Phil Adderley, B. Bullard, John Hansknecht,
C. Hernandez-Garcia, G. Palacios, Matt Poelker,
Daniel Moser, Marcy Stutzman, Shukui Zhang
LHeC, FCC-eh and PERLE Workshop
LAL Orsay
June 27-29, 2018

## Slide 2: Outline
PEPPo – an application requiring milliampere polarized electron beams
Ion bombardment, the dominant lifetime limiting mechanism of polarized photocathodes
To operate at mA current without interruption, requires kC charge lifetime
R&D to extend the charge lifetime of polarized electron sources

## Slide 3: Polarized Electrons for Polarized Positrons
electron beam polarization
85.2 ± 0.6 ± 0.7 %
PEPPo demonstrated efficient transfer of polarization from electrons to positrons by bremsstrahlung + pair creation at low energy (<10 MeV).
In the range of 10-100 MeV conversion efficiency 10-4 to 10-3 suggests useful polarized positron current benefits from milliamperes of polarized electrons
D. Abbott et al, "Production of Highly Polarized Positrons Using Polarized Electrons at MeV Energies", Phys. Rev. Lett, 116, 214801 (2016)

## Slide 4: Polarization Studies at mA Beam Current
First measurement of beam polarization at JLab from superlattice (GaAs/GaAsP photocathode at milli-Ampere current
CEBAF 5 MeV Mott polarimeter: on-going effort to ascribe sub-percent accuracy (collaborators D. Moser, X. Roca-Maza, Charles Sinclair, M.J. McHugh, and Tim Gay)
CEBAF 5 MeV Mott Polarimeter
Chart: Polarization (%)
| 1.67 | 10.4 | 50.5 | 100.5 | 250.5 | 504 | 755 | 1011 | 1.06
 | 85.6704 | 84.5218 | 84.3896 | 85.3479 | 84.9536 | 86.116 | 84.7714 | 85.9647 | 87.1486

## Slide 5
CEBAF Polarized Inverted Load Lock Gun (Spring 2017)
  CEBAF Load Lock Photogun (-130kV)
1 mA 86 C/day
5 mA 432 C/day
10 mA 860 C/day
50 mA 4320 C/day

## Slide 6
Recent CEBAF Polarized Source Performance
Gun2 Photocathode (Fall 2016 – Spring 2017)
  Strained Superlattice GaAs/GaAsP #5756-4
  Good Polarization 85-87% (measured at Mott)
  Good QE > 1% after activation
  Lifetime about 200C (s4D ~ 1mm) with intensity < 200mA

## Slide 7: Ion Bombardment

## Slide 8: Improving Lifetime with Larger Laser Size
J. Grames, et al., Phys. Rev. ST Accel. Beams 14 043501 (2011)
GaAs @ 532nm

## Slide 9: Improving charge lifetime with GaAs/GaAsP
Indeed, we enhanced the Charge Lifetime for QWeak by a factor of four when doubling the laser spot size from 0.5 mm to 1.0 mm (diameter)
but milliampere applications require kiloCoulomb charge lifetime to provide uninterrupted operation of reasonable duration

## Slide 10: Lifetime Studies at mA Beam Current
Polarized positrons for CEBAF, and on-going discussions with BNL related to high current eRHIC EIC, prompted experiments at CEBAF to characterize lifetime vs. laser spot size using high-polarization photocathodes
CEBAF 130kV polarized “inverted gun” with load lock
Make beam here
(-130kV, 0-1.5mA, 0-3pC)
Deliver it here
(Faraday cup)
Vary the laser beam size
(f=499 MHz, st ~ 50 ps)
Monitor vacuum and radiation levels along beam line

## Slide 11
Variation of Laser Spot Size
Photocathode diameter 5 mm (defined by a mask during activation)
Varied laser diameter s4D ~1-5 mm (area 3-20 mm2)
Laser profile defined at photocathode plane

## Slide 12: Lifetime Studies at mA Beam Current
X-ray detectors were distributed along beam line at locations of likely beam loss, e.g. apertures (where beam pipe size changes or intentional apertures).
Beam Size

## Slide 13
Sensitivity of x-ray detectors for beam loss
While increased vacuum levels are a good indicator of decreased photocathode lifetime, in this study we observe little indication of beam loss.
X-ray monitors demonstrate high sensitivity and localization for beam intentionally lost. Sensitivity as good as 60 pA (typ. 1-5 nA)
loss
x-ray
loss
vacuum

## Slide 14
Radiation Level vs. Intensity
Low x-ray levels (<10 Hz) along beam pipe (35mm) suggest ~nA loss.
High x-ray levels (>100’s Hz) are in close proximity to smallest aperture (3mm)

## Slide 15
Vacuum Level vs. Intensity
Vacuum levels similarly increase with beam current, but “scatter” in vacuum level downstream of the gun larger than with the x-ray monitors.

## Slide 16: Lifetime Studies at mA Beam Current
1mA
Required laser power, slope proportional to QE decay
Increasing laser size reduces QE decay proportionally
Adjust beam size to decrease x-ray level

## Slide 17
Emittance Aperture Interception vs. Lifetime
Interception on a 4mm aperture measures beam size
Largest interception (circles) occur with smallest laser size (space charge)

## Slide 18
Radiation Level vs. Lifetime
The best charge lifetime is achieved when x-ray levels are smallest.

## Slide 19
Vacuum vs. Lifetime
Correlation of vacuum with charge lifetime most evident near the Gun
Vacuum levels generally not as sensitive as x-ray levels

## Slide 20: First Results: GaAs/GaAsP at mA Current
  CEBAF charge lifetime improves with spot size, as expected, but eventually beam size becomes “too large”
  Laser diameters greater than ~4 mm (4 sigma) will require properly designed cathode/anode electrodes, to ensure 100% transmission, to maintain excellent vacuum, to minimize ion bombardment
1 mA for 7 days is 600 C
1mA(2007)
4mA(2011)
CEBAF

## Slide 21
Managing Laser Power to Improve Charge Lifetime
A large fraction of laser light (33%) is reflected from GaAs leading to the possibility of “stray” electrons, a bad thing…
The remaining light is mainly absorbed in GaAs substrate, leading to heating, also a bad thing…
Laser OFF
200 mW
300 mW
100 mW
(6mA/%/W)
I = 1 mA
&
QE < 1%
=> P > ~100’s mW

## Slide 22: Benefits of Distrubted Bragg Reflector (DBR)
Enhanced absorption occurs only at specific laser wavelengths
non-DBR Photocathode : absorption in the GaAs/GaAsP superlattice < 5%
  Most light passes into the substrate leading to unwanted heating
DBR photocathode : absorption in the GaAs/GaAsP superlattice > 20%
  Less light required to make required beam, less light means less heat
Promising for high current initiatives like polarized positrons at CEBAF and EIC
Non-DBR photocathode
DBR photocathode
Photocathode with DBR
Photocathode without DBR
(57 layers!)

## Slide 23: World Record QE from High Polarization Photocathode
Others have tried…but very difficult to obtain QE enhancement at the laser wavelength that also provides high polarization, CEBAF lasers operate at ~ 776 nm (doubled-telecom lasers)
Standard strained-superlattice
  QE = 0.89%
  Polarization = 92%
DBR
  QE = 6.4%
  Polarization = 84%
The highest reported QE of any high polarization photocathode
Excellent candidate for mA operations, will test at CEBAF this shutdown
SBIR partnership
W. Liu, S. Zhang, M. Stutzman, M. Poelker, Y. Chen, W. Lu, and A. Moy, Appl. Phys. Lett. 109, 252104 (2016)

## Slide 24: GaAs Photocathode Polarization vs. Time
30 mA/W
Bulk GaAs
1 mA/W
100 nm
Strained GaAs
Strained Superlattice GaAs/GaAsP
6 mA/W
100 nm
14 Layers
Photocathode capability (polarization and QE) has grown significantly.
Pe- 35% 35% 75% 75% 85% 89%
Ie- 30mA 100mA 50mA 100mA 150mA 200mA
1995 1998 1999 2000 2004 2017
SLSP-DBR
30 mA/W
?

## Slide 25: Inverted-Insulator Photoguns
CEBAF 200 kV Gun
350 kV gun for GTS and UITF
with optimized triple point shields and mildly conductive insulators
Both designs, maximum field strength < 10 MV/m
Notes: Interior Page Design 2

## Slide 26: 3 photoguns with barrel polished electrodes
CEBAF 200 kV
Installed June 2018
Commissioning now.
UITF 350 kV
Polarized Gun
Under assembly
GTS 350 kV
In operation since Nov. 2016 with CsK2Sb photocathode:
500 uA magnetized beam
4.5 mA non-magnetized

## Slide 27: Summary
Extending the charge lifetime of today’s spin polarized GaAs photoguns from tens to thousands of Coulombs is a requirement for extended uninterrupted operation at milliampere beam current
These new results demonstrate highest charge lifetime from high polarization GaAs/GaAsP photocathodes by increasing laser spot sizes using at mA current but…
Managing ALL of the beam remains essential. These results suggest CEBAF gun requires larger electrodes for sustainable milliampere operation
New DBR photocathode is an excellent candidate for high current (mA) polarized electron beam initiatives. Lifetime tests at CEBAF to happen soon, during this shutdown
Managing application of high voltage to the cathode and eliminating field emission are essential for achieving long charge lifetime
Importantly, realistic dynamic lifetime models are critically needed to to separate and understand the dependencies of operational gun conditions.

## Slide 28
Backup Slides

## Slide 29: Inverted Insulator Photoguns
CEBAF 130 kV, used since 2010
350 kV gun for GTS and UITF
Longer “R30” insulator
Spherical electrode

## Slide 30: The Reality of HV Breakdown
The first test with R30 pure alumina ceramic suffered breakdown at ~315kV with subsequent puncture at 330kV.
A second test with a new R30 pure alumina suffered breakdown at ~315 kV.
* M. BastaniNejad, A. A. Elmustafa, E. Forman, J. Clark, S. Covert, J. Grames, J. Hansknecht, C. Hernandez-Garcia, M. Poelker and R. Suleiman, “Improving the performance of stainless-steel DC high voltage photoelectron gun cathode electrodes via gas conditioning with helium or krypton,” Nucl. Instr. and Meth. in Phys. Res. A, Vol. 762, pp. 135–141, 2014
Field emission managed via krypton-processing*, i.e., voltage was applied with ~10-5 Torr krypton added to gun chamber

## Slide 31: Careful design of triple-junction-shield
Gradients shown for 350 kV
Simulationsby Y. Wang
Ceramic
HV plug
Design overall shape for low gradient here !!

## Slide 32: The ultimate metric of success: High Voltage
Reached
360 kV in 70 hours
Vacuum and radiation levels indistinguishable from bkgd at 350kV
10 MV/m at 350 kV

## Slide 33
Example Lifetime Run (1 mA ,14mm2)

## Slide 34
Photocurrent Dependence of Laser Profile
The scaling of photocathode lifetime, however, depends on the convolution of the laser profile and the changing photocathode QE.
The QE hole at the electro-static center (left) is imaged on a view screen (right) when using a laser with a diameter than a very “deep” QE hole.

## Slide 35
Lifetime Dependence of Laser Position/Profile
Bulk GaAs, 532nm
5mm active area
PHYSICAL REVIEW SPECIAL TOPICS - ACCELERATORS AND BEAMS 14, 043501 (2011)
Dependence on proximity to the electro-static center has been thoroughly measured with bulk GaAs.
We have begun a similar study...when CEBAF operations permit.
positon
size

## Slide 36
We don’t run beam from the electrostatic center of the cathode/anode
Laser
IN
Electrons
OUT
Ions create QE trough to electrostatic center
Laser spot diameter <1 mm can be moved to different locations on the photocathode (5mm)
Pragmatically Avoiding the “EC”
Here, QE ion damage forms QE trough from four spots to EC.
Gas