## Slide 1: Magnetized Electron Beam Development
JLEIC Collaboration Meeting
April 3, 2017
R. Suleiman, D. Bullard, F. Hannon, C. Hernandez-Garcia, A. Mamun, Y. Wang,
J. Grames, J. Hansknecht, R. Kazimi, G. Krafft, M. Poelker,
S. Wijethunga, P. Adderley, J. Benesch, S. Zhang

## Slide 2: Recall Old Results – Summer 2016
First insulator conditioned to 325 kV
1 mA non-magnetized
Learning how to use new photocathode
Need mask and ion precipitator
Notes: Interior Page Design 2

## Slide 3: Outline
Magnetized Electron Source
  K2CsSb Photocathode
  Gun HV Chamber
  Gun Solenoid
  Steel Photocathode Holders (Pucks)
  Beamline
Generation of Magnetized Beam
Measuring Magnetization
  Slit and Viewscreens
  TE011 Cavity: new method
Outlook

## Slide 4
Beamline
Gun Solenoid
Photocathode
Preparation
Chamber
Gun HV Chamber
We are now running magnetized beam to Faraday Cup – to dump in two weeks

## Slide 5: Photocathode Preparation Chamber
Bias puck to monitor photocurrent during activation and measure QE in-situ
Control gap between puck and Cs-K effusion source for precise film growth
Use a mask for reducing active area to minimize beam halo

## Slide 6: K2CsSb Quantum Efficiency ~ 6%
K2CsSb grown with a mask – limit photocathode active area (3 mm ɸ) to reduce beam halo
Active area can be offset from electrostatic center
5 mm active area also available
Entire photocathode can be activated too
Work of M. Mamun and Y. Wang

## Slide 7
Gun HV Chamber
Upgraded HV Chamber with new doped alumina insulator and newly designed HV shed (triple point junction shield) to lower gradient from 12 MV/m to 10 MV/m at 350 kV
Gun HV operating at 300 kV with gun solenoid at 400 A

## Slide 8
Size | 11.811" ID, 27.559" OD, 6.242" Z
Conductor | L=500 m, A=0.53 cm2 16 layers by 20 turns
Coil Weight | 254 kg (560 lbs)
Resistance | 0.198 Ω
Field at Photocathode | 1.4 kG
Voltage | 79 V
Current | 400 A
Mapped and installed at GTS
Using new spare CEBAF Dogleg magnet power supply (500A, 80V)
Learned that gun solenoid can influence field emission
First trials with gun at HV and solenoid on resulted in field emission and vacuum activity
HV conditioned gun with solenoid up to 400 A
Gun Solenoid

## Slide 9
New steel holders (pucks) to enhance field to 2.0 kG at photocathode. Two types:
  Molybdenum and carbon steel hybrid puck
  Carbon steel puck
Molybdenum
Steel
Steel
New Steel Photocathode Holders

## Slide 10
Beamline
Slit
YAG Screen
Shield Tube

## Slide 11
Magnetized Beam at GTS
Generated magnetized beam on March 8
Measured magnetization at 300 kV and solenoid field from 0 – 1.4 kG
Delivered 20 µA to Faraday Cup – higher currents once beamline to dump is ready

## Slide 12
Measuring Magnetized Beam – I
Use slit and viewscreens to measure mechanical angular momentum:
: solenoid field at photocathode
: laser rms size

## Slide 13
0 A
400 A
σ1 = 3.7 mm
σ2 = 4.9 mm
φ = 15°
= 38 neV s
= 38 neV s

## Slide 14
Measuring Magnetized Beam – II
Having a non-invasive technique to measure beam magnetization is very critical for JLEIC e-cooler. An RF cavity could be right device. Cavities distributed around e-cooler will monitor magnetization and others installed inside cooling solenoid will ensure magnetization is completely removed during cooling process. Once beam exists solenoid, cavities measure whether magnetization is fully restored.
RF field will be excited by rotating bunched beam producing an easily detectable signal – beam will deposit longitudinal energy into cavity, but not angular momentum
Coupling to both electric and magnetic fields – expect main contribution to signal from electric field

## Slide 15: TE011 Mode in Pill-box Cavity

## Slide 16
Magnetic Moment of Magnetized Beam
Magnetic moment along beam axis:
at photocathode
at cavity
For Gaussian beam with sigma of = 1 mm and = 2 kG :
  Average canonical angular momentum is = 200 (neV s) at photocathode
  After exiting solenoid = 200 (neV s) = 3x108 ħ
  Beam angular frequency, = 1.1x1010 rad/s

## Slide 17
TE011 Cavity Magnetized Beam Test
Plan to build and install a cavity at GTS to measure beam magnetization in collaboration with Electrodynamic, NM (Brock Roberts) and SRF Institute (Jiquan Guo et al.) – good project for a student
Will be part of year 3 LDRD proposal – requires $20k for shop and materials
Axially-symmetric electric field mode cannot create angular momentum for a passing electron beam – one must take into account presence of associated RF magnetic field – due to conservation of canonical angular momentum before and after cavity
Can we generate magnetized beam with TE011 cavity?

## Slide 18: Outlook: April – September
Measure magnetization vs gun solenoid field and laser size
Benchmark simulation against measurements
Measure photocathode lifetime vs magnetization at 5 mA and 300 kV
Measure magnetization with steel/hybrid puck
Study beam halo and beam loss vs magnetization
Install RF laser
Install TE011 cavity and commission with magnetized beam
Sajini Wijethunga, student from ODU started her Ph.D. thesis on magnetized beam (advisor: Jean Delayen, funded by 75% JLab + 25% ODU)
Plan to submit LDRD proposal for 3rd year funding – TE011 cavity included