## Slide 1: Spin Polarization Sensitivity of Electrons Emitted from Bulk GaAs Photocathodes
Wei Liu
Brookhaven National Laboratory
Matt Poelker, Shukui Zhang, Marcy Stutzman
Jefferson Lab
PSTP 2017, October 19, 2017

## Slide 2: Production of spin-polarized electrons
The energy bands diagram
The optical transitions
For ,
In general,
Notes: The energy bands diagram of unstrained GaAs at the center of Brillouin zone and the optical transitions between sublevels for circularly polarized light, right circularly polarized light (solid lines) and left circularly polarized light (dashed lines), with the relative transition probabilities given by circled numbers

## Slide 3: Factors affected the spin polarization
Absorption of photons
Transportation of photoelectrons
Emission of photoelectrons
Material quality
Temperature
Dopant density
Thickness
Activation layer
Surface contamination
Laser
Others
Three-Step Model
The QE is also affected by these factors

## Slide 4: Spin relaxation mechanism
The equilibrium polarization of electrons in conduction band
For highly doping p-type GaAs photocathodes, the spin relaxation time can be given by , with

## Slide 5: BAP and DP mechanism
Temperature dependence of the spin relaxation rate

## Slide 6: Evaluation of electron escape probability
The QE can be derived base on Three-Step Model
The electron escape probability can be solved from this equation and given by
By measuring the QE as a function of the wavelength, one can obtain the electron escape probability that would prove relevant for interpreting polarization behavior

## Slide 8: Measurement of electron spin polarization (ESP)
Schematic of experimental apparatus for measuring ESP of photocathodes
Spin-polarized electrons incident to the target and scatter with target nuclei
The cross section drawing of Mott polarimeter
CEM
Target
CEM
A=

## Slide 9: Experiment
Cleave plane | (111A) | (110) | (100) | (100) | (100)
Dopant | GaAs-Zn | GaAs-Zn | GaAs-Zn | GaAs-Zn | GaAs-Zn
Orientation | (111A) ±0.5° | (110) ±0.5° | (100) ±0.5° | (100) ±0.5° | (100) ±0.5°
Carrier concentration (a./c.c.) |  |  |  |  | 
Resistivity (ohm.cm) |  |  |  |  | 
Mobility (cm2/v.s.) |  |  |  |  | 
Thickness (µm) |  |  |  |  | 
Cleave plane | (111A) | (110) | (100) | (100) | (100)
Dopant | GaAs-Zn | GaAs-Zn | GaAs-Zn | GaAs-Zn | GaAs-Zn
Orientation | (111A) ±0.5° | (110) ±0.5° | (100) ±0.5° | (100) ±0.5° | (100) ±0.5°
Carrier concentration (a./c.c.) |  |  |  |  | 
Resistivity (ohm.cm) |  |  |  |  | 
Mobility (cm2/v.s.) |  |  |  |  | 
Thickness (µm) |  |  |  |  | 
mini-Mott chamber
Dopant dependence: , ,
Temperature dependence: 300 K, 195 K, 77 K
Activation layer dependence: Cs, 1st, 6th, 13th yo-yo cycle
Cleave plane dependence: GaAs(100), (110) and (111A)
Experiment content

## Slide 10: Photocurrent evolution while cooling GaAs
Cathodes cool down from 300 K to 77K
High dopant
  300K: QE=6.9%
  77K: QE=10%
Low dopant
  300K: QE=1.5%
  77K: QE=0.79%
300 K
77 K
77 K

## Slide 11: Temperature and dopant dependence
ESP@300 K: high dopant: 30%, low dopant: 41%
ESP@77 K: high dopant: 41%, low dopant: 52%
300 K
77 K

## Slide 12: Temperature and dopant dependence
Polarization is inversely proportional to temperature and dopant density
Notes: Lower dopant concentration, higher ESP; Lower temperature, higher ESP

## Slide 13: Activation layer dependence
Max ESP
only Cs: 36%
1st cycle: 32%
6th and 13th cycles: 30%
Thinner thickness of activation layer, lower QE and Pesc
Notes: QE and ESP for bulk GaAs (110) with dopant concentration of as a function of surface activation layer. Cycle number refers to the number of applications of Cs and F
QE and ESP for bulk GaAs (110) with dopant concentration of 1×〖10〗^19 〖𝑐𝑚〗^(−3) as a function of surface activation layer. Cycle number refers to the number of applications of Cs and F

## Slide 14: Cleave plane dependence
Cleave plane samples (100) and (110) provided higher QE compared to cleave plane (111A)
There was no ESP sensitivity to crystal orientation (plane)
Notes: QE and ESP of bulk GaAs with three different cleave planes, Zn dopant concentration 11019 cm-3, measured at room temperature
QE and ESP of bulk GaAs with three different cleave planes, Zn dopant concentration 1×1019 cm-3, measured at room temperature

## Slide 15: Reported maximum ESP values from GaAs
Reference | note | Dopant Concentration (cm-3) | Temperature (K) | Max ESP (%)
This work |  |  | 77 | 52
Ref. 1 (Pierce) | PEA |  | < 10 | 54
Ref. 2 (Maruyama) | 0.2 um thick |  | 300 | 49
Ref. 3 (Fishman) |  |  | 4.2 | 45
Ref. 4 (Hartmann) | Time resolved – Max. value |  | 300 | 43
Reference | note | Dopant Concentration (cm-3) | Temperature (K) | Max ESP (%)
This work |  |  | 77 | 52
Ref. 1 (Pierce) | PEA |  | < 10 | 54
Ref. 2 (Maruyama) | 0.2 um thick |  | 300 | 49
Ref. 3 (Fishman) |  |  | 4.2 | 45
Ref. 4 (Hartmann) | Time resolved – Max. value |  | 300 | 43
[1] D. T. Pierce and F. Meier, Phys. Rev. B 13, 5484 (1976)
[2] T. Maruyama, R. Prepost, E. L. Garwin, C. K. Sinclair, B. Dunham, and S. Kalem, Appl. Phys. Lett. 55, 1686 (1989)
[3] Guy Fishman, and Georges Lampel, Phys. Rev. B 16, 820 (1977)
[4] P. Hartmann, Aufbau einer gepulsten Quelle polarisierter Elektronen, Dissertation, Shaker Verlag, Aachen, 1998
Notes: polarization exceeds max theory value, but also point out that Dan Peirce saw polarization > 50%
Sure, this might be caused by systematic error, wrong analyzing power, or interesting physics

## Slide 16: Maximum ESP versus Pesc
ESP is inversely proportional to Pesc (excepted “cleave plane”)
In general, it can be said that ESP can be increased at the expense of QE

## Slide 17: Conclusions
A systematic experimental evaluation of polarization sensitivities to four factors has been presented
Both Lower temperature, lower dopant concentration and thinner activation layer lead to higher polarization.
Polarization can be increased at the expense of QE
A maximum polarization of 52% was obtained from low dopant sample (51017 cm-3 ) at low temperature (77 K)
This work can be found at: Wei Liu, etc., J. Appl. Phys. 122, 035703 (2017)

## Slide 18: Thanks for your attention