## Slide 1
Milliampere beam studies using high polarization photocathodes at the CEBAF Photoinjector
J. Grames
JLAAC Review September 13-15, 2017

## Slide 2: Outline
Ion bombardment, the dominant lifetime limiting mechanism of polarized photocathodes
PEPPo – an application requiring milliampere polarized electron beams
To operate at mA current without interruption, requires kC charge lifetime
R&D to extend the charge lifetime of polarized electron sources

## Slide 3: Ion Bombardment

## Slide 4: Polarized Electrons for Polarized Positrons
electron beam polarization
85.2 ± 0.6 ± 0.7 %
(PEPPo Collaboration) D. Abbott et al., Phys. Rev. Lett. 116 (2016) 214801
Bremsstrahlung produced by polarized electrons results in efficient production of polarized positrons
PEPPo’s success suggests nanoAmps of polarized positrons for CEBAF using milliamperes of polarized electrons
D. Abbott et al, "Production of Highly Polarized Positrons Using Polarized Electrons at MeV Energies", Phys. Rev. Lett, 116, 214801 (2016)

## Slide 5: High Polarization Photocathodes
30 mA/W
Bulk GaAs
1 mA/W
100 nm
Strained GaAs
Strained Superlattice GaAs/GaAsP
6 mA/W
100 nm
14 Layers
Photocathode capability (polarization and QE) has grown significantly.
Pe- 35% 35% 75% 75% 85% 89%
Ie- 30mA 100mA 50mA 100mA 150mA 200mA
1995 1998 1999 2000 2004 2017
with DBR
30 mA/W
Test
at CEBAF

## Slide 6: Improving Lifetime with Larger Laser Size
J. Grames, et al, Phys. Rev. ST Accel. Beams 14 043501 (2011)
GaAs @ 532nm

## Slide 7: Improving charge lifetime with GaAs/GaAsP
Indeed, we enhanced the Charge Lifetime for Qweak by a factor of four when doubling the laser spot size from 0.5mm to 1.0 mm (diameter)
but milliampere applications require kiloCoulomb charge lifetime to provide uninterrupted operation of reasonable duration

## Slide 8: Lifetime Studies at mA Beam Current
Polarized positrons for CEBAF, and on-going discussions with BNL related to high current eRHIC EIC, prompted experiments at CEBAF to characterize lifetime vs. laser spot size using high-polarization photocathodes
CEBAF 130kV polarized “inverted gun” with load lock
Make beam here
Deliver it here
Vary the laser beam size
Monitor vacuum and radiation
1mA
Required laser power, slope proportional to QE decay
Increasing laser size reduces QE decay proportionally
Note:
1 mA 86 C/day
5 mA 432 C/day
10 mA 860 C/day
50 mA 4320 C/day

## Slide 9: First Results: GaAs/GaAsP at mA Current
  CEBAF charge lifetime improves with spot size, as expected, but eventually beam size becomes “too large”
  Laser diameters greater than ~4 mm (4 sigma) will require properly designed cathode/anode electrodes, to ensure 100% transmission, to maintain excellent vacuum, to minimize ion bombardment

## Slide 10: Polarization Studies at mA Beam Current
First measurement of polarization from superlattice photocathode at milliampere current
CEBAF 5 MeV Mott polarimeter: on-going effort to ascribe sub-percent accuracy (collaborators D. Moser, X. Roca-Maza, Charles Sinclair, M.J. McHugh, and Tim Gay)
CEBAF 5 MeV Mott Polarimeter
Chart: Polarization (%)
| 1.67 | 10.4 | 50.5 | 100.5 | 250.5 | 504 | 755 | 1011 | 1.06
 | 85.6704 | 84.5218 | 84.3896 | 85.3479 | 84.9536 | 86.116 | 84.7714 | 85.9647 | 87.1486

## Slide 11: Summary
Extending the charge lifetime of today’s spin polarized GaAs photoguns from tens to thousands of Coulombs is a requirement for extended uninterrupted operation at milliampere beam current
These new results demonstrate improved charge lifetime with larger laser spot sizes using GaAs/GaAsP photocathodes at mA current but…
Managing ALL of the beam remains essential. These results suggest CEBAF gun requires larger electrodes for sustainable milliampere operation
New DBR photocathode is an excellent candidate for high current (mA) polarized electron beam initiatives. Lifetime tests at CEBAF to happen soon, during this shutdown
Thanks to P. Adderley, B. Bullard, J. Hansknecht, M. Stutzman, S. Zhang

## Slide 12
Backup Slides

## Slide 13: Ions Bombarding the Electrostatic Center
Ionized gas focused at electrostatic center
cathode
electrons OUT
anode
laser IN

## Slide 14
We don’t run beam from electrostatic center
laser light IN
electron beam
OUT
Ions create QE trough to electrostatic center
Laser spot diameter ~0.5 mm and can be moved to different locations on the photocathode.
Pragmatically Avoiding the “EC”