## Slide 1: Simulations of Water Cooled Tungsten Target of Positron Source at Low e- Beam Energy (8 MeV)
Andriy Ushakov
IJCLab, Orsay
June 8, 2022
This project has received funding from the European Union’s Horizon 2020 research and innovation program under grant agreement No 824093

## Slide 2: Parameters of Primary Beam and Target of Positron Source
Beam energy: electron beam with energy of 8 MeV
Beam current: 1 mA (and 2 mA)
RMS beam size on target: 1.5 mm
Target material: pure Tungsten
Target thickness: 1 mm
Average power deposited in 1 mm thick W target: 4.4 kW (55% of e- beam power)

## Slide 3: Optimal Target Thickness (Jonathan Dumas, PhD Thesis, 2011)
3

## Slide 4: Energy Deposited by 120 MeV e- (left) and 8 MeV e- (right) in Stationary Tungsten Target
PEDD = 0.36 GeV/(e- cm3)
Edep = 0.5487 Ebeam
1 mA e- beam: Pdep = 4.4 kW
PEDD = 0.34 GeV/(e- cm3)
Edep = 0.1425 Ebeam
1 mA e- beam: Pdep = 17 kW
4
8 MeV e- , 1 mm Target Thickness
120 MeV e-, 4 mm Target Thickness

## Slide 5: Energy Deposited by 120 MeV e- (left) and 8 MeV e- (right) along Beam Axis (r = 0)
PEDD = 0.36 GeV/(e- cm3)
PEDD = 0.34 GeV/(e- cm3)
5
8 MeV e-
120 MeV e-

## Slide 6: W Rim Cooled from One Side by Copper Disk with 10mm x 20mm Cross Section of Water Channel and 2 m/s Flow (ANSYS Fluent) Beam Passing through the Target at Radius of 17.5 cm
R = 17.5 cm
Beam
W
Water
Cu

## Slide 7: 1 mA @ 8 MeV e- Beam: Average Temperature of Tungsten (left) and Temperature of Water (right) for 2 m/s Water Flow
Tmax = 32.8 °C
(120 MeV Beam: Tmax = 61 °C)
Tmax = 181 °C
(120 MeV Beam: Tmax = 260 °C)
7

## Slide 8: Average Thermal Stress (left) and Yield Strength of Tungsten vs Temperature (right)
Yield Strength (200°C) ≈ 1220 MPa
Max σvon-Mises = 214 MPa
(120 MeV Beam: σvon-Mises = 282 MPa)
Tungsten produced by Plansee
8

## Slide 9: Temperature of Tungsten moving with 4 m/s
ΔTmax ≈ 108 °C
(120 MeV Beam: ΔTmax = 120 °C)
Snapshot of T at front side after 2.5 ms
Snapshot of T at back side after 2.5 ms

## Slide 10: Temperature vs Time at Selected Point on Target moving with 4 m/s
“Global” max Temperature vs time
Temperature at selected point (probe) vs time
at R = 17.5 cm
Tmax ≈ 289 °C

## Slide 11: Thermal Stress after 2.5 ms for Beam Moving with 4 m/s
Max σvM ≈ 108 MPa

## Slide 12: Average Temperature of Tungsten at 1 mA (left) and 2 mA (right) for 2 m/s Water Flow
Tmax = 339 °C
Tmax = 181 °C
12

## Slide 13: Average Temperature of Water at 1 mA (left) and at 2 mA (right)
Tmax = 42.6 °C
Tmax = 32.8 °C
13

## Slide 14: Average Thermal Stress at 1 mA (left) and 2 mA (right)
Max σvon-Mises = 214 MPa
14
Max σvon-Mises = 432 MPa

## Slide 15: Temperature of Tungsten moving with 4 m/s at 1 mA (left) and 2 mA (right)
Tmax ≈ 289 °C
Snapshot of T at front side after 2.5 ms at 1 mA
Snapshot of T at front side after 2.5 ms at 2 mA
Tmax ≈ 549 °C

## Slide 16: Thermal Stress of Tungsten moving with 4 m/s at 1 mA (left) and 2 mA (right)
Snapshot of stress at front side after 2.5 ms at 1 mA
Snapshot of stress at front side after 2.5 ms at 2 mA
Max σvM ≈ 108 MPa
Max σvM ≈ 212 MPa

## Slide 17: Summary
Same concept of positron target can be used for the positron source at 120 MeV and 8 MeV
For target thickness of 1 mm at 1 mA and 8 MeV e- beam and 2 m/s water flow:
  Average deposited power is 4.4 kW
  Average Tmax of Tungsten = 181 °C
  Average thermal stress of Tungsten = 214 MPa
  Peak T of target moving with 4 m/s = 289 °C
  Peak thermal stress of target moving with 4 m/s = 108 MPa
For target thickness of 1 mm at 2 mA and 8 MeV e- beam and 2 m/s water flow:
  Average deposited power is 8.8 kW
  Average Tmax of Tungsten = 339 °C
  Average thermal stress of Tungsten = 432 MPa
  Peak T of target moving with 4 m/s = 549 °C
  Peak thermal stress of target moving with 4 m/s = 212 MPa

## Slide 18
Backup Slides

## Slide 19: Fatigue Strength of Tungsten. S-N Curve for Pure Tungsten at 22 °C (ANSYS Granta)

## Slide 20: Temperature of stationary tungsten target after 64 ms irradiation by 1 mA @ 8 MeV electrons