## Slide 1: New Simulations for Ion-Production and Back-Bombardment in GaAs Photo-guns
Motivation
Ion Production
Ion Tracking using GPT
QE Degradation of the CEBAF Photocathode
Conclusions/Future Work
Questions?
Josh Yoskowitz, Joe Grames, John Hansknecht, Carlos Hernandez-Garcia, Geoffrey Krafft, Gabriel Palacios-Seranno, Matthew Poelker, Sebastian Van Der Geer, Riad Suleiman, Sajini Wijethunga

## Slide 2: Motivation: Ion Back-Bombardment leads to QE Reduction
Residual gas in the photo-gun or adjacent beam line may be ionized by the electron beam
These ions may strike the photocathode, generate secondary electrons or x-rays, and desorb gas from surfaces; all leading to a reduction of the photocathode quantum efficiency (QE).
A positively biased anode should improve photocathode lifetime by limiting ion back-bombardment of the GaAs photocathode.
Anode
e-beam
Cathode
Ions
Ions

## Slide 3: Theory: Ionization Cross Section & Rate
Ionization Cross Section For H2+
= Gas density (m-3)
= Ionization cross section (m2)
= Distance traveled by electron (m)
= Electron current (A)
= Elementary charge (C)
Ion Production Rate Per Unit Length
H2+ Production Rate Per Unit Length
Example Calculations
Name | Value
Name | Value
Assuming and …
Energy
Energy

## Slide 4: GPT Ion Tracking CEBAF Gun (-130 kV Cathode, 0 kV Anode)
e-beam
Ions
Ions
Photocathode
Anode
Drift Space
Anode
Photocathode
Anode
Ez vs z On Axis
Photocathode
Anode
Photocathode
Side View of CEBAF Photo-gun
CST Model
CST Model

## Slide 5: GPT Ion Tracking CEBAF Gun (-130 kV Cathode, 1 kV Anode)
e-beam
Ions
Ions
Photocathode
Anode
Drift Space
Anode
Photocathode
Anode
Ez vs z On Axis
Photocathode
Anode
Photocathode
Side View of CEBAF Photo-gun
CST Model
CST Model

## Slide 6: Biased Anode Experiments during CEBAF Summer Run
HV Cable
Gun Chamber
Anode Bias Feedthrough
E-Beam Direction
Ran Halls A, B & C (3 lasers) from June 15 – Sep 9.
Lasers positioned about 1 mm off axis (GaAs active area 5 mm dia.)
Measured the quantum efficiency at laser position each morning, using each of the lasers.
Alternated the anode potential between 0 V and +1 kV every 2-3 weeks (every 50-60 C).
6/15
7/1
8/1
9/1
9/9

## Slide 7: QE vs Charge for the CEBAF Photocathode
1
2
3
4
Region | Anode Bias (V) | Laser A Lifetime (C) | Laser B Lifetime (C) | Laser C Lifetime (C)
1 | 0 | 181 ± 8 | 161 ± 9 | 169 ± 7
2 | 961 | 424 ± 53 | 392 ± 23 | 346 ± 16
3 | 0 | 288 ± 39 | 304 ± 14 | 297 ± 5
4 | 961 | 303 ± 18 | 302 ± 9 | 314 ± 11
Laser A:
Laser B:
Laser C:
Photocathode lifetime improved on average by ~1.5x with anode biased.
Effect is most pronounced during periods 1-3 (most of the run).

## Slide 8: QE Degradation of the CEBAF Photocathode
QE Scan Before Run (5/24/19)
QE Scan After Run (9/9/19)
Red Circle = Photocathode Active Area => NEG region 5 mm diameter at (0 mm, 0 mm)
Green Circle = Laser Spot => FWHM 1 mm positioned at (-1 mm, -1 mm)

## Slide 9: GPT Ion Simulations for CEBAF -130 kV Cathode
Parameter | Value
Macro-particle # | 105
Cathode Position | Z = 0 m
Anode Position | Z = 0.06 m
Ion Species | H2+
Ion Initial KE | 38 meV
Initial Conditions
130 kV Cathode, 0 V Anode
130 kV Cathode, 1 kV Anode

## Slide 10: Ion Position-Energy Distribution at the Photocathode
130 kV Cathode, 0 V Anode
eV
eV
130 kV Cathode, 1 kV Anode
Ions created near the cathode are least focused and have lowest kinetic energy
Ions created near the anode (upstream) are most focused due to the cathode geometry and have highest kinetic energy
Ions created near the anode (downstream) are repelled for a biased anode or behave similarly to the grounded anode

## Slide 11: Ion Position-Number Distribution at the Laser Spot
130kV Cathode, 0V Anode
130kV Cathode, 1000V Anode
x (mm)
x (mm)
x (mm)
x (mm)
y (mm)
y (mm)
y (mm)
y (mm)

## Slide 12: Biased Anode vs. Grounded Anode Comparison
Description | Ratio | Value
Total ions at the photocathode |  | 1.59
Total ions at the photocathode, weighted by incident energy |  | 1.97
Total ions within the laser spot |  | 0.994
Total ions within the laser spot, weighted by incident energy |  | 0.934
Laser A average charge lifetime |  | 
Laser B average charge lifetime |  | 
Laser C average charge lifetime |  | 
Description | Ratio | Value
Total ions at the photocathode |  | 1.59
Total ions at the photocathode, weighted by incident energy |  | 1.97
Total ions within the laser spot |  | 0.994
Total ions within the laser spot, weighted by incident energy |  | 0.934
Laser A average charge lifetime |  | 
Laser B average charge lifetime |  | 
Laser C average charge lifetime |  | 

## Slide 13: Conclusions
Higher photocathode lifetimes are observed when the anode is biased.
The charge lifetime increase for the biased anode compared to the grounded anode is similar to the decrease in the number of ions incident on the photocathode (not necessarily on the laser spot).
No significant difference in the number of ions incident on the laser spot for the biased and unbiased cases.

## Slide 14: Ongoing work: GPT Ionization Custom Element
Working on GPT custom element that allows for the real-time production of ions and secondary electrons based on the ion production rate formula
Future Work

## Slide 15: Questions?
yoskowij@jlab.org
Josh Yoskowitz
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics under contract DE-AC05-06OR23177.