## Slide 1: Bialkali Photocathode Update
Rocio Hernandez
Summer 2016

## Slide 2
Chart: Effect of cryocooling on bialkali antimonide QE
| RT1 | LN1 | RT2-a post LN1 | RT2-b post LN1 | LN2 | RT3 post LN2 | RT4 post heating | LN3 | RT5 post LN3 | RT6 post heating | LN4 | RT7 post LN4 | RT8 post heating | 6/20/16 4:44 PM | 6/20/16 6:20 PM | 6/21/16 11:14 AM | 6/21/16 5:04 PM | 6/21/16 6:30 PM | 6/22/16 9:55 AM | 6/22/16 5:14 PM | 6/22/16 6:25 PM | 6/23/16 10:10 AM | 6/23/16 3:09 PM | 6/23/16 5:45 PM | 6/24/16 10:35 AM | 6/24/16 2:10 PM
QE (no-bake) | 4.632 | 1.5459 | 2.2506 | 2.4622 | 0.54704 | 0.5631 | 5.3338 | 1.2882 | 1.524 | 5.1207 | 1.1687 | 1.5968 | 4.6115
Dark Life Time, h | 168 | 7.7754 | -3.351 | 9.1309 | 4.9503 | -6.0827 | 143.7153 | 1.2343 | -56.9917 | -19.213 | 3.8875 | -42.0408 | 11.0149
1/e Lifetime, h | 3.66 | 2.65 | 8.9
Brief ly 170 to 200 °C
H2O 34%
Brief ly 170 to 200 °C
H2O 26%
Brief ly 170 to 200 °C
H2O 37%
QE drops by 74±9 % (2σ error ) each time when cryocooled
QE can be fully recovered by desorbing water via brief heating at 170-200° C
Water PP increase (~25-40%) is detected by RGA during heating which eventually decreases at the end of heating
Lifetime improves when QE is recovered by heating
Water adsorption at 77 K causes the low lifetime

## Slide 3: Plan for following week
We will improve QE by adding more alkali and repeat at least one cycling of temperature prior to baking the system
Bake the system, activate the photocathode and repeat the process.