## Slide 1: FE-SEM foil thickness measurements

## Slide 2: Process
Mount sister foils to Si wafers
  Static for thinner foils
  “glue” with aerodag carbon suspension for thicker
Mamun makes images
Use ImageJ software to measure .tiff images saved from FE-SEM process

## Slide 3: Comparison of edge find tool
Analyzed images 05 and 06 with edge contrast on or off
Find that the edge contrast tends to skew measurements slightly larger
  Variation between images larger than variation between images
Conclusion:
  make sure to go on inside edges of “edge find” line to get more accurate results
Chart: Measured thickness
| image 02 | image 05 | image 06
original image analyzed | 0.376 | 0.388 | 0.391
edge find | 0.378 | 0.394 | 0.40061

## Slide 4: Image 06 Measurement with and without edge find

## Slide 5: Image 05: original image, edge find

## Slide 6: Statistical analysis of points measured spots selected by eye, original image
Chart: film thickness
| 0.37791625708286469 | 0.38206086536082989 | 0.38620547363879515 | 0.39035008191676035 | 0.39449469019472555 | 0.39863929847269081 | 0.40278390675065601
 | 0 | 1 | 6 | 16 | 9 | 3 | 1

## Slide 7: Thickness distribution, edge find 5613D image05, spots selected by eye
Chart: bins for foil thickness
| 0.38126488254404406 | 0.38346848320111782 | 0.38567208385819157 | 0.38787568451526533 | 0.39007928517233909 | 0.39228288582941284 | 0.3944864864864866 | 0.39669008714356035 | 0.39889368780063411 | 0.40109728845770787 | 0.40330088911478162 | 0.40550448977185538 | 0.40770809042892914 | 0.40991169108600289
data | 0 | 1 | 1 | 0 | 7 | 3 | 4 | 8 | 9 | 4 | 0 | 0 | 0 | 0

## Slide 8: Statistics from even distribution 5613 M05 even stripe distance (don’t skip any oddities)
Chart: Frequency

## Slide 9: 5613D
Image 03: 360 ± 17 nm
Image 05: 397 ± 10 nm
Image 06: 392 ± 10.5 nm

## Slide 10: Conclusions: 5613D
Original image,
Weighted mean
0.388 microns ± 0.0022
Edge find image,
Weighted mean
0.392 microns ± 0.0036
Chart: Effect of measurement style
| image 02 | image 05 | image 06
original image analyzed | 0.376 | 0.388 | 0.391
edge find | 0.378 | 0.394 | 0.40061
even stripes | 0.397 | 0.392
Even stripes image,
Weighted mean
0.389 microns ± 0.0066
Thickness is robust to within
error bars for any of the methods

## Slide 11: Foil 5134
782 ± 16 nm
772 ± 13 nm
Average: 776 nm ± 10.1

## Slide 12: Foil 6809
Image 03: 54.005 +/- 3.443
Image 04: 51.254 ± 2.766 nm
Image 06: 51.824 ± 2.252 nm
51.539 ± 2.766

## Slide 13
Ladder position | Foil number | Quoted thickness (nm) | Measured thickness (nm)
13 | 6845 | 50 ± 5 | 51.539 ± 2.766
1 | 7029 | 225 ± 22.5 | 
8 | 5613 | 350 ± 35 | 389 ± 6.6
5 | 5275 | 500 ± 50 | 
2 | 7028 | 625 ± 62.5 | 
4 | 5134 | 750 ± 75 | 776 nm ± 10.1
3 | 3057 | 870 ± 87 | 
15 | 5385 | 1000 ± 100 | 

## Slide 14
Chart: Asymmetry vs. Foil thickness
| 0.05 | 0.05 | 0.22500000000000001 | 0.35 | 0.5 | 0.625 | 0.75 | 0.87 | 1
Jan 2015 | 43.4 | 43.07 | 40.92 | 39.16 | 38.61 | 37.21 | 35.61 | 34.61 | 33.65
fit | 44.2 | 44.0612 | 43.9233 | 43.7862 | 43.65 | 43.5146 | 43.3801 | 43.2464 | 43.1135 | 42.9815 | 42.8502 | 42.7198 | 42.5901 | 42.4612 | 42.3331 | 42.2058 | 42.0792 | 41.9534 | 41.8283 | 41.704 | 41.5804 | 41.4576 | 41.3355 | 41.214 | 41.0933 | 40.9733 | 40.3837 | 39.8109 | 39.254 | 38.7125 | 38.1857 | 37.6731 | 37.1741 | 36.6881 | 36.2147 | 35.7533 | 35.3035 | 34.8649 | 34.4371 | 34.0196 | 33.6122 | 33.2144 | 32.8258
measured thicknesses | 43.4 | 43.07 | 40.92 | 39.16 | 38.61 | 37.21 | 35.61 | 34.61 | 33.65