## Slide 1
Injectors and Sources
Operations and R&D
M. Poelker
Jefferson Lab Accelerator Advisory Committee Mtg., September 13-15, 2017

## Slide 2: Outline
Matt: Record level QE from High Polarization Photocathode with Distributed Bragg Reflector (DBR)
Carlos: Photogun with Inverted-Insulator geometry, 300 kV design
Mamun: Magnetized beam for JLEIC
Joe: Evaluating the performance of CEBAF polarized injector at milliampere beam current, for a possible polarized positron source
Notes: Interior Page Design 2

## Slide 3
Always Tweaking the Design
The endless (?) quest for perfection
1
2
3
4
Lifetime increased from 10s to 100s of Coulombs
Notes: Interior Page Design 1

## Slide 4: Key Features of a Polarized Photogun
Photocathode
  High Polarization
  High QE (photoemission yield)
  Long Lifetime
Vacuum
  Static Vacuum
  Dynamic Vacuum
High Voltage
  Must eliminate field emission
Drive Laser
  Reliable, phase locked to machine
  Adequate Power
  Wavelength Tunable
Notes: Interior Page Design 2

## Slide 5: Key Features of a Polarized Photogun
Photocathode
  High Polarization
  High QE (photoemission yield)
  Long Lifetime (how to increase from 100s to 1000s Coulombs?)
Vacuum
  Static Vacuum
  Dynamic Vacuum
High Voltage
  Must eliminate field emission
Drive Laser
  Reliable, phase locked to machine
  Adequate Power
  Wavelength Tunable
Notes: Interior Page Design 2

## Slide 6: GaAs Energy Levels
Use circularly polarized light to selectively populate the conduction band with electrons of a particular spin state
Notes: Interior Page Design 2

## Slide 7: Breaking the 50% Barrier
The band gap of the substrate layer must be larger than surface layer
Lattice constants must differ enough to introduce suitable strain
Adjust lattice constant of substrate by varying concentration of third element
Lattice mismatch provides stress
Pablo Saez, PhD Thesis, SLAC Report 501, 1997
1% lattice mismatch provides equivalent force as hydraulic press!
Notes: Interior Page Design 2

## Slide 8: Benefits of Distributed Bragg Reflector
Enhanced absorption occurs only at specific laser wavelengths
non-DBR Photocathode : absorption in the GaAs/GaAsP superlattice < 5%
  Most light passes into the substrate leading to unwanted heating
DBR photocathode : absorption in the GaAs/GaAsP superlattice > 20%
  Less light required to make required beam, less light means less heat
Great for high current initiatives like polarized positrons at CEBAF and EIC
Non-DBR photocathode
DBR photocathode
Photocathode without DBR
Photocathode with DBR
(57 layers!)

## Slide 9: World Record QE from High Polarization Photocathode
Others have tried…but very difficult to obtain QE enhancement at the laser wavelength that also provides high polarization, CEBAF lasers operate at ~ 776 nm (doubled-telecom lasers)
Standard strained-superlattice
  QE = 0.89%
  Polarization = 92%
DBR
  QE = 6.4%
  Polarization = 84%
The highest reported QE of any high polarization photocathode
Excellent candidate for mA operations, will test at CEBAF this shutdown
SBIR partnership
W. Liu, S. Zhang, M. Stutzman, M. Poelker, Y. Chen, W. Lu, and A. Moy, Appl. Phys. Lett. 109, 252104 (2016)

## Slide 10: New Photoguns for…
CEBAF Injector Full-Energy Upgrade
  Replace 130 kV gun with 200 kV gun
  New baked beamline, Wien filters at proper locations
  New Quarter Cryomodule
Upgraded Injector Test Facility
  Help commission the re-designed HDIce target
  Verify the new QCM functions properly
  Polarized positron source
JLab Electron Ion Collider
  Higher voltage gun for higher bunch charge
  Very high average current un-polarized beams for cooling ions – magnetized cooling
Replace the vent/bake gun at LERF/FEL
Notes: Interior Page Design 2

## Slide 11: Inverted-Insulator Photoguns
(At 350 kV, beam is sufficiently relativistic, don’t need a “capture” section )
CEBAF 130 kV, used since 2010
350 kV gun for GTS and UITF
Longer “R30” insulator
Spherical electrode
Notes: Interior Page Design 2

## Slide 12: Parity Table
Upgrading the CEBAF Injector will help us conduct PREx, CREx and proposed parity violation experiments that are even more demanding
Notes: Interior Page Design 2

## Slide 13
Injector Upgrade
Increase gun voltage, modify Wien filters for 200kV operation
Improve baked beam line vacuum so gun does not pump on beam line
Locate H-Wien (energy filter) upstream of pre-buncher cavity
New SRF booster eliminates warm capture, RF deflection and x/y coupling
Our new “1/4 cryomodule”, or QCM:
2 cell capture section + 7 cell cavity,
should provide 10 MeV beam and introduce no x/y coupling, allow better matching, more adiabatic damping
200 kV

## Slide 14: Upgraded Injector Test Facility - UITF
TEST NEW PHOTOGUNS
COMMISSION NEW QUARTER CRYOMODULE
TEST 200 kV WIEN FILTER
UITF beamline has BPMs, pockels cell tests can happen here…..
TEST HDIce
14

## Slide 15: Upgraded Injector Test Facility
Expect keV beam operations soon
Apply RF to cold QCM this Fall
Build some portion of the MeV beamline
Work through some safety issues…
Make MeV beam during FY18

## Slide 16: Summary
Actively engaged in CEBAF operations and in close contact with Users - we know their beam requirements
Making effective use of shutdown time, to improve the CEBAF injector and demonstrate new capabilities (e.g., 5 MeV Mott polarimeter characterization, PEPPo and Bubble Chamber experiments, beam acceleration with SRF cavities at 4K, etc.,)
Gun Test Stand is bearing fruit, and we expect fruitful endeavors at UITF: testing critical components before installation at CEBAF (e.g., 200 kV gun, QCM and HDIce), pockels cell studies for parity violation experiments, production of polarized targets, bubble chamber astrophysics experiment at MeV energy, polarized positron source development, etc.,
Center for Injectors and Sources: P. Adderley, D. Bullard, J. Grames, J. Hansknecht, C. Hernandez-Garcia, Md. Abdullah A. Mamun, M. Stutzman, R. Suleiman, S. Zhang
Students: Wei Liu, Gabriel Palacios, Sajini Wijethunga, Josh Yoskowitz, Yan Wang

## Slide 17
2017
C. Sinclair, T. Gay, J. Grames, M.J. McHugh, D. Moser, A.K. Opper, M. Poelker, X. Roca-Maza, R. Suleiman, and M. Stutzman, “The CEBAF 5 MeV Mott Polarimeter”, analysis complete, in press
Marcy L. Stutzman, Philip A. Adderley, M.A. Mamun, Matt Poelker, “NEG coated chambers to achieve 1x10-12 Torr”, to be submitted J. Vac. Sci. Technol. A
M.A. Mamun, M. D. Hernandez-Flores, E. Morales, C. Hernandez-Garcia, and M. Poelker, “Temperature Dependence of Alkali-Antimonide Photocathodes: Evaluation at Cryogenic Temperatures”, submitted for publication Phys. Rev. Accel. and Beams
Wei Liu, Shukui Zhang, Marcy Stutzman, and Matt Poelker, “A Comprehensive Evaluation of Factors that Influence the Spin Polarization of Electrons Emitted from Bulk GaAs Photocathodes”, J. Appl. Phys., 122, 035703 (2017)
C. Hernandez-Garcia, D. Bullard, F. Hannon, Y. Wang and M. Poelker, “High voltage performance of a dc photoemission electron gun with centrifugal barrel-polished electrodes”, accepted for publication Rev. Sci. Instrum.
Yoshitaka Taira, Shukui Zhang, "Split in phase singularities of an optical vortex by off-axis diffraction through a simple circular aperture", Opt. Lett. 42, 1373 (2017)
2016
Wei Liu, Yiqiao Chen, Wentao Lu, Aaron Moy, Matt Poelker, Marcy Stutzman, and Shukui Zhang, "Record-level quantum efficiency from a high polarization strained GaAs/GaAsP superlattice photocathode with distributed Bragg reflector", Appl. Phys. Lett. 109, 252104 (2016)
Wei Liu, Shukui Zhang, Marcy Stutzman, and Matt Poelker, "Effects of ion bombardment on bulk GaAs photocathodes with different surface-cleave planes", Phys. Rev. Accel. Beams 19, 103402 (2016)
J. Grames et al., "Production of Highly Polarized Positrons Using Polarized Electrons at MeV Energies", Phys. Rev. Lett., 116, 214801 (2016)
B. Roberts, F. Hannon, M. M. Ali, E. Forman, J. Grames, R. Kazimi, W. Moore, M. Pablo, M. Poelker, A. Sanchez, and D. Speirs, "Harmonically resonant cavity as a bunch-length monitor", Phys. Rev. Accel. Beams 19, 052801 (2016)
C. Hernandez-Garcia, M. Poelker, and J. Hansknecht, "High Voltage Studies of Inverted-geometry Ceramic Insulators for a 350kV dc Polarized Electron Gun", IEEE Transactions on Dielectrics and Electrical Insulation, Vol. 23, No. 1; February 2016
Md Abdullah A. Mamun, Abdelmageed A. Elmustafa, Carlos Hernandez-Garcia, Russell Mammei, and Matthew Poelker, "Effect of Sb thickness on the performance of bialkali-antimonide photocathodes", J. Vac. Sci. Technol. A 34 021509 (2016)
Publications