## Slide 1: CEBAF Source/Injector Update PREX/CREX Collaboration Meeting October 2, 2017
Joe Grames
Center for Injectors and Sources

## Slide 2: Outline
Polarized Source
  Recent performance
  Preparing for simultaneous 4-Hall operation
  High polarization photocathode studies
Injector Upgrade
  Status of the 200 keV upgrade
  Plans for next SAD
Some “Plan B” Options to Consider

## Slide 3
CEBAF Polarized Inverted Load Lock Gun (Spring 2017)
CEBAF Injector Gun2 @ 130 keV

## Slide 4
4
Polarized Source Operation
Photocathode
  Strained Superlattice GaAs/GaAsP #5756-4
  Good Polarization 85-87% (measured at Mott)
  Good QE > 1% after activation
Last Spring 2017
  Delivered 20-40 uA to 3 halls at a time (249.5 & 499 MHz)
  Hall A (Physics), Hall B (KPP), Hall C (KPP), Hall D (Physics)
This Fall 2017 – Winter 2018
  CEBAF restoration starts late November
  12 weeks of running scheduled
  Start simultaneous 4-Hall Operation

## Slide 5
Condition | (D+2) | (D+3)
Maximum number of halls receiving beam | 3 halls | 4 halls
ABC Beam @ 5th pass (Hall D on) | 499 MHz | 249.5 MHz
ABC Beam @ 5th pass (Hall D off) | 499 MHz | 499 MHz
ABC Beam @ lower passes | 499 MHz | 499 MHz
  Simultaneous CEBAF 4-Hall Operations
4 Hall Delivery Conditions (called D+3)
4 Hall Setup Considerations
  Two 249.5 MHz beams share a 499 MHz “Chopper Bucket”
  750 MHz separators used for the 5th pass ABC + D separation
  Pairs of lasers have opposite helicity (A/B opposite of C/D)

## Slide 6
4-Hall Source Laser System – Spring 2016

## Slide 7
Summer 2017 Shutdown
  Replaced damaged or aging RTP cells, exhibiting poor extinction or optical after-pulse. We backed out of applying DC high voltage to RTP crystals, which DO suffer ion migration from electrode.
  Improved independent management of laser size/divergence
    Added stages to readily vary laser size
    Modified lens for PPLN doubling and improved performance
    Added splitters/targets to improve combining lasers
  Completed installation of production LLRF (replaced proto-type)
  Identified a vendor in China providing less costly bare RTP crystal
4-Hall Source Laser System Update

## Slide 8: Improving Lifetime with Larger Laser Size
J. Grames, et al, Phys. Rev. ST Accel. Beams 14 043501 (2011)
GaAs @ 532nm

## Slide 9: Improving charge lifetime with GaAs/GaAsP
Indeed, we enhanced the Charge Lifetime for Qweak by a factor of four when doubling the laser spot size from 0.5mm to 1.0 mm (diameter)

## Slide 10: Lifetime Studies at mA Beam Current
Polarized positrons for CEBAF, and on-going discussions with BNL related to high current eRHIC EIC, prompted experiments at CEBAF to characterize lifetime vs. laser spot size using high-polarization photocathodes
CEBAF 130kV polarized “inverted gun” with load lock
Make beam here
Deliver it here
Vary the laser beam size
Monitor vacuum and radiation
1mA
Required laser power, slope proportional to QE decay
Increasing laser size reduces QE decay proportionally
Note:
1 mA 86 C/day
5 mA 432 C/day
10 mA 860 C/day
50 mA 4320 C/day

## Slide 11: First Results: GaAs/GaAsP at mA Current
  CEBAF charge lifetime improves with spot size, as expected, but eventually beam size becomes “too large”
  Laser diameters greater than ~4 mm (4 sigma) will require properly designed cathode/anode electrodes, to ensure 100% transmission, to maintain excellent vacuum, to minimize ion bombardment
We operate left of this line
Although PREX/CREX doesn’t need milliAmp’s, by performing these studies we aim to improve Lifetime and QE Uniformity

## Slide 12: Polarization Studies at mA Beam Current
First measurement of polarization from superlattice photocathode at milliampere current
CEBAF 5 MeV Mott polarimeter: on-going effort to ascribe sub-percent accuracy (collaborators D. Moser, X. Roca-Maza, Charles Sinclair, M.J. McHugh, and Tim Gay)
CEBAF 5 MeV Mott Polarimeter
Chart: Polarization (%)
| 1.67 | 10.4 | 50.5 | 100.5 | 250.5 | 504.0 | 755.0 | 1011.0 | 1.06
 | 85.6704 | 84.5218 | 84.3896 | 85.3479 | 84.9536 | 86.116 | 84.7714 | 85.9647 | 87.1486

## Slide 13: High Polarization Photocathodes
30 mA/W
Bulk GaAs
1 mA/W
100 nm
Strained GaAs
Strained Superlattice GaAs/GaAsP
6 mA/W
100 nm
14 Layers
Photocathode capability (polarization and QE) has grown significantly.
Pe- 35% 35% 75% 75% 85% 89%
Ie- 30mA 100mA 50mA 100mA 150mA 200mA
1995 1998 1999 2000 2004 2017
with DBR
30 mA/W
Testing at
CEBAF now

## Slide 14: Benefits of Distributed Bragg Reflector
Enhanced absorption occurs only at specific laser wavelengths
non-DBR Photocathode : absorption in the GaAs/GaAsP superlattice < 5%
DBR photocathode : absorption in the GaAs/GaAsP superlattice > 20%
Non-DBR photocathode
DBR photocathode

## Slide 15: World Record QE from High Polarization Photocathode
Others have tried…but very difficult to obtain QE enhancement at the laser wavelength that also provides high polarization, CEBAF lasers operate at ~ 776 nm (doubled-telecom lasers)
Standard strained-superlattice
  QE = 0.89%
  Polarization = 92%
DBR
  QE = 6.4%
  Polarization = 84%
The highest reported QE of any high polarization photocathode
Excellent candidate for mA operations, will test at CEBAF this shutdown
SBIR partnership
W. Liu, S. Zhang, M. Stutzman, M. Poelker, Y. Chen, W. Lu, and A. Moy, Appl. Phys. Lett. 109, 252104 (2016)

## Slide 16
Injector Upgrade (what remains after R100)
Increase gun voltage and Wien filters for 200kV operation
Improve baked beam line vacuum so gun does not pump on beam line
Locate Wien filters (energy filter) upstream of pre-buncher cavity
New SRF booster eliminates warm capture, RF deflection and x/y coupling
Our new “1/4 cryomodule”:
2 cell capture section + 7 cell cavity,
should provide 10 MeV beam and introduce no x/y coupling, allow better matching, more adiabatic damping
200 kV

## Slide 17
1. Build and install a HV chamber that can produce 200keV beam to explore operation.
2. Replace “NEG tube” with one that also includes two BPM’s.
3. Remove Gun3.
Reminder: Our summer 2017 “early start” goal

## Slide 18
Modified M20
New NEG tube w/ two BPM’s
We will take advantage of replacing the gun high voltage chamber to replace the NEG coated beam pipe with one that has two BPM’s
BPM’s will have S/H cards for parity DAQ
With solenoid off measure position/angle
Test resolution to measure 2nd moment

## Slide 19
Modify spare CEBAF/ILC gun for reliable 200 kV operation
  One must is very high vacuum ~1E-12 Torr
  Another is no field emission; a “shed” protects the ceramic-vacuum-metal triple point, mitigates unwanted field emission
200 kV Gun
Work of G. Palacios, C.H. Garcia

## Slide 20: Hand-Polishing Nightmare!
New CEBAF 200 kV Gun
Work of G. Palacios, C.H. Garcia

## Slide 21: Centrifugal Barrel Polishing to Rescue
Reduced polishing time from Months to hours !!!
  From machine shop
30 min. plastic cones
30 min. crushed corncob
C. Hernandez-Garcia, D. Bullard, F. Hannon, Y. Wang, and M. Poelker, “High voltage performance of a dc photoemission electron gun with centrifugal barrel-polished electrodes,” accepted Rev. Sci. Instrum, 22 August 2017
  Barrel polishing machine at JLab SRF

## Slide 22
Gun assembled and baked successfully.
HV conditioned at the UITF using available with 225kV HVPS (Spellman) and SF6
Small, yet measurable on-set of field emission above 200kV – requires conditioning > 225kV to process
Conditioning the 200 kV gun at UITF (June 2017)
Chart: Ch. 2 (Top) Radiation vs. Voltage
| 210.0 | 200.0 | 180.0 | 150.0 | 130.0
23-Jun | 0.58934 | 0.2597 | 0.14107 | 0.12581 | 0.15827
30-Jun | 0.82728 | 0.27563 | 0.15534 | 0.14838 | 0.1289

## Slide 23
Steps moving forward…
Spellman HVPS supply inadequate for CEBAF operations
  Require higher voltage > 225 kV to process field emission
  PR’s for Glassman 350kV/4.5mA HVPS and SF6 tank submitted
  System identical to UITF (spare)
Fall/Winter
  Process 200kV gun w/ UITF spare
  Build 350kV HVPS for CEBAF
  Re-design of beam line started already
Spring 2018 SAD Goals
  350kV HVPS + 200kV Gun + NEG tube
  Commission 200 keV beam operation
  Time/$ permitting, rebuild the beam line

## Slide 24
200 kV Wien filter
Upgrade the actual 130 keV Wien filters for 200 keV operation
Barrel polished electrodes and successfully tested to 20kV
Replace 14 kV supplies with 30 kV power supplies
Replace 10 A coils with 20 A coils (J. Benesch, JLAB-TN-15-032)
First upgrade prototype to be tested at the UITF this Fall
Wien Upgrade for 100 deg precession |  | 
Beam Voltage | keV | 200.00
Integrated BL | G-cm | 3993.86
Magnet Current | A | 15.36
Electric Field | MV/m | 2.67
Electrode High Voltage | kV | 20.05

## Slide 25
Testing CEBAF Upgrade Cryounit at UITF
Upgrade Cryounit Commissioning at Test Lab
  Spring 2017 – cryostat positioned at UITF
  Summer 2017 – keV vacuum beam line connected
  Winter 2018 – application of klystron power

## Slide 26
A. Freyberg Aug 2016 ECT’16 =>
PREX/CREX
timescale
Not likely if we test at UITF first

## Slide 27
Summary - Running PREX/CREX
The >130keV Gun
We plan to install a gun capable of 200 keV operation by Fall 2018
Until remaining beamline fully upgrade (chopper/cryounit) we may still find a higher voltage operating point that benefits gun operation
Parity Quality Beam
Laser table setup for QWeak successfully meet the PREX/CREX requirements
Large laser size of about 1 mm consistent KD*P benefit photocathode lifetime
Helicity magnets downstream of all apertures are ready for position feedback
SRF Operation at 4K
We have demonstrated capability to operate C20/C50 5-cell modules at 4K
At the injector produced indistinguishable beam up to about 15 MeV
Tested the NL @ 4K to 130 MeV suggesting 1 GeV; maybe 2 GeV possible?
Propose to invite Grigory Eremeev to give a talk to PREX/CREX.