## Slide 1
DOE-NP Accelerator R&D
PI Meeting
P. Adderley, D. Bullard, J. Grames, J. Hansknecht,
C. Hernandez-Garcia, Md. Abdullah Mamun, M. Poelker,
M. Stutzman, R. Suleiman, S. Zhang
Students: W. Liu, Y. Wang
DOE Headquarters, Germantown 11/14/2016
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 2: Recently Funded Projects
500kV DC High Voltage Inverted Gun with Load-locked CsK2Sb Deposition Chamber - Research and Development for Next Generation Nuclear Physics Accelerator Facilities (LAB 12-632) and (LAB 14-1082)
New Photocathode Materials for Electron Ion Colliders - Research and Development for Next Generation Nuclear Physics Accelerator Facilities (LAB 12-632) and (LAB 14-1082)
Cryo-Pumped DC High Voltage Polarized Electron Source - Small Project, DOE Office of Nuclear Physics, (LAB 10-339)
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 3: Recently Funded Projects
500kV DC High Voltage Inverted Gun with Load-locked CsK2Sb Deposition Chamber - Research and Development for Next Generation Nuclear Physics Accelerator Facilities (LAB 12-632) and (LAB 14-1082)
New Photocathode Materials for Electron Ion Colliders - Research and Development for Next Generation Nuclear Physics Accelerator Facilities (LAB 12-632) and (LAB 14-1082)
Cryo-Pumped DC High Voltage Polarized Electron Source - Small Project, DOE Office of Nuclear Physics, (LAB 10-339)
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 4: Recently Funded Projects
To improve photogun vacuum and thereby improve lifetime of polarized electron sources, particularly at mA current, i.e., eRHIC
To extend the “inverted gun” geometry design, to operate at higher voltage, for high bunch charge and high average current EIC cooling applications
To design a photocathode test stand to measure QE and polarization of new photocathode materials that might help EIC
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 5: The CEBAF - ILC Inverted Gun
Load-locked GaAs polarized photogun
130 kV at CEBAF, 200 kV at Injector Test Stand
Gun Vacuum ~ low 10-12 Torr
New design
NEG pumps
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 6: 500 kV Photogun?
Longer “R30” insulator
Spherical electrode
CEBAF 130 kV Inverted Gun
“R28” insulator
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 7: Building the 500 kV Gun
Start with “dummy” electrodes and test different insulators and cathode screening electrode
Notes: Interior Page Design 2

## Slide 8: Insulators and Screening electrode
Longer R30 insulators, conventional alumina
Short R28 insulator, bulk resistivity, mildly conductive
Longer R30 insulator, bulk resistivity, mildly conductive
ZrO-coated R30 insulator, also mildly conductive
dummy electrode with a screening electrode (shed)
Notes: Interior Page Design 2

## Slide 9: Breakdown at Cable/Insulator Interface
Problems at the cable junction, atmosphere side
Note: Field emission was managed via krypton-processing. i.e., voltage first applied with ~10-5 Torr krypton added to gun chamber
Notes: Interior Page Design 2

## Slide 10: Summary of Tests
Two and 1/2 configurations reached our voltage goal
Notes: Interior Page Design 2

## Slide 11: Linear Potential Drop
Want a linear potential gradient along length of the insulator
Note - POISSON does not accurately model the mildly-conductive feature of the black insulator
Notes: Interior Page Design 2

## Slide 12
Matt Poelker, Jefferson Lab
Combine the two features that provided incremental success: screening electrode and doped black R30 insulator
Replaced dummy ball with electrode that can hold photocathode
Notes: Interior Page Design 2

## Slide 13: The gap between shed and insulator
Keep field strength low at triple point (metal, insulator, vacuum)
reduce
9.5 MV/m
10 MV/m
10.8 MV/m
7 MV/m
7 MV/m
8 MV/m
Gap = 1 mm
8 MV/m
9.5 MV/m

## Slide 14: CsK2Sb deposition Chamber
Effusion source, compact, high capacity
Contains both Cs and K species, co-deposition
Photocathodes grown on stalks
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 15: Distinguishing QE Drop due to Contamination
Systematic decrease in QE at RT in repeated cooling events
Considerable increase in water partial pressure during brief heating was observed
Rejuvenation of QE by brief heating at 170-200 C was consistently observed in the non-baked system which can be considered as a signature of water adsorption
Chart: QE (non-baked chamber)
| RT1 | LN1 | RT2-a post LN1 | LN2 | RT3 post LN2 | RT4 post heating | LN3 | RT5 post LN3 | RT6 post heating | LN4 | RT7 post LN4 | RT8 post heating
QE (non-baked) | 4.632 | 1.5459 | 2.2506 | 0.54704 | 0.5631 | 5.3338 | 1.2882 | 1.524 | 5.1207 | 1.1687 | 1.5968 | 4.6115
QE Recovery
QE Recovery
QE Recovery
RT
LN2
RT (Post Heating)
Brief heating 170 - 200 °C,
H2O 34%
Brief heating 170 - 200 °C,
H2O 26%
Brief heating 170 - 200 °C,
H2O 37%
  Pre-bake vacuum ~10-8 Pa
Work of M.A. Mamun
Notes: Interior Page Design 2

## Slide 16
Chart: QE (baked chamber)
| RT (1) | 77 K (1) | RT (2) post 77 K (1) | 77 K (2) | RT (3) post 77 K (2) | 77 K (3) | RT (5) post 77 K (3) | 77 K (4) | RT (7)
QE (Baked) | 6.7821 | 6.2039 | 9.8276 | 6.4974 | 11.27 | 7.45 | 12.89 | 7.29 | 11.05
Reproducible QE - Cryocooled Photocathode
The QE at RT did not show any decrease between repeated cooling events
QE at Liquid N2 temperature (77 K) showed similar QE every time it was cooled
Initial QE rise due to stoichiometric optimization
We did our spectral response and temperature analysis from this phocathode.
RT
LN2
RT (Post Heating)
Work of M.A. Mamun
  baked vacuum ~10-9 Pa
Notes: Interior Page Design 2

## Slide 17: Depo Chamber at Gun Test Stand
Always something to fix: Valve between gun and depo chamber leaked, working distance between puck and chemical sources too large, no mask to limit active area
Notes: Interior Page Design 2

## Slide 18: 300 kV Inverted Gun and CsK2Sb Photocathode
8 MV/m
11 MV/m
First insulator conditioned to 325 kV
New insulator, installed now, supports higher voltage operation
1mA
Learning how to use the new photocathode
Need mask and precipitator
Notes: Interior Page Design 2

## Slide 19: 500 kV Gun
Notes: Interior Page Design 2

## Slide 20: 500 kV Gun
Notes: Interior Page Design 2

## Slide 21: Barrel-Polished Electrodes
Gun electrodes traditionally polished using sand paper and diamond paste
Tedious process, takes about 30 days to complete
Now performed in 1 day using SRF barrel polishing machine
  From machine shop
30 minutes with plastic cones
30 minutes with corncob
Work by Don Bullard
Notes: Interior Page Design 2

## Slide 22: Magnetized Beam Tests
Fixed the gun and deposition chamber, added solenoid
Notes: Interior Page Design 2

## Slide 23: 350 kV Gun at Injector Test Facility
Old and New inverted guns
Vacuum low 10-12 Torr
Working on the beamline now
450 kV 3mA supply
Notes: Interior Page Design 2

## Slide 24: kV beamline at Injector Test Facility
Dif pump
200 kV Wien
RF deflector cavities
Buncher
2.5 kW dump
Notes: Interior Page Design 2

## Slide 25
Matt Poelker, Jefferson Lab
Screening electrode
Doped insulator
SF6
R350 epoxy receptacle
Our plan to reach 500 kV
Combination of long doped insulator and shed, SF6 and epoxy receptacle
And likely a different vacuum chamber
Plan Z
Work of Yan Wang
Notes: Interior Page Design 2

## Slide 26
Matt Poelker, Jefferson Lab
Screening electrode
Doped insulator
SF6
R350 epoxy receptacle
We have the big insulators
Cables in Receptacles: very reliable
Receptacles in SF6: very reliable
Use cold SF6 to remove heat from photocathode
Plan Z
Notes: Interior Page Design 2

## Slide 27: Thank You
Will continue to work on 500 kV inverted gun, CsK2Sb deposition chamber (and Cryopumped gun)
Magnetized beam tests
We can revisit high current (mA) lifetime tests with polarized beam but need support
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2