## Slide 1: High Power Solid Target for Positron Source at CEBAF
e+ Production by Polarized e‒ Beam
Radiation Damage and Heat Load in Target
Design of High Power Target
Target Material Tests with e‒ Beam and Laser
A. Ushakov1,2, S. Covrig1, J. Grames1, S. Habet1,2, C. Le Galliard2, E. Voutier2
This work is supported by the European Union’s Horizon 2020 Research and Innovation program under Grant Agreement No 824093 and the U.S. DOE, Office of Science, Office of Nuclear Physics, contract DE-AC05-06OR23177.
1 Thomas Jefferson National Accelerator Facility, Newport News, VA,USA
2 Université Paris-Saclay, CNRS/IN2P3/IJCLab, Orsay, France

## Slide 2: Polarization Transfer from e‒ to e+ in a Single High-Z Target
PEPPo (Polarized Electrons for Polarized Positrons) experiment demonstrated the feasibility of using bremsstrahlung of MeV Polarized Electrons for production of Positrons with a high level of polarization.
(PEPPo Collaboration) D. Abbott et al. Phys. Rev. Lett. 116 (2016) 214801
1 μA @ 8.2 MeV e‒, 1 mm W target
e+ Polarization vs Energy

## Slide 3: Optimal Target Thickness and e+ Yield
Δpe+/pe+ = ±0.05
Tungsten
Yield vs Target Thickness
Power Deposition in Target (17 kW)
High-Current e‒ Beam (1 mA)
For e+ source at polarized mode and 120 MeV e‒ beam (at maximal Figure-of-Merit FoM = ):
Optimal Thickness of W Target = 4 mm
e+ Yield 10-3

## Slide 4: LERF Polarized Positron Injector Concept
Development of polarized e+ injector at LERF – J. Grames et al., IPAC’23, MOPL152
  High current polarized e− source (10 MeV/10 mA) – C. Hernandez-Garcia, LCWS2023; R. Kazimi et al., IPAC’23, WEPA035
  High current 1-3 mA e− LINAC (two C75 CM)
  Positron conversion target (~100 kW) – A. Ushakov et al., LCWS2023; IPAC’23, WEPM120
  Capture of e+ beam and momentum selection
  e+ bunch compression and acceleration to 123 MeV
  CEBAF acceptance studies – A. Sy et al., IPAC’23, MOPM081
S. Habet et al., LCWS2023

## Slide 5: Concept and Challenges of High-Power Target
Static target would melt in 64 ms
1 mA @ 120 MeV cw e‒ beam
σbeam = 1.5 mm
Temperature in Stationary Target
Some parameters of currently considered model of e+ target:
Beam passes through the target at R of 18 cm
2.3 m/s target tangential speed at R of 18 cm
Ø16 mm water channel inside Cu disk
1.5 m/s speed of water flow
Target Challenges:
Radiation damage → rotate
High (average) heat → cool and rotate
Material fatigue cause by cycling temperature → study material properties under realistic conditions
Target Concept

## Slide 6: Radiation Damage of 17 kW Tungsten Target
Radiation Damage of Stationary Target
Annual Max Rad. Damage of Rotated Target
0.21 dpa
Ø36 cm W Target
1 mA @ 120 MeV e‒
1.5 mm rms spot size σ
Radiation Damage of Rotated Target
Max Rad. Damage of Stationary Target
5.7E-22 dpa/e‒
120 MeV e‒
1.5 mm rms spot size
Tests of target thermal and mechanical properties at such level of rad. damage are planned

## Slide 7: Energy Deposition and Heat Power Density in 17 kW Target
120 MeV e‒
1.5 mm RMS spot size
Energy Deposition in W Target
Max Edep = 0.321 GeV/(e‒ cm3)
Heat Power Density
Pmax = 321 W/mm3
For 1 mA e‒ beam:

## Slide 8: Temperature in Rotated Tungsten Target
1 mA @ 120 MeV e‒ Beam
1.5 mm rms spot size
2.3 m/s
ΔTmax = 188 °C
Tmax = 681 °C
Temperature vs Time
Temperature Distribution for Beam Moving with 2.3 m/s
PEDD = 28.2 J/g
2 Hz target revolution frequency

## Slide 9: Equivalent von-Mises Stress in Rotated 17 kW Target
Equivalent von-Mises Stress
Tests of target fatigue are desired
Tmax = 681 °C in Tungsten
σvM max = 878 MPa
Distribution of Temperature

## Slide 10: Test of Target Materials with e‒ Beam at Mainz Microtron (MAMI)
Investigate changes/degradation of target material after 106-107 thermal cycles. Test fatigue of target materials: W, Ta, W-alloys (JLab target) and Ti-alloys (ILC target) at different temperatures
Study impact of radiation damage on target material properties between 0.1 and 0.5 dpa at expected elevated temperatures
Beam energy: 3.5 MeV
Pulsed current: I 50 μA
Pulse length tp 0.3 ms
Beam rms size on target: σ 250 μm
MAMI e‒ Beam:
DESY: S. Riemann
Helmholtz-Zentrum hereon: T. Lengler, D. Lott
IJCLab: S. Habet, C. Le Galliard, E.Voutier
Jefferson Lab: J. Grames, A. Ushakov
University of Hamburg: M. Formela, G. Moortgat-Pick
Johannes Gutenberg University Mainz: K. Aulenbacher, T. Beiser, M. Dehn

## Slide 11: Radiation Damage of Tungsten by 3.5 MeV e‒ Beam with 50 µm Spot Size
Max Rad. Damage = 1.02E-19 dpa/e‒
Material | Displacement Threshold Energy [eV]
W | 90
Ta | 90
Re | 60
Cu | 30
50 μA → 3.125E+14 e‒/s
For e‒ beam with duty cycle of 22%
(1.1 ms pulse length, 5 ms pulse period)
to reach the damage of 0.21 dpa
9h of irradiation is needed

## Slide 12: Tested Targets and Measured Temperatures (March 31 – April 5, 2023)
# | Material | Target Size [mm] | Thermo-couples | Pulse Length [ms] | Pulse Period [ms] | Tave [°C] | Irrad. Time [h]
1a | Ti Grade5 | 0.5x14x42 | Yes | 1.0 | 10. | 108 | 8.5
1b | Ti Grade5 | 0.5x14x42 | Yes | 0.5 | 7.1 | 98 | 5.5
2 | W | 0.1x3x42 | No | 0.4 | 3.7 | - | 6.0
3 | W | 0.1x10x42 | Yes | 1.1 | 5.0 | 197 | 9.1
4 | Ta | 0.1x3x42 | No | 0.4 | 3.7 | - | 5.5
5 | Ti Grade5 | 0.75x14x42 | Yes | 0.5 | 10. | 131 | 21.2
 |  |  |  |  |  |  | Ʃ 55.8
# | Material | Target Size [mm] | Thermo-couples | Pulse Length [ms] | Pulse Period [ms] | Tave [°C] | Irrad. Time [h]
1b | Ti ELI | 0.5x10x42 | Yes | 1.0 | 10. | 421 | 0.7
1a | Ti ELI | 0.5x10x42 | Yes | 1.0 | 10. | 782 | 3.8
1c | Ti ELI | 0.5x10x42 | Yes | 1.1 | 5.0 | 223 | 3.7
2 | Ta | 0.1x10x42 | No | 1.1 | 5.0 | - | 10.6
3 | Ta | 0.1x10x42 | Yes | 0.75 | 10. | 850 | 8.0
4 | W | 0.1x10x42 | Yes | 0.75 | 10. | x | 8.0
5a | Ti ELI | 0.75x10x42 | No | 1.0 | 10. | - | 8.5
5b | ELI alloy | 0.75x10x42 | No | 0.5 | 7.1 | - | 6.0
 |  |  |  |  |  |  | Ʃ 48.3
1st 5 Targets
2nd 5 Targets
Thermal/electric isolation: Aluminum Oxide with 1.6 mm thickness
Beam size was estimated by T. Beiser
(based on photos of beam on OTR screen):
2σx 527 µm,
2σy 585 µm

## Slide 13: Targets after Irradiation
1st 5 Targets
2nd 5 Targets

## Slide 14: Target 1a: Temperature in 0.5 mm Ti Grade5 (1 ms Pulse Lengh, 10 ms Period)
200 µm rms beam spot size
50 µm rms beam spot size
Measured T = 108°C
Tmax = 325°C
Tmax = 392°C

## Slide 15: Target 5: Temperature in 0.75 mm Ti Grade5 (0.5 ms Pulse Lengh, 10 ms Period)
200 µm rms beam spot size
50 µm rms beam spot size
Measured T = 131°C
Tmax = 209°C
Tmax = 253°C

## Slide 16: Target 3: Temperature in W (1.1 ms Pulse Lengh, 5.0 ms Period)
200 µm rms beam spot size
50 µm rms beam spot size
Measured T = 197°C
Tmax = 379°C
Tmax = 428°C

## Slide 17: Target 2: Temperature in W (0.4 ms Pulse Lengh, 3.7 ms Period)
200 µm rms beam spot size
50 µm rms beam spot size
Tmax = 235°C
Tmax = 257°C

## Slide 18: Target 4: Temperature in Ta (0.4 ms Pulse Lengh, 3.7 ms Period)
200 µm rms beam spot size
50 µm rms beam spot size
Tmax = 472°C
Tmax = 516°C
Calculations of cycling temperature and analysis of 2nd 5 targets are ongoing

## Slide 19: Test of Target Materials with Laser at JLab LERF Laser Lab 6
Existing laser setup will be used for testing e+ target materials
10 W lasers (532 nm) were used for testing 18 µm W foils to their limits and beyond [S. Gopinath, S. Covrig “APEX Target Thermal Assessment”, PMAG0000-0001-A0001, 10/29/2020]:
Experimental Setup
CAD assembly
S. Gopinath
SEM Images of APEX Target with Micro-Fractures at Beam Spot

## Slide 20: Test of Target Materials with Laser at JLab LERF Laser Lab 6
Experimental setup at LERF Laser Lab 6 would allow us to test the high peak heat loads and fatigue of target materials in a wide temperature range
Test of thermal contact conductance between high-Z materials and Cu or Al (Ce+BAF and ILC targets)
Possibility of testing low-power stationary target is being studied
Cooling Tube
Design of Low-Power Target (S. Covrig). Beam View
Cu Frame
Targets (25x25 mm2)
Cu Washer
Beam Clearance: 16x8 mm2
Side View
e‒ Beam
W
e‒ Beam

## Slide 21: Summary and Outlook
We are focused on the development of 123 MeV e+ injector at LERF
Development and test of e+ targets:
  JLab Phase I: Prototype/proof-of-principle of low-power stationary solid water-cooled target (< 1 kW)
  JLab Phase II: High-power rotated solid water-cooled target (17 ‒ 20 kW)
Target material tests:
  Test of target materials with pulsed 3.5 MeV e+ beam at MAMI was performed on Mar 31 – Apr 5, 2023 (W, Ta, Ti-alloys)
  ANSYS calculations of temperature for targets tested at MAMI are ongoing
  Study of irradiated targets with PETRA X-rays at DESY will be done soon
  Fatigue target tests with a laser at JLab LERF Laser Lab 6 are planned in 2023
  Two proposals this year related to target tests:
    SLAC/KEK/JLAB on target fatigue laser studies (US-Japan Collaboration)
    JLab LDRD (Laboratory Directed Research & Development) on e‒ beam irradiation studies
We are open to collaboration on all aspects of the JLab e+ injector design, especially in the case where we can be a test bed.