## Slide 1
350 kV Photoelectron Gun with Inverted-Insulator Geometry
P. Adderley, D. Bullard, E. Forman, J. Grames, J. Hansknecht,
C. Hernandez-Garcia, M. Poelker, M. Stutzman,
R. Suleiman, S. Zhang
Students: M. BastaniNejad, Md. Abdullah A. Mamun, Y. Wang
Polarized Sources, Targets and Polarimeters Workshop, Bochum Germany, Sept. 14-18, 2015
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 2: Things we’ve been Studying
Neutron
Proton
Electron
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 3: A New Photogun for New Initiatives
Compact 10 MeV accelerator to commission new hardware destined for CEBAF
  HDIce
  New SRF capture section for injector
  Test bed to improve beam quality for demanding parity-violation experiments
Load-locked gun for JLab’s FEL/ERL for DarkLight and other experiments
  DC high voltage gun, but with CsK2Sb photocathode
Electron Ion Collider (MEIC, eRHIC, LHeC)
  High average current polarized beams and very high current un-polarized beams for cooling proton beams
  Magnetized beam
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 4: 10 MeV beam to commission HDIce
350kV inverted gun + chopper + buncher + “traditional” JLab ¼ cryomodule

## Slide 5
Preparing for the next generation Parity-Violation Experiment
deliver 100% long polarization to two halls simultaneously - each gun/beamline has spin manipulators
parity violation experiments can monitor helicity correlated beam properties directly from gun. No other superimposed beams from gun to merger point
apertures at injector are good for non-parity users, they keep them. Apertures are bad for parity Users, the new line could eliminate them, hopefully even the chopper
Parity violation experiments get a laser "clean-up polarizer" to provide near perfect circular polarization, which helps reduce helicity correlated beam asymmetries
Proposed by Joe Grames

## Slide 6: ERL Circulator Cooler Concept
ion bunch
electron bunch
circulator ring
Cooling section
solenoid
Fast kicker
Fast kicker
SRF Linac
dump
injector
recirculating 10+ turns  reduction of current from an ERL by a same factor
Design Choices
Energy Recovery Linac (ERL)
Compact circulator ring to meet design challenges
Large RF power, up to 81 MW
Very high electron beam current: 1.5 A
Required technologies
High current ERL (55 MeV, 15 to150 mA)
Magnetized beam
High bunch charge (2 nC)
Ultra fast kicker
energy recovery
Proposed by S. Derbenev
injector
dump
cooling solenoids
rechirper
dechirper
recompression
CCR
ERL
beam exchange system
SRF
decompression
D. Douglas C. Tennant
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 7
Text goes here
Always Tweaking the Design
Endless (?) quest for perfection
1
2
3
4
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 1

## Slide 8: The CEBAF - ILC 200kV Inverted Gun
Our “Load-locked” GaAs photogun:
Gun Vacuum ~ mid to low 10-12 Torr
Beamline vacuum could be improved…
New design
NEG pumps
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 9: Benefits of Higher Gun Voltage
Reduce space-charge-induced emittance growth, maintain small transverse beam profile and short bunch-length. In other words, make a “stiff” beam right from the gun
Reduce problems associated with Surface Charge Limit (i.e., QE reduction at high laser power)
Prolong Charge Lifetime (?)
Compact, less-complicated and less-expensive injector
Biggest Obstacle: Field Emission and HV Breakdown… which lead to bad vacuum and photocathode death
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 10: Field Emission
Sources of Field Emission: micro-protrusions, contamination on surface, material defects and impurities, ionization of desorbed gas, etc.,
Material choices: hardness, work function, grain structures and grain boundaries, electrical conductivity, thermal conductivity
Surfaces: generally people assume smooth is better than coarse, although experiments indicate smooth does not guarantee “good”
Mostly, people assume 5 MV/m is “easy” - we want to operate at 10 MV/m or higher
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 11: Breakdown in Vacuum
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 12: 350 kV Photogun
Longer “R30” insulator
Spherical electrode
Thin NEG sheet - move ground plane further away
CEBAF 200kV Inverted Gun
“R28” insulator
Maximum Field strength ~ 10 MV/m
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 13: Building the 350 kV Gun
Start with “dummy” electrodes and test different insulators and cathode screening electrode
Notes: Interior Page Design 2

## Slide 14: Insulators and Screening electrode
Longer R30 insulators, conventional alumina
Short R28 insulator, bulk resistivity, mildly conductive
Longer R30 insulator, bulk resistivity, mildly conductive
ZrO-coated R30 insulator, also mildly conductive
dummy electrode with a screening electrode (shed)
Notes: Interior Page Design 2

## Slide 15: Breakdown at Cable/Insulator Interface
Problems at the cable junction, atmosphere side
Note: Field emission was managed via krypton-processing. i.e., voltage first applied with ~10-5 Torr krypton added to gun chamber
Notes: Interior Page Design 2

## Slide 16: Summary of Tests
Two and 1/2 configurations reached our voltage goal
Notes: Interior Page Design 2

## Slide 17: Linear Potential Drop
Want a linear potential gradient along length of the insulator
Note - POISSON does not accurately model the mildly-conductive feature of the black insulator
Notes: Interior Page Design 2

## Slide 18
Plan Y: Combine the two features that provided incremental success: screening electrode and doped black R30 insulator
Replace dummy ball with electrode that can hold photocathode

## Slide 19: The gap between shed and insulator
Keep field strength low at triple point (metal, insulator, vacuum)
reduce
9.5 MV/m
10 MV/m
10.8 MV/m
7 MV/m
7 MV/m
8 MV/m
Gap = 1 mm
8 MV/m
9.5 MV/m

## Slide 20
Screening electrode
Doped insulator
SF6
R350 epoxy receptacle
Combination of doped insulator and shed, SF6 and epoxy receptacle, plus added length
the screening electrode, a good design…
Plan Z
Work of Yan Wang

## Slide 21: Field Emission: Things we’ve been Studying
Fowler-Nordheim Theory: a good place to start, but it will disappoint …
Diamond-paste polished stainless steel
  Is it necessary to have such a smooth surface?
Gas conditioning: an essential tool
Electropolished stainless steel: speed the process?
Barrel-polished stainless steel: another option
BCP-d niobium: expensive
TiN-coated aluminum: promising…
900 oC degas, CO2 snow, high pressure rinsing…
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 22: Field Emission Test Stand
Spellman -225kV supply, small “R28” inverted insulators, variable cathode/anode gap from to 10 to 50mm, field strength to ~ 20 MV/m
Build a test stand that resembles an actual gun (tests with small gaps and high field strength but low voltage, don’t appear to be very useful)
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 23: Diamond-Paste Polishing
Receive the electrode from the machine shop with “32” surface finish
Silicon carbide polishing with 300 grit paper to remove obvious visible scratches
Solvent cleaning in ultrasonic bath of alkali solution
Silicon carbide polishing with 600 grit paper
Solvent cleaning in ultrasonic bath of alkali solution
Polish with 6mm grit
Ultrasonic clean
Polish with 3mm grit
Ultrasonic clean
High pressure rinsing (1200 psi) for 20 minutes with ultrapure de-ionized water with resistivity > 18 MWcm.
High temperature (900oC) vacuum degas for one hour
Two months later and the electrode is ready for high voltage!
Maybe it will work!?
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 24: Gas Conditioning
Field emission ionizes inert gas
Ions bombard electrode, hopefully near field emitter, which can be sputtered away
And ions get implanted, increasing work function
Gas Bottle
Leak Valve
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 25: What Does Gas Conditioning Do?
Benefits of implantation are reversible
Chart: Voltage(kV)
| 130 | 140 | 145 | 150 | 155 | 160 | 165 | 170
50mm | 12.8313 | 34.1552 | 60.6168 | 157.3375 | 161.0348 | 362.6544 | 605.7589 | 976.6129
50mm fit | 7.2957 | 31.8035 | 61.7633 | 115.0183 | 206.213 | 357.1857 | 599.5639 | 977.9558
50mm Post Kr | 44.5765 | 63.8627 | 87.5678 | 126.9394 | 151.0407 | 281.1932
50mm post Kr fit | 23.2367 | 25.5006 | 27.9581 | 30.6235 | 33.5118 | 36.6389 | 40.0218 | 43.6783 | 47.6272 | 51.8885 | 56.4833 | 61.4337 | 66.7632 | 72.4964 | 78.6593 | 85.2792 | 92.3849 | 100.0066 | 108.1759 | 116.9262 | 126.2924 | 136.3111 | 147.0206 | 158.4612 | 170.6748 | 183.7055 | 197.5992 | 212.404 | 228.1701 | 244.9498 | 262.7979 | 281.7712 | 301.9292 | 323.3339 | 346.0495 | 370.1434 | 395.6851 | 422.7473 | 451.4054 | 481.7378 | 513.8258 | 547.754 | 583.61 | 621.4848 | 661.4726 | 703.671
50 Post Heat | 10.1271 | 20.4936 | 25.9845 | 42.6052 | 73.3234 | 134.4807 | 174.3246 | 301.2494 | 459.0172 | 725.192 | 1117.2914
50 Post heat fit | 5.3833 | 6.1872 | 7.0988 | 8.1308 | 9.2972 | 10.6135 | 12.0966 | 13.765 | 15.6393 | 17.7417 | 20.0966 | 22.7305 | 25.6727 | 28.9545 | 32.6105 | 36.6778 | 41.1972 | 46.2123 | 51.7708 | 57.9241 | 64.7277 | 72.2415 | 80.5301 | 89.6631 | 99.7153 | 110.7671 | 122.9049 | 136.2214 | 150.8159 | 166.7947 | 184.2715 | 203.3681 | 224.2142 | 246.9485 | 271.7187 | 298.6823 | 328.0067 | 359.8703 | 394.4624 | 431.9842 | 472.6492 | 516.6837 | 564.3277 | 615.8351 | 671.4747 | 731.5307 | 796.3033 | 866.1098 | 941.2847
Matt Poelker, Jefferson Lab
Work of M. BastaniNejad, E. Forman, C. Hernandez-Garcia
Notes: Interior Page Design 2

## Slide 26: What Does Gas Conditioning Do?
Sputtering and Implantation
Sputtering Yield
Helium
Krypton
Implantation
Helium: provides a shallow implantation depth, so it seems to work best when FE turns ON at lower voltages, and/or with small gaps (10 to 20mm), don’t expect much sputtering
Krypton: can work at any voltage, good for larger gaps (30 to 50mm), sometimes too much sputtering creates a new field emitters
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 27: A Powerful Technique
Gas conditioning can turn a BAD electrode into a GOOD electrode
TURN OFF ion pump
NEG pumps don’t pump inert gas
Set voltage to excite field emitter
Add gas at 10-5 Torr, apply voltage and watch for sharp decrease in FE current
Perhaps 316L is better than 304L?
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 28: Backup Slides
Thank You
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 29: Diamond-Paste Polished Stainless Steel
Variable performance is common
Favorable response to gas conditioning
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 30: I to V curves for Niobium
Text goes here
304-SS
Fine Grain Nb
Large Grain Nb
Single Crystal Nb
Notes: Interior Page Design 2

## Slide 31: Buffered Chemical Polishing of Niobium
Receive the electrode from the machine shop with “32” surface finish
Silicon carbide polishing with 600 grit paper, if necessary, to remove obvious visible scratches
Solvent cleaning in ultrasonic bath of alkali solution
Buffered-chemical polishing to remove ~ 100 mm material
High pressure rinsing (1200 psi) for 20 minutes with ultrapure de-ionized water with resistivity > 18 MWcm.
High temperature (900oC) vacuum degas for one hour
Notes: Interior Page Design 2

## Slide 32: FE results of BCP-ed Niobium
Field strength at which the electrode exhibited 100pA of field emission, post krypton gas conditioning
“>” symbol….the electrode did not produce 100pA of field emission
Notes: Interior Page Design 2

## Slide 33: Niobium Electrodes
More evidence that there’s more to field emission than topography
SS Roughness: 10.9 nm
FGNb Roughness: 215.1 nm
LGNb Roughness: 141.01 nm
SCNb Roughness: 17.6 nm
This one performed best!
Notes: Interior Page Design 2

## Slide 34: Electropolished Stainless Steel
Can we avoid time-consuming diamond-paste polishing?
Start with three test electrodes having different surface finish, and send them to commercial electropolishing company
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 35: TiN-coated aluminum
Aluminum is cheap and easy to machine
Takes just hours to polish to mirror-like finish with silicon-carbide paper
Good thermal conductor, compared to steel, a nice feature when gun provides high current
We used a “boutique” vendor to coat our small electrodes
Can an industrial TiN-coating provide the same benefit? Need to test
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 36: Surface Images Al and TiN-Al
Al: 400 grit
Al: 600 grit
Al: 800 grit
Al: 1200 grit
TiN coated: 1200 grit
Note, the black spots are voids and defects, not particulate contamination from sand paper polishing
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 37: TiN-coated aluminum
Bare aluminum:
easily damaged
Diamond-paste polished Ti-alloy:
a traditional “hard” electrode
TiN-coated
aluminum
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 38: Fowler-Nordheim Line Plots
= -
intercept =
Chart: 1/E (m/V)
| 1.4517159282271744E-7 | 1.3938447814451455E-7 | 1.2909222348445823E-7 | 1.2021542604347079E-7 | 1.1248087825069815E-7 | 1.0897519724510805E-7
50mm | -25.332 | -24.9733 | -23.9922 | -23.3893 | -23.0871 | -22.9542
40mm | -25.3428 | -24.4531 | -23.7971 | -23.3099 | -22.8395
30mm | -25.5737 | -24.528 | -23.9002 | -23.3234 | -22.9737
20mm | -26.0064 | -24.3516 | -23.8119 | -23.3283 | -22.9891
50mm | -26.066 | -25.973 | -25.6438 | -25.3029 | -25.0805 | -24.7873
40mm | -25.8659 | -25.4115 | -25.137 | -24.8534 | -24.6127
30mm | -25.6619 | -25.0252 | -24.7644 | -24.4842 | -24.2283
20mm | -24.4783 | -24.2362 | -23.9555 | -23.7152
These plots tell you b, the field enhancement factor, and Ae, the field emitter area
But it’s wrong to assume work function, F , is a constant
With three variables, there are an infinite number of solutions that provide a good fit
Notes: Interior Page Design 2

## Slide 39: Fowler-Nordheim Line Plots
Text goes here
Identical here
Why not identical here?
Notes: Interior Page Design 2

## Slide 40: Electropolished Stainless Steel
EP-d electrodes exhibited less variability
EP-d electrodes did not respond favorably to gas conditioning
Best electrodes were DPP-d
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 41: Barrel Polishing of Stainless Steel
On our to-do list for testing
Notes: Interior Page Design 2

## Slide 42: CEBAF – Just a big Microscope
A
B
C
A
B
C
RF Synchronous
Lasers
499 MHz,
ΔФ = 120
Pockels Cell
Gun
two SRF Linacs
1497 MHz
RF Separators
499 MHz
B
A
C
A B C A B C
111 ps
Photoemission from GaAs photocathode
Matt Poelker, Jefferson Lab
Continuous Electron Beam Accelerator Facility
Notes: Interior Page Design 2

## Slide 43: JLab Energy Recovery Linac
Powerful light source
IR and UV FEL
THz light
Search for Dark Matter
Fixed Target Options
Beam accelerated from 5 to 100 MeV and then decelerated back to 5 MeV, to recover the energy
Matt Poelker, Jefferson Lab
10 mA at 100 MeV : 1 MW beam power!!
Energy Recovery Linac, with internal target, makes this experiment possible
But with CsK2Sb photocathode…
Notes: Interior Page Design 2

## Slide 44: Electron Ion Collider at JLab
Pre-booster
Ion linac
MEIC
High-Energy Arc (Stage II)
e injection
IP2
IP1
Hall D
Halls A-C
C E B A F
Stage I MEIC
  CEBAF as full-energy e-/e+ injector
  3 to12 GeV e-/e+
  25 to100 GeV protons
  12 to40 GeV/u ions
Stage II EIC
  up to 20 GeV e-/e+
  up to 250 GeV protons
  up to 100 GeV/u ions
Two independent but complementary detectors
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 45: MEIC Layout
Cross sections of tunnels for MEIC
Warm large booster
(up to 25 GeV/c)
Warm 3-12 GeV
electron collider ring
Medium-energy IPs with
horizontal beam crossing
Injector
12 GeV CEBAF
Prebooster
SRF linac
Ion
source
Cold 25-100 GeV/c
proton collider ring
Three Figure-8 rings
stacked vertically
Electron cooling
Matt Poelker, Jefferson Lab
Notes: Interior Page Design 2

## Slide 46: Plan B
Plan A
Plan D
Plan C
Insulator sleeve
Screening electrode, or “shed”
No Improvement