## Slide 1: Positron Target Design and Fatigue Studies
e+ Production by Polarized e‒ Beam
Radiation Damage and Heat Load in Target
Design of High Power Target
Target Material Tests with e‒ Beam and Laser
A. Ushakov (Ce+BAF WG)
This project has received funding from the European Union’s Horizon 2020 research and innovation program under grant agreement STRONG-2020 No 824093

## Slide 2: Polarization Transfer from e‒ to e+ in a Single High-Z Target
PEPPo (Polarized Electrons for Polarized Positrons) experiment demonstrated the feasibility of using bremsstrahlung of MeV Polarized Electrons for production of Positrons with a high level of polarization.
(PEPPo Collaboration) D. Abbott et al. Phys. Rev. Lett. 116 (2016) 214801
1 μA @ 8.2 MeV e‒, 1 mm W target
e+ Polarization vs Energy

## Slide 3: Optimal Target Thickness and e+ Yield
Δpe+/pe+ = ±0.05
Tungsten
Yield vs Target Thickness
High-current e‒ beam is needed (1 mA)
High deposited in target power (17 kW)
For 120 MeV e‒ at polarized mode (max FoM = ):
Optimal Thickness of W Target = 4 mm
e+ Yield 10-3

## Slide 4: LERF Polarized Positron Injector Concept
#6 – SRF accelerate e+ to 123 MeV
#4 - Produce and collect e+ 20 to 60 MeV
#2 - SRF accelerate to 120 MeV
#1 – Compact 10 mA P-Gun, Wien filter, 10 MeV e- injector
#3 – Extract e- to target
#8 – Transport e+ at 123 MeV to CEBAF
#5 – Transport e+
Focus is developing a technical report on a polarized e+ injector at LERF
  High current polarized electron injector (10 MeV/10 mA)
  High current 1-3 mA LINAC (two C75 CM)
  Positron conversion target (~100 kW)
  Positron bunch collection and momentum selection
  Positron bunch compression and acceleration to 123 MeV
#7 – Evaluating 123 MeV spin rotator concept

## Slide 5: Concept and Challenges of High-Power Target
Static target would melt in 64 ms
1 mA @ 120 MeV cw e‒ beam
σbeam = 1.5 mm
Temperature in Stationary Target
Some parameters of currently considered model of e+ target:
Beam passes through the target at R of 17.5 cm
4 m/s target tangential speed at R of 17.5 cm
10x20 mm2 cross-section of water channel inside Cu disk
24 l/min rate of water flow
Target Challenges:
High (average) heat → cool and rotate
Radiation damage → rotate
Material fatigue cause by cycling temperature → study material properties under realistic conditions
1/12 Segment of Rotated Target
Target Concept

## Slide 6: Radiation Damage of 17 kW Tungsten Target
Radiation Damage of Stationary Target
Radiation Damage < 0.5 dpa
Ø35 cm W Target
1 mA @ 120 MeV e‒
1.5 mm rms spot size σ
Radiation Damage of Rotated Target
Max Rad. Damage of Tungsten = 1.02E-19 dpa/e‒

## Slide 7: Average Temperature and Radiation Damage in 17 kW Tungsten Target
Average Temperature in Tungsten
Temperature of Water
Tmax = 258 °C
Tmax = 61 °C
Average Thermal Stress
σvM max = 282 MPa

## Slide 8: Thermal Cycling in 17 kW Tungsten Spinning Target (Ø35 cm, vrot = 4 m/s)
Thermal Cycle
Heating Phase
Temperature and Stress at the End of Heating Phase
ΔTmax ≈ 120°C
Tmax ≈ 340°C
σvM max ≈ 150 MPa
+ 280 MPa due to Tave = 258°C
Duration of Heating ≈
2.5 ms
Period of Cycles =
275 ms
σfatigue = ? MPa
Check fatigue limits experimentally

## Slide 9: Fatigue Limit (Plansee and ANSYS Granta Data)
Fatigue Limit = k (Number of Cycles) * Yield Strength (T), where k = < 1
Yield Strength σ0.2 vs Temperature
Tungsten (Plansee)
High temperature reduces the yield strength
Material fatigue under cyclic thermal loading can initiate and grow cracks (fracture)
Tungsten at 22°C
(ANSYS Granta)
Max Alternating Stress vs Number of Cycles
For 17 kW Tungsten Target
Ø35 cm, 4 m/s rot. speed
6.5E+7 cycles/5000h
Tmax ≈ 340°C
σvM max ≈ 430 MPa
k (6.5E+7 cycles) = 0.52
σ0.2 (340°C) = 1020 MPa
σfatigue (6.5E+7 cycles; 340°C) ≈ 530 MPa

## Slide 10: Test of Target Materials with e‒ Beam at Mainz Microtron (MAMI)
Test changes/degradation of target properties after 106-107 thermal cycles. Check target fatigue at average elevated temperature of about 300°C
Investigate impact of radiation damage on target material properties between 0.1 and 0.5 dpa at expected elevated temperatures
Test different high Z materials: W, Ta, W-alloys, to evaluate candidate target materials
3.5 MeV e‒
I < 50 μA
σ > 50 μm
Sketch of Targets and e‒ Beam

## Slide 11: Peak Heat Density and Cycling Temperature in Tungsten for 3.5 MeV e‒ Beam
Deposited Power Density in 0.1 mm W Foil
50 μA @ 3.5 MeV e‒ beam, σ = 0.1 mm
Peak Heat Density = 2.18 kW/mm3
Average T
Pulse Length = 0.4 ms
Cycling Temperature
Pulse Period = 3.74 ms
Tave = 300 °C
Tmax = 400 °C
ΔT = 120 °C

## Slide 12: Temperature of Tungsten Foil. 3.5 MeV e‒ Beam with Duty Cycle of 0.107
Average Temperature
Thickness of W target: 100 μm
Length of W target: 42 mm
Width of W target: 3 mm
0.4 ms pulse length
3.74 ms pulse periodi
Tmax = 300 °C
Profiles of Max and Min Cycling Temperatures

## Slide 13: Thermal Stress in Tungsten Foil. 3.5 MeV e‒ Beam with Duty Cycle of 0.107
Average Temperature
Max Thermal Stress at t = 3.74 ms
0.4 ms pulse length, 3.74 ms pulse periodi
Max Thermal Stress at t = 0.4 ms
σvM ≈ 133 MPa
σvM ≈ 46 MPa

## Slide 14: Radiation Damage by 50 μA @ 3.5 MeV e‒ Beam with Spot Size σ = 50 μm
Max Rad. Damage of Tungsten = 1.02E-19 dpa/e‒
50 μA 3.125E+14 e‒/s
For radiation damage of 0.23 dpa:
Pulsed e‒ beam with 50% duty cycle (1 ms pulse length and 2 ms pulse period):
  4 hours of beam time
  Average temperature of 700 °C
or/and
Pulsed e‒ beam with 22% duty cycle (1.1 ms pulse length and 5 ms pulse period):
  9.1 hours of beam time
  Average temperature of 300 °C
Radiation Damage in the Middle of Beam

## Slide 15: Test of Target Materials with Laser at JLab LERF Laser Lab 6
Existing laser setup will be used for testing e+ target materials
10 W lasers (532 nm) were used for testing 18 µm W foils to their limits and beyond [S. Gopinath, S. Covrig “APEX Target Thermal Assessment”, PMAG0000-0001-A0001, 10/29/2020]:
Experimental Setup
CAD assembly
S. Gopinath
SEM Images of APEX Target with Micro-Fractures at Beam Spot

## Slide 16: Test of Target Materials with Laser at JLab LERF Laser Lab 6
Experimental setup at LERF Laser Lab 6 would allow us to test the high peak heat loads (significantly higher than could be achieved with MAMI e‒ beam) and fatigue of target materials in the wide temperature range
Test of thermal contact conductance between high-Z materials and Cu or Al (Ce+BAF and ILC targets)
Possibility of testing low-power stationary target is being studied
Cooling Tube
Target Design (Silviu Covrig)
Target (25x25 mm)
Cu
Frame
Targets
Cu
Washer
Beam Clearance 12.5x12.5 mm2

## Slide 17: Summary and Outlook
We are focused on developing 123 MeV e+ injector at LERF
By the end of the year we want to complete a technical design report on e+ injector
Development and test of e+ targets:
  JLab Phase I: Prototype/proof-of-principle of low-power stationary solid water-cooled target (< 4 kW)
  JLab Phase II: High-power rotated solid water-cooled target (17 ‒ 20 kW)
  Xelera Research LLC is exploring (DOE SBIR) liquid metal targets (Ga-In-Sn / Pb-Bi)
Target material tests:
  Radiation damage and fatigue of target materials with pulsed 3.5 MeV e+ beam at MAMI on Mar 31 – Apr 5, 2023 (W, Ta) and in Fall 2023 (W-alloys)
  Study of irradiated targets with PETRA X-rays at DESY
  Fatigue target tests with a laser at JLab LERF Laser Lab 6 (Summer 2023)
This project has received funding from the European Union’s Horizon 2020 research and innovation program under grant agreement STRONG-2020-No 824093

## Slide 18: Acknowledgments
I would like to acknowledge those who have contributed to this presentation
Silviu Covrig
Christine Le Galliard
Sandesh Gopinath
Joe Grames
Sami Habet
Eric Voutier
Shukui Zhang

## Slide 19
Backup Slides

## Slide 20: Temperature Profiles at the End of Pulse for Different Sizes of Beam Spot
Thermocouples have to be placed very close to the beam in order to be able to measure cycling temperature
50 μA @ 3.5 MeV e‒ beam, 100 μm W foil