Charge Lifetime Studies Summer 2017
Data taken between May and September
Cathode SLSP 5756-4 used – type?
Four Activations done on this cathode, data taken after each and prior to first
Cathode used for previous CEBAF Run and Isotope production experiment at CEBAF prior to Charge Lifetime Studies
C-laser used in 4 different beam size configurations
Laser table lens “Caption Expando” installed => 4 * 2 (Lens in vs out) Laser beam sizes used

---
Charge Lifetime Studies Summer 2017
Each Run –
Delivered 0.25 – 2.00 mA of electron beam several meters to FC1
Before and after beam delivery, measured laser power for given laser size and attenuator
Run durations ~4 – 10hrs each
Recorded vacuum ion pump signals from gun to FC1
Recorded radiation levels using DecaRad system with 8 probes strategically placed around electron gun and apertures

---
C-Laser Sizes
Configuration	Lens State	X-avg (mm)	Y-avg (mm)	Area (mm^2)
c1	OUT	1.919	2.191	3.30
c1	IN	3.349	3.763	9.90
c2	OUT	3.942	3.557	11.01
c2	IN	5.354	5.032	21.16
c3	OUT	3.225	3.053	7.73
c3	IN	4.412	4.152	14.39
c4	OUT			2.54
c4	IN			7.06

---
Activations and Cathode Spots
Configuration	Activation Date	Cathode X Pos	Cathode Y Pos
a0		12000	9000
a1	6/19	12000	9000
a2	6/27	13500	10500
a3	7/21	11000	9500
a4	8/18	12000	11250
		11750	9750
		10250	10500
		11250	11750
		10500	11500
		10500	9500
a4

---
Charge Lifetime Calculation

---
Charge Lifetime Calculation

---
Charge Lifetime vs Laser Spot Size and e-beam Current

---
Charge Lifetime vs Distance from Electrostatic Center of Cathode – a4c4
Before Spot 1 {12000, 11250}	Before Spot 2 {11750, 9750}	Before Spot 3 {10250, 10500}
Before Spot 4 {11250, 11750}	Before Spot 5 {10500, 11500}	Before Spot 6 {10500, 9500}

---
Charge Lifetime vs Distance from Electrostatic Center of Cathode – a4c4
After all runs (2 on each spot with different lens states) in activation a4
Electrostatic Center
X = 11250
Y = 11750

---
Charge Lifetime vs Distance from Electrostatic Center of Cathode – a4c4

---
Charge Lifetime vs Vacuum and Radiation Monitors