## Slide 1: Update on magnetized electron gun development at the Gun Test Stand GTS
P. Adderley, D. Bullard, F., Hannon, C. Hernandez-Garcia, A. Mamun, M. Poelker, R.Suleiman, Y. Wang
JLEIC R&D weekly meeting, Thursday Jan 26, JLab.

## Slide 2
Anode
K2CsSb
Photocathode
Cathode
Solenoid
(Bz=2kG)
Diagnostic Cross 1
(Slit + YAG Screen)
Diagnostic Cross 2
(Slit + YAG Screen)
Diagnostic Cross 3
(YAG Screen)
Beamline
Focusing
Solenoid
Experimental Overview: Gun Test Stand
Generate magnetized beam:
  Laser size: 1– 5 mm, Bz = 0 – 2 kG
  Bunch charge: 1 – 500 pC
  Frequency: 15 Hz – 476.3 MHz
  Bunch length: 10 – 100 ps
  Average beam currents up to 32 mA
  Gun high voltage: 200 – 350 kV
Green
Laser
150 cm

## Slide 3
K2CsSb Photocathode Preparation Chamber, Gun and Beamline: delivered 1 mA, 300 keV to dump (non-magnetized)
  Simulation (Fay Hannon):
  Used ASTRA and GPT simulation to design beamline and to locate magnets and diagnostics at optimum positions
  Simulated magnetized electron beam properties along beamline for various starting conditions
  Simulated a round to flat transformer
FY16 Accomplishments (summer 2016)

## Slide 4: GTS Beam Line as it was in Summer 2016 for beam ops
EB Viewers
Faraday Cup (dump)
Focusing solenoids
Steering magnets
The EB is generated at the HV Gun and transported to the Faraday Cup (beam dump) where the beam current is measured (QE evaluation over time).
1 m
Photocathode preparation chamber
HV Gun

## Slide 5
300kV Inverted insulator gun with CsK2Sb Photocathode
8 MV/m
11 MV/m
Pure alumina insulator with diamond paste hand polished electrodes conditioned to 325kV, but operated at 300kV due to field emission (from dusty NEG strips on bottom of vacuum chamber)
@ 350kV
6” ball diameter

## Slide 6
First beam on May 20 2016

## Slide 7
We observed no QE decay up to 1 mA:
We were not been able to increase to 5 mA because ion back bombarding induces arcing in the photocathode, decreasing the QE…
1mA DC
0.5 mA DC
Same cathode, two different runs
Canales, Mexican Autonomous University,
intern student summer 2016.

## Slide 8: ..even so, CsK2Sb cathode is very robust
8
18 Jul
Initial QE
Are arcing events vacuum induced ?
Laser ON
Laser OFF
Freshly made cathode
1 cm
Non-masked cathode = significant beam halo
Grown on GaAs substrate
1 cm
Some other times the QE at laser-illuminated spot barely changes after each arcing event
Sometimes QE at laser-illuminated spot drops significantly after each arcing event
Large initial QE drop
Same cathode, different runs
HVPS current bursts correlated to arcing events
Canales, Mexican Autonomous University intern student summer 2016.

## Slide 9
Molybdenum
Steel
After concluding beam studies in summer 2016, we proceeded with Magnet Coil installation & beamline upgrade
New Pucks
  Designed to enhance magnetic field at cathode to 2.0 kG
Design and
modeling by Jay Benesch

## Slide 10
The upgrade beamline currently under installation has slits for magnetized beam characterization and emittance measurements.
Slit
YAG Screen

## Slide 11
The magnet coil has been installed and commissioned

## Slide 12: The cathode prep chamber has been improved
Making photocathode in the original chamber was tremendously difficult because the photocurrent could not me monitored, ie the puck was at ground through its heater and holder.
Biasing a nearby anode ring proved useless because it was collecting photoemission from the chamber walls!

## Slide 13: Mamun developed a novel concept for grabbing the puck based on the retainer mechanism used inside the ball electrode, allowing to:
  Bias the puck to monitor photocurrent during activation and measuring QE in-situ
  Heat the puck during activation
  Finely control the gap between puck and Cs-K effusion source for precise film growth
  Use a mask for reducing active area to minimize electron beam halo

## Slide 14: The gun has been refurbished
Pure alumina insulator replaced with doped alumina for higher voltage stand-off and robust operations
Electrode ‘shed’ (triple junction shield) re-designed by Yan Wang to lower gradient from 12 MV/m to 10 MV/m at 350kV
Pure alumina insulator
Doped alumina insulator

## Slide 15: Gun refurbishing continued
Electrodes have been polished with barrel tumbling technique developed by Don Bullard, cutting down the polishing time from 1 week to 1 day !!!
As received from machine shop
After barrel polishing for 30 min in plastic cones + 30 min corncob

## Slide 16: Gun refurbishing continued
Replaced dusty NEG sheets and wire mesh shield with full NEG modules and perforated plate to minimize dust and keep electric field from pulling it towards electrode

## Slide 17: As a result of gun improvements the gun high voltage conditioning takes 1/3 of the time!
Indicated voltage reached with Kr processing
Diamond Paste Polished
Barrel Polished

## Slide 18: The inverted insulator gun electrostatic ‘package’ shows robust operation at 365kV with Kr
kV

## Slide 19: The gun has been conditioned up to 340kV in vacuum

## Slide 20: But first trials with gun at 340kV AND magnet coil at 200 A resulted in field emission and vacuum activity

## Slide 21: Is this the first time a 300kV DC gun has been operated with a solenoid coil !!??!!

## Slide 22: For the sake of progress, we decided to operate at 300kV and re-condition for 100, 200, 300 and 400 A magnet coil current set points
300kV
Vacuum 5 nA
Ion pump current
Magnet coil ON 200 A
Field emission 20 Counts per Second
Vacuum 2 nA
Ion pump current

## Slide 23: The GTS work also benefits activities at CEBAF for the gun upgrade and at the UITF
Barrel polishing applied to the Wien electrodes which tested successfully for the gradient needed to support 200keV Ops at CEBAF
The UITF DC Photogun is a copy of the improved GTS gun
We anticipate implementing the GTS gun improvements to the upgrade 200keV photogun at CEBAF

## Slide 24
In the next few weeks we plan to:
Make CsK2Sb photocathode in improved cathode preparation chamber
Complete beam line assembly
Vacuum bake beam line
Implement Instrumentation and Control for new diagnostics, added solenoids and steering coils
Complete gun high voltage conditioning at 300kV with magnet coil at 100, 200, 300 and 400 A current set points
      Make beam!