## Slide 1
JLAB/BNL High Current Polarized Photogun Partnership Brainstorming
November 9, 2015

## Slide 2
Parameter | Value | Value | Value
Gun | CEBAF | Test Cave | Test Cave
Laser Rep Rate | 499 MHz | 499 MHz | 1500 MHz
Laser Pulse Length | 50 ps | 30 ps | 50 ps
Laser Wavelength | 780 nm | 780 nm | 780 nm
Laser Spot Size | 0.75 mm | 0.45 mm | 0.35 mm
Photocathode | GaAs/GaAsP | GaAs/GaAsP | GaAs/GaAsP
Gun Voltage | 130 kV | 100 kV | 200 kV
Beam Current | 0.2 mA | 1 mA | 4 mA
Run Duration | Months | 8.25 hr | 1.4 hr
Extracted Charge | >1000 C | 30.3 C | 20 C
Charge Lifetime | 100 - 200 C | 210 C | 80 C
Fluence Lifetime | 25 – 50 kC/cm2 | 132 kC/cm2 | 83 kC/cm2
Bunch Charge | 0.36 pC | 2.0 pC | 2.7 pC
Peak Current | 7.2 mA | 67 mA | 53 mA
Peak Current Density | 1.6 kA/cm2 | 42 A/cm2 | 55 A/cm2
Charge Fluence Lifetime of GaAs/GaAsP at 780 nm making 0.2 – 4.0 mA at
500-1500 MHz using best practice 100-200 kV JLAB inverted gun is 25 – 130 kC/cm2
Charge Fluence Lifetime Performance of JLAB Guns

## Slide 3
Speculating that 25 – 130 kC/cm2 is a scalable property of the source then the FWHM laser spot size of 0.9 – 2.0 mm would be required to generate an 800 C lifetime
We learned that operating at constant current best reflects a consistent measure of the photocathode lifetime. We can approach in one of two avenues…
Maintain power < 2 W
Assuming QE can fall from 1.0 to 0.2% means operating with a current <2.5 mA
This can be achieved with the 225kV (32mA) or 450kV (3mA) HVPS
At 2.5 mA an 800 C lifetime can be measured in 3.5 days
Maintain current 10 mA
Assuming QE can fall from 1.0 to 0.2% means increasing power from 1.6 to 8 W
This can only be achieved with the 225kV (32mA) HVPS
At 10 mA and 800 C lifetime can be measured in 1 day

## Slide 4
Considerations…
Retain or implement best practices
  Minimize or eliminate beam loss (vacuum diagnostics)
  Reduce outgassing (baked beam line, baked dump)
  Increase isolation (differential pumping)
  Operate with biased anode
  Operate in DC mode (eliminate longitudinal space charge)
Maintain power < 2 W and current < 2.5 mA
“Immediately” operate up to 225kV (10mA) with previous beam line components
“UITF Commission” operate up to 350kV from 450kV (3mA) HVPS
  Implement biased anode
  Design and fabricated higher voltage 15 deg dipole
  Study ion voltage dependence and increase laser spot size
Maintain current 10 mA and laser power < 8 W
Can only be done with 225kV (10mA) HVPS so existing beam line components satisfactory
Requires higher power laser (dc is good; doubled 1560nm requires more beam care)
Cathode cooling required
  Opportunity to introduce cooling circuit
  Replace electrode “inner-tee” with copper or aluminum to provide thermal short
  Cooling between R350 socket / FEL insulator with Fluroinert of SF6