Weight %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min_pt1 | 4.97 | 2.11 |  | 43.53 | 49.40 |  |  |
| 90 min_pt2 | 8.73 | 8.89 |  | 61.98 | 20.40 |  |  |
| 90 min_pt3 | 4.75 | 19.56 | 4.55 |  |  | 32.08 | 39.06 |
| 90 min_pt4 | 6.55 | 20.46 | 5.38 |  |  | 25.76 | 41.85 |

Weight % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min_pt1 | +/-0.80 | +/-0.37 |  | +/-4.25 | +/-9.07 |  |  |
| 90 min_pt2 | +/-1.24 | +/-0.95 |  | +/-7.42 | +/-8.16 |  |  |
| 90 min_pt3 | +/-0.58 | +/-0.72 | +/-0.50 |  |  | +/-2.32 | +/-2.67 |
| 90 min_pt4 | +/-0.76 | +/-0.51 | +/-0.50 |  |  | +/-2.24 | +/-2.71 |

Normalized Wt. %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min_pt1 | 4.97 | 2.11 |  | 43.53 | 49.40 |  |  |
| 90 min_pt2 | 8.73 | 8.89 |  | 61.98 | 20.40 |  |  |
| 90 min_pt3 | 4.75 | 19.56 | 4.55 |  |  | 32.08 | 39.06 |
| 90 min_pt4 | 6.55 | 20.46 | 5.38 |  |  | 25.76 | 41.85 |

Norm. Wt. % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min_pt1 | +/-0.80 | +/-0.37 |  | +/-4.25 | +/-9.07 |  |  |
| 90 min_pt2 | +/-1.24 | +/-0.95 |  | +/-7.42 | +/-8.16 |  |  |
| 90 min_pt3 | +/-0.58 | +/-0.72 | +/-0.50 |  |  | +/-2.32 | +/-2.67 |
| 90 min_pt4 | +/-0.76 | +/-0.51 | +/-0.50 |  |  | +/-2.24 | +/-2.71 |

Atom %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min_pt1 | 22.61 | 7.20 |  | 34.14 | 36.05 |  |  |
| 90 min_pt2 | 29.75 | 22.74 |  | 36.37 | 11.14 |  |  |
| 90 min_pt3 | 17.25 | 53.35 | 5.08 |  |  | 11.50 | 12.82 |
| 90 min_pt4 | 21.91 | 51.40 | 5.53 |  |  | 8.51 | 12.66 |

Atom % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min_pt1 | +/-3.63 | +/-1.27 |  | +/-3.33 | +/-6.62 |  |  |
| 90 min_pt2 | +/-4.21 | +/-2.44 |  | +/-4.36 | +/-4.46 |  |  |
| 90 min_pt3 | +/-2.12 | +/-1.96 | +/-0.56 |  |  | +/-0.83 | +/-0.88 |
| 90 min_pt4 | +/-2.55 | +/-1.29 | +/-0.51 |  |  | +/-0.74 | +/-0.82 |

Weight %

|  | C | O | P | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min(2)_pt1 |  |  |  |  | 80.77 | 19.23 |  |  |
| 90 min(2)_pt2 |  |  |  |  | 84.85 | 15.15 |  |  |
| 90 min(2)_pt3 | 4.37 |  |  |  | 51.32 | 44.31 |  |  |
| 90 min(2)_pt4 |  |  |  |  | 78.65 | 21.35 |  |  |
| 90 min(2)_pt5 | 5.75 | 19.73 |  | 4.56 |  |  | 26.30 | 43.66 |
| 90 min(2)_pt6 | 7.61 | 27.25 | 3.30 | 8.05 |  |  |  | 53.78 |
| 90 min(2)_pt7 | 6.63 | 25.81 |  | 6.54 |  |  |  | 61.02 |

Weight % Error

|  | C | O | P | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min(2)_pt1 |  |  |  |  | +/-7.03 | +/-8.45 |  |  |
| 90 min(2)_pt2 |  |  |  |  | +/-7.95 | +/-8.77 |  |  |
| 90 min(2)_pt3 | +/-0.74 |  |  |  | +/-4.16 | +/-8.54 |  |  |
| 90 min(2)_pt4 |  |  |  |  | +/-7.38 | +/-8.54 |  |  |
| 90 min(2)_pt5 | +/-0.58 | +/-0.52 |  | +/-0.36 |  |  | +/-1.61 | +/-0.84 |
| 90 min(2)_pt6 | +/-0.47 | +/-0.62 | +/-0.20 | +/-0.31 |  |  |  | +/-2.02 |
| 90 min(2)_pt7 | +/-0.37 | +/-0.54 |  | +/-0.27 |  |  |  | +/-1.93 |

Normalized Wt. %

|  | C | O | P | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min(2)_pt1 |  |  |  |  | 80.77 | 19.23 |  |  |
| 90 min(2)_pt2 |  |  |  |  | 84.85 | 15.15 |  |  |
| 90 min(2)_pt3 | 4.37 |  |  |  | 51.32 | 44.31 |  |  |
| 90 min(2)_pt4 |  |  |  |  | 78.65 | 21.35 |  |  |
| 90 min(2)_pt5 | 5.75 | 19.73 |  | 4.56 |  |  | 26.30 | 43.66 |
| 90 min(2)_pt6 | 7.61 | 27.25 | 3.30 | 8.05 |  |  |  | 53.78 |
| 90 min(2)_pt7 | 6.63 | 25.81 |  | 6.54 |  |  |  | 61.02 |

Norm. Wt. % Error

|  | C | O | P | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min(2)_pt1 |  |  |  |  | +/-7.03 | +/-8.45 |  |  |
| 90 min(2)_pt2 |  |  |  |  | +/-7.95 | +/-8.77 |  |  |
| 90 min(2)_pt3 | +/-0.74 |  |  |  | +/-4.16 | +/-8.54 |  |  |
| 90 min(2)_pt4 |  |  |  |  | +/-7.38 | +/-8.54 |  |  |
| 90 min(2)_pt5 | +/-0.58 | +/-0.52 |  | +/-0.36 |  |  | +/-1.61 | +/-0.84 |
| 90 min(2)_pt6 | +/-0.47 | +/-0.62 | +/-0.20 | +/-0.31 |  |  |  | +/-2.02 |
| 90 min(2)_pt7 | +/-0.37 | +/-0.54 |  | +/-0.27 |  |  |  | +/-1.93 |

Atom %

|  | C | O | P | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min(2)_pt1 |  |  |  |  | 81.87 | 18.13 |  |  |
| 90 min(2)_pt2 |  |  |  |  | 85.75 | 14.25 |  |  |
| 90 min(2)_pt3 | 21.51 |  |  |  | 43.52 | 34.97 |  |  |
| 90 min(2)_pt4 |  |  |  |  | 79.83 | 20.17 |  |  |
| 90 min(2)_pt5 | 20.18 | 51.97 |  | 4.91 |  |  | 9.10 | 13.84 |
| 90 min(2)_pt6 | 20.76 | 55.77 | 3.49 | 6.74 |  |  |  | 13.25 |
| 90 min(2)_pt7 | 19.77 | 57.79 |  | 5.99 |  |  |  | 16.45 |

Atom % Error

|  | C | O | P | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 90 min(2)_pt1 |  |  |  |  | +/-7.13 | +/-7.97 |  |  |
| 90 min(2)_pt2 |  |  |  |  | +/-8.03 | +/-8.25 |  |  |
| 90 min(2)_pt3 | +/-3.66 |  |  |  | +/-3.53 | +/-6.74 |  |  |
| 90 min(2)_pt4 |  |  |  |  | +/-7.49 | +/-8.07 |  |  |
| 90 min(2)_pt5 | +/-2.04 | +/-1.37 |  | +/-0.38 |  |  | +/-0.56 | +/-0.26 |
| 90 min(2)_pt6 | +/-1.28 | +/-1.27 | +/-0.22 | +/-0.26 |  |  |  | +/-0.50 |
| 90 min(2)_pt7 | +/-1.12 | +/-1.22 |  | +/-0.25 |  |  |  | +/-0.52 |

Weight %

|  | C | O | Al | Si | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min_pt1 | 6.28 | 26.24 |  |  | 9.25 |  |  |  | 58.22 |
| 60 min_pt2 | 7.02 | 18.88 |  | 0.14 | 4.28 | 10.48 | 9.16 | 21.86 | 28.18 |
| 60 min_pt3 | 5.98 | 22.25 |  |  | 4.98 | 6.28 |  | 29.16 | 31.34 |
| 60 min_pt4 | 7.61 | 22.37 |  |  | 4.38 | 5.90 |  | 25.72 | 34.01 |
| 60 min_pt5 | 7.19 | 21.47 |  |  | 5.23 | 4.53 |  | 25.67 | 35.90 |
| 60 min_pt6 | 7.40 | 23.98 | 0.13 | 0.13 | 5.30 |  |  | 25.76 | 37.29 |

Weight % Error

|  | C | O | Al | Si | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min_pt1 | +/-0.27 | +/-0.44 |  |  | +/-0.22 |  |  |  | +/-1.32 |
| 60 min_pt2 | +/-0.51 | +/-0.39 |  | +/-0.05 | +/-0.22 | +/-1.01 | +/-2.02 | +/-1.02 | +/-1.13 |
| 60 min_pt3 | +/-0.64 | +/-0.52 |  |  | +/-0.28 | +/-1.14 |  | +/-1.31 | +/-1.63 |
| 60 min_pt4 | +/-0.41 | +/-0.36 |  |  | +/-0.10 | +/-0.80 |  | +/-0.81 | +/-1.10 |
| 60 min_pt5 | +/-0.42 | +/-0.39 |  |  | +/-0.21 | +/-0.86 |  | +/-0.93 | +/-1.20 |
| 60 min_pt6 | +/-0.41 | +/-0.40 | +/-0.06 | +/-0.06 | +/-0.11 |  |  | +/-0.40 | +/-1.26 |

Normalized Wt. %

|  | C | O | Al | Si | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min_pt1 | 6.28 | 26.24 |  |  | 9.25 |  |  |  | 58.22 |
| 60 min_pt2 | 7.02 | 18.88 |  | 0.14 | 4.28 | 10.48 | 9.16 | 21.86 | 28.18 |
| 60 min_pt3 | 5.98 | 22.25 |  |  | 4.98 | 6.28 |  | 29.16 | 31.34 |
| 60 min_pt4 | 7.61 | 22.37 |  |  | 4.38 | 5.90 |  | 25.72 | 34.01 |
| 60 min_pt5 | 7.19 | 21.47 |  |  | 5.23 | 4.53 |  | 25.67 | 35.90 |
| 60 min_pt6 | 7.40 | 23.98 | 0.13 | 0.13 | 5.30 |  |  | 25.76 | 37.29 |

Norm. Wt. % Error

|  | C | O | Al | Si | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min_pt1 | +/-0.27 | +/-0.44 |  |  | +/-0.22 |  |  |  | +/-1.32 |
| 60 min_pt2 | +/-0.51 | +/-0.39 |  | +/-0.05 | +/-0.22 | +/-1.01 | +/-2.02 | +/-1.02 | +/-1.13 |
| 60 min_pt3 | +/-0.64 | +/-0.52 |  |  | +/-0.28 | +/-1.14 |  | +/-1.31 | +/-1.63 |
| 60 min_pt4 | +/-0.41 | +/-0.36 |  |  | +/-0.10 | +/-0.80 |  | +/-0.81 | +/-1.10 |
| 60 min_pt5 | +/-0.42 | +/-0.39 |  |  | +/-0.21 | +/-0.86 |  | +/-0.93 | +/-1.20 |
| 60 min_pt6 | +/-0.41 | +/-0.40 | +/-0.06 | +/-0.06 | +/-0.11 |  |  | +/-0.40 | +/-1.26 |

Atom %

|  | C | O | Al | Si | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min_pt1 | 18.44 | 57.79 |  |  | 8.34 |  |  |  | 15.44 |
| 60 min_pt2 | 22.99 | 46.40 |  | 0.19 | 4.31 | 5.91 | 4.81 | 7.06 | 8.34 |
| 60 min_pt3 | 19.30 | 53.87 |  |  | 4.93 | 3.49 |  | 9.28 | 9.13 |
| 60 min_pt4 | 23.50 | 51.87 |  |  | 4.16 | 3.14 |  | 7.84 | 9.49 |
| 60 min_pt5 | 22.84 | 51.22 |  |  | 5.10 | 2.48 |  | 8.05 | 10.31 |
| 60 min_pt6 | 22.39 | 54.46 | 0.18 | 0.17 | 4.92 |  |  | 7.69 | 10.19 |

Atom % Error

|  | C | O | Al | Si | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min_pt1 | +/-0.80 | +/-0.96 |  |  | +/-0.20 |  |  |  | +/-0.35 |
| 60 min_pt2 | +/-1.68 | +/-0.95 |  | +/-0.07 | +/-0.22 | +/-0.57 | +/-1.06 | +/-0.33 | +/-0.33 |
| 60 min_pt3 | +/-2.07 | +/-1.26 |  |  | +/-0.28 | +/-0.63 |  | +/-0.42 | +/-0.48 |
| 60 min_pt4 | +/-1.28 | +/-0.84 |  |  | +/-0.09 | +/-0.42 |  | +/-0.25 | +/-0.31 |
| 60 min_pt5 | +/-1.35 | +/-0.92 |  |  | +/-0.20 | +/-0.47 |  | +/-0.29 | +/-0.35 |
| 60 min_pt6 | +/-1.24 | +/-0.91 | +/-0.08 | +/-0.07 | +/-0.10 |  |  | +/-0.12 | +/-0.34 |

Weight %

|  | C | O | K | Sb | Cs |
| --- | --- | --- | --- | --- | --- |
| 60 min(1)_pt1 | 7.22 | 25.49 | 8.72 |  | 58.57 |
| 60 min(1)_pt2 | 6.41 | 26.43 | 9.13 |  | 58.03 |
| 60 min(1)_pt3 | 4.15 | 17.63 | 8.53 | 14.34 | 55.34 |
| 60 min(1)_pt4 | 7.65 | 21.54 | 6.10 | 28.62 | 36.09 |
| 60 min(1)_pt5 | 7.84 | 22.24 | 5.31 | 26.32 | 38.30 |

Weight % Error

|  | C | O | K | Sb | Cs |
| --- | --- | --- | --- | --- | --- |
| 60 min(1)_pt1 | +/-0.38 | +/-0.61 | +/-0.30 |  | +/-1.88 |
| 60 min(1)_pt2 | +/-0.38 | +/-0.62 | +/-0.33 |  | +/-1.99 |
| 60 min(1)_pt3 | +/-0.38 | +/-0.56 | +/-0.24 | +/-0.66 | +/-2.53 |
| 60 min(1)_pt4 | +/-0.44 | +/-0.41 | +/-0.33 | +/-1.59 | +/-1.89 |
| 60 min(1)_pt5 | +/-0.63 | +/-0.42 | +/-0.17 | +/-0.59 | +/-1.88 |

Normalized Wt. %

|  | C | O | K | Sb | Cs |
| --- | --- | --- | --- | --- | --- |
| 60 min(1)_pt1 | 7.22 | 25.49 | 8.72 |  | 58.57 |
| 60 min(1)_pt2 | 6.41 | 26.43 | 9.13 |  | 58.03 |
| 60 min(1)_pt3 | 4.15 | 17.63 | 8.53 | 14.34 | 55.34 |
| 60 min(1)_pt4 | 7.65 | 21.54 | 6.10 | 28.62 | 36.09 |
| 60 min(1)_pt5 | 7.84 | 22.24 | 5.31 | 26.32 | 38.30 |

Norm. Wt. % Error

|  | C | O | K | Sb | Cs |
| --- | --- | --- | --- | --- | --- |
| 60 min(1)_pt1 | +/-0.38 | +/-0.61 | +/-0.30 |  | +/-1.88 |
| 60 min(1)_pt2 | +/-0.38 | +/-0.62 | +/-0.33 |  | +/-1.99 |
| 60 min(1)_pt3 | +/-0.38 | +/-0.56 | +/-0.24 | +/-0.66 | +/-2.53 |
| 60 min(1)_pt4 | +/-0.44 | +/-0.41 | +/-0.33 | +/-1.59 | +/-1.89 |
| 60 min(1)_pt5 | +/-0.63 | +/-0.42 | +/-0.17 | +/-0.59 | +/-1.88 |

Atom %

|  | C | O | K | Sb | Cs |
| --- | --- | --- | --- | --- | --- |
| 60 min(1)_pt1 | 21.03 | 55.75 | 7.81 |  | 15.42 |
| 60 min(1)_pt2 | 18.68 | 57.85 | 8.17 |  | 15.29 |
| 60 min(1)_pt3 | 15.70 | 50.10 | 9.92 | 5.35 | 18.93 |
| 60 min(1)_pt4 | 24.07 | 50.88 | 5.90 | 8.89 | 10.27 |
| 60 min(1)_pt5 | 24.32 | 51.82 | 5.06 | 8.06 | 10.74 |

Atom % Error

|  | C | O | K | Sb | Cs |
| --- | --- | --- | --- | --- | --- |
| 60 min(1)_pt1 | +/-1.12 | +/-1.33 | +/-0.27 |  | +/-0.49 |
| 60 min(1)_pt2 | +/-1.11 | +/-1.37 | +/-0.29 |  | +/-0.52 |
| 60 min(1)_pt3 | +/-1.42 | +/-1.59 | +/-0.28 | +/-0.25 | +/-0.87 |
| 60 min(1)_pt4 | +/-1.38 | +/-0.97 | +/-0.32 | +/-0.49 | +/-0.54 |
| 60 min(1)_pt5 | +/-1.95 | +/-0.98 | +/-0.16 | +/-0.18 | +/-0.53 |

Weight %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(2)_pt1 | 8.90 | 21.99 | 4.71 | 6.65 | 0.00 | 22.14 | 35.60 |
| 60 min(2)_pt2 | 8.92 | 23.98 | 5.26 |  |  | 26.29 | 35.55 |

Weight % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(2)_pt1 | +/-0.48 | +/-0.59 | +/-0.16 | +/-1.35 | +/-0.00 | +/-1.36 | +/-1.83 |
| 60 min(2)_pt2 | +/-0.63 | +/-0.59 | +/-0.16 |  |  | +/-0.57 | +/-1.77 |

Normalized Wt. %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(2)_pt1 | 8.90 | 21.99 | 4.71 | 6.65 | 0.00 | 22.14 | 35.60 |
| 60 min(2)_pt2 | 8.92 | 23.98 | 5.26 |  |  | 26.29 | 35.55 |

Norm. Wt. % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(2)_pt1 | +/-0.48 | +/-0.59 | +/-0.16 | +/-1.35 | --- | +/-1.36 | +/-1.83 |
| 60 min(2)_pt2 | +/-0.63 | +/-0.59 | +/-0.16 |  |  | +/-0.57 | +/-1.77 |

Atom %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(2)_pt1 | 26.64 | 49.42 | 4.34 | 3.43 | 0.00 | 6.54 | 9.63 |
| 60 min(2)_pt2 | 25.98 | 52.41 | 4.70 |  |  | 7.55 | 9.35 |

Atom % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(2)_pt1 | +/-1.45 | +/-1.32 | +/-0.14 | +/-0.70 | +/-0.00 | +/-0.40 | +/-0.49 |
| 60 min(2)_pt2 | +/-1.83 | +/-1.29 | +/-0.14 |  |  | +/-0.16 | +/-0.47 |

Weight %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(3)_pt1 |  |  |  | 43.10 | 56.90 |  |  |
| 60 min(3)_pt2 | 8.02 | 28.83 | 10.71 |  |  |  | 52.44 |
| 60 min(3)_pt3 | 8.27 | 28.83 | 8.18 |  |  |  | 54.73 |
| 60 min(3)_pt4 | 7.33 | 20.70 | 4.69 |  |  | 30.55 | 36.73 |

Weight % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(3)_pt1 |  |  |  | +/-4.72 | +/-6.25 |  |  |
| 60 min(3)_pt2 | +/-0.38 | +/-0.63 | +/-0.31 |  |  |  | +/-1.72 |
| 60 min(3)_pt3 | +/-0.40 | +/-0.63 | +/-0.29 |  |  |  | +/-1.80 |
| 60 min(3)_pt4 | +/-0.62 | +/-0.53 | +/-0.15 |  |  | +/-1.29 | +/-1.72 |

Normalized Wt. %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(3)_pt1 |  |  |  | 43.10 | 56.90 |  |  |
| 60 min(3)_pt2 | 8.02 | 28.83 | 10.71 |  |  |  | 52.44 |
| 60 min(3)_pt3 | 8.27 | 28.83 | 8.18 |  |  |  | 54.73 |
| 60 min(3)_pt4 | 7.33 | 20.70 | 4.69 |  |  | 30.55 | 36.73 |

Norm. Wt. % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(3)_pt1 |  |  |  | +/-4.72 | +/-6.25 |  |  |
| 60 min(3)_pt2 | +/-0.38 | +/-0.63 | +/-0.31 |  |  |  | +/-1.72 |
| 60 min(3)_pt3 | +/-0.40 | +/-0.63 | +/-0.29 |  |  |  | +/-1.80 |
| 60 min(3)_pt4 | +/-0.62 | +/-0.53 | +/-0.15 |  |  | +/-1.29 | +/-1.72 |

Atom %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(3)_pt1 |  |  |  | 44.87 | 55.13 |  |  |
| 60 min(3)_pt2 | 21.28 | 57.42 | 8.73 |  |  |  | 12.57 |
| 60 min(3)_pt3 | 22.12 | 57.92 | 6.72 |  |  |  | 13.24 |
| 60 min(3)_pt4 | 23.92 | 50.71 | 4.70 |  |  | 9.83 | 10.83 |

Atom % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 60 min(3)_pt1 |  |  |  | +/-4.91 | +/-6.06 |  |  |
| 60 min(3)_pt2 | +/-1.00 | +/-1.25 | +/-0.25 |  |  |  | +/-0.41 |
| 60 min(3)_pt3 | +/-1.07 | +/-1.28 | +/-0.24 |  |  |  | +/-0.43 |
| 60 min(3)_pt4 | +/-2.03 | +/-1.31 | +/-0.15 |  |  | +/-0.41 | +/-0.51 |

Weight %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min_pt1 |  |  |  | 52.22 | 47.78 |  |  |
| 30 min_pt2 | 7.78 | 20.94 | 2.94 | 10.12 | 10.33 | 15.11 | 32.78 |
| 30 min_pt3 | 8.21 | 24.68 | 4.46 | 6.55 | 2.42 | 18.91 | 34.77 |

Weight % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min_pt1 |  |  |  | +/-3.97 | +/-8.41 |  |  |
| 30 min_pt2 | +/-0.55 | +/-0.42 | +/-0.21 | +/-1.02 | +/-1.89 | +/-0.97 | +/-1.19 |
| 30 min_pt3 | +/-0.46 | +/-0.42 | +/-0.20 | +/-0.88 | +/-1.82 | +/-0.87 | +/-1.15 |

Normalized Wt. %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min_pt1 |  |  |  | 52.22 | 47.78 |  |  |
| 30 min_pt2 | 7.78 | 20.94 | 2.94 | 10.12 | 10.33 | 15.11 | 32.78 |
| 30 min_pt3 | 8.21 | 24.68 | 4.46 | 6.55 | 2.42 | 18.91 | 34.77 |

Norm. Wt. % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min_pt1 |  |  |  | +/-3.97 | +/-8.41 |  |  |
| 30 min_pt2 | +/-0.55 | +/-0.42 | +/-0.21 | +/-1.02 | +/-1.89 | +/-0.97 | +/-1.19 |
| 30 min_pt3 | +/-0.46 | +/-0.42 | +/-0.20 | +/-0.88 | +/-1.82 | +/-0.87 | +/-1.15 |

Atom %

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min_pt1 |  |  |  | 54.01 | 45.99 |  |  |
| 30 min_pt2 | 24.12 | 48.73 | 2.80 | 5.41 | 5.13 | 4.62 | 9.19 |
| 30 min_pt3 | 23.71 | 53.49 | 3.96 | 3.26 | 1.12 | 5.39 | 9.07 |

Atom % Error

|  | C | O | K | Ga | As | Sb | Cs |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 min_pt1 |  |  |  | +/-4.10 | +/-8.10 |  |  |
| 30 min_pt2 | +/-1.69 | +/-0.98 | +/-0.20 | +/-0.54 | +/-0.94 | +/-0.30 | +/-0.33 |
| 30 min_pt3 | +/-1.33 | +/-0.90 | +/-0.18 | +/-0.44 | +/-0.84 | +/-0.25 | +/-0.30 |

Weight %

|  | O | K | Mo | Cs |
| --- | --- | --- | --- | --- |
| 10 min_pt1 |  |  | 100.00 |  |
| 10 min_pt2 | 21.08 | 2.47 | 70.43 | 6.02 |
| 10 min_pt3 |  | 0.79 | 99.21 |  |
| 10 min_pt4 |  |  | 100.00 |  |
| 10 min_pt5 |  | 0.84 | 99.16 |  |

Weight % Error

|  | O | K | Mo | Cs |
| --- | --- | --- | --- | --- |
| 10 min_pt1 |  |  | +/-1.47 |  |
| 10 min_pt2 | +/-0.93 | +/-0.23 | +/-0.92 | +/-1.07 |
| 10 min_pt3 |  | +/-0.13 | +/-1.15 |  |
| 10 min_pt4 |  |  | +/-1.11 |  |
| 10 min_pt5 |  | +/-0.14 | +/-1.18 |  |

Normalized Wt. %

|  | O | K | Mo | Cs |
| --- | --- | --- | --- | --- |
| 10 min_pt1 |  |  | 100.00 |  |
| 10 min_pt2 | 21.08 | 2.47 | 70.43 | 6.02 |
| 10 min_pt3 |  | 0.79 | 99.21 |  |
| 10 min_pt4 |  |  | 100.00 |  |
| 10 min_pt5 |  | 0.84 | 99.16 |  |

Norm. Wt. % Error

|  | O | K | Mo | Cs |
| --- | --- | --- | --- | --- |
| 10 min_pt1 |  |  | +/-1.47 |  |
| 10 min_pt2 | +/-0.93 | +/-0.23 | +/-0.92 | +/-1.07 |
| 10 min_pt3 |  | +/-0.13 | +/-1.15 |  |
| 10 min_pt4 |  |  | +/-1.11 |  |
| 10 min_pt5 |  | +/-0.14 | +/-1.18 |  |

Atom %

|  | O | K | Mo | Cs |
| --- | --- | --- | --- | --- |
| 10 min_pt1 |  |  | 100.00 |  |
| 10 min_pt2 | 60.99 | 2.92 | 33.99 | 2.10 |
| 10 min_pt3 |  | 1.91 | 98.09 |  |
| 10 min_pt4 |  |  | 100.00 |  |
| 10 min_pt5 |  | 2.03 | 97.97 |  |

Atom % Error

|  | O | K | Mo | Cs |
| --- | --- | --- | --- | --- |
| 10 min_pt1 |  |  | +/-1.47 |  |
| 10 min_pt2 | +/-2.68 | +/-0.27 | +/-0.45 | +/-0.37 |
| 10 min_pt3 |  | +/-0.32 | +/-1.14 |  |
| 10 min_pt4 |  |  | +/-1.11 |  |
| 10 min_pt5 |  | +/-0.34 | +/-1.17 |  |

Weight %

|  | B | C | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- | --- |
| 10 min(3)_pt1 | 0.00 |  |  | 1.01 | 98.99 |  |
| 10 min(3)_pt2 |  | 10.50 | 41.50 | 6.22 | 34.10 | 7.68 |

Weight % Error

|  | B | C | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- | --- |
| 10 min(3)_pt1 | +/-0.00 |  |  | +/-0.17 | +/-1.33 |  |
| 10 min(3)_pt2 |  | +/-0.76 | +/-0.94 | +/-0.15 | +/-0.50 | +/-1.03 |

Normalized Wt. %

|  | B | C | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- | --- |
| 10 min(3)_pt1 | 0.00 |  |  | 1.01 | 98.99 |  |
| 10 min(3)_pt2 |  | 10.50 | 41.50 | 6.22 | 34.10 | 7.68 |

Norm. Wt. % Error

|  | B | C | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- | --- |
| 10 min(3)_pt1 | --- |  |  | +/-0.17 | +/-1.33 |  |
| 10 min(3)_pt2 |  | +/-0.76 | +/-0.94 | +/-0.15 | +/-0.50 | +/-1.03 |

Atom %

|  | B | C | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- | --- |
| 10 min(3)_pt1 | 0.00 |  |  | 2.43 | 97.57 |  |
| 10 min(3)_pt2 |  | 21.64 | 64.19 | 3.94 | 8.80 | 1.43 |

Atom % Error

|  | B | C | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- | --- |
| 10 min(3)_pt1 | +/-0.00 |  |  | +/-0.40 | +/-1.31 |  |
| 10 min(3)_pt2 |  | +/-1.56 | +/-1.46 | +/-0.09 | +/-0.13 | +/-0.19 |

Weight %

|  | B | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- |
| 10 min(5)_pt1 | 6.10 |  | 0.76 | 93.13 |  |
| 10 min(5)_pt2 | 10.32 |  |  | 89.68 |  |
| 10 min(5)_pt3 |  | 27.53 | 2.59 | 63.51 | 6.38 |

Weight % Error

|  | B | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- |
| 10 min(5)_pt1 | +/-2.46 |  | +/-0.15 | +/-1.23 |  |
| 10 min(5)_pt2 | +/-2.31 |  |  | +/-1.18 |  |
| 10 min(5)_pt3 |  | +/-1.11 | +/-0.14 | +/-0.93 | +/-0.48 |

Normalized Wt. %

|  | B | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- |
| 10 min(5)_pt1 | 6.10 |  | 0.76 | 93.13 |  |
| 10 min(5)_pt2 | 10.32 |  |  | 89.68 |  |
| 10 min(5)_pt3 |  | 27.53 | 2.59 | 63.51 | 6.38 |

Norm. Wt. % Error

|  | B | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- |
| 10 min(5)_pt1 | +/-2.46 |  | +/-0.15 | +/-1.23 |  |
| 10 min(5)_pt2 | +/-2.31 |  |  | +/-1.18 |  |
| 10 min(5)_pt3 |  | +/-1.11 | +/-0.14 | +/-0.93 | +/-0.48 |

Atom %

|  | B | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- |
| 10 min(5)_pt1 | 36.30 |  | 1.26 | 62.44 |  |
| 10 min(5)_pt2 | 50.52 |  |  | 49.48 |  |
| 10 min(5)_pt3 |  | 68.91 | 2.65 | 26.52 | 1.92 |

Atom % Error

|  | B | O | K | Mo | Cs |
| --- | --- | --- | --- | --- | --- |
| 10 min(5)_pt1 | +/-14.61 |  | +/-0.25 | +/-0.83 |  |
| 10 min(5)_pt2 | +/-11.33 |  |  | +/-0.65 |  |
| 10 min(5)_pt3 |  | +/-2.77 | +/-0.14 | +/-0.39 | +/-0.15 |

# Text boxes

Image Name: 90 min

Accelerating Voltage: 15.0 kV

Magnification: 1500

Image Name: 90 min

Accelerating Voltage: 15.0 kV

Magnification: 1500

Image Name: 90 min(2)

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 90 min(2)

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 90 min(2)

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 90 min(2)

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 60 min

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 60 min

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 60 min

Accelerating Voltage: 15.0 kV

Magnification: 30

Image Name: 60 min(1)

Accelerating Voltage: 15.0 kV

Magnification: 1500

Image Name: 60 min(1)

Accelerating Voltage: 15.0 kV

Magnification: 1500

Image Name: 60 min(1)

Accelerating Voltage: 15.0 kV

Magnification: 1500

Image Name: 60 min(2)

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 60 min(3)

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 60 min(3)

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 30 min

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 30 min

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 10 min

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 10 min

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 10 min

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 10 min(3)

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 10 min(5)

Accelerating Voltage: 15.0 kV

Magnification: 8000

Image Name: 10 min(5)

Accelerating Voltage: 15.0 kV

Magnification: 8000