## Slide 1: Photocathodes with 90% polarization and QE greater than 1% for DOE NP
Annual NP Accelerator R&D virtual PI Exchange meeting - November 29, 2022
Matt Poelker and M. Stutzman, Jefferson Lab
Sylvain Marsillac, ODU
Erdong Wang, BNL

## Slide 2: MBE, GSMBE, CBE and MOCVD (aka MOVPE)
MOCVD
Metal organic chemical vapor deposition (metal organic vapor phase epitaxy)
AsH3, PH3, trimethylgallium (TMGa)
Pressures >100 mbar during growth
Growth Rates 10 µm/hr
Some claim difficult to get sharp interfaces
GSMBE
Gas Source Molecular Beam Epitaxy
AsH3, PH3, elemental Gallium
CBE
Chemical Beam Epitaxy
AsH3, PH3, triethyl gallium (TEGa) or elemental Gallium
Pressure <10-4 mbar
Growth rates 0.5-1 µm/hr
MBE
Gas Source Molecular Beam Epitaxy
elemental As, P, Ga
Pressure ~10-8 mbar
Growth rates ~ 1 µm/hr
Very precise control
Molecular
beams
Molecular
and gas sources
Gas sources
Notes: The difference between the different wafer growth mechanisms vary in the sources they use for the growth. Traditionally, Molecular beam epitaxy uses solid sources for the elements, requires base pressures in the 10^-10 Torr range, and offers precise growth with sharp interfaces. Drawbacks include the vacuum requirements and the need to rotate samples during growth to ensure equal species distribution.
Gas source MBE, and chemical beam epitaxy replace some or all of the solid sources with gas sources such as arsine or phosphine, reducing the requirements for sample rotation or allowing larger wafer growth.
MOCVD is done at much higher pressures with the wafer in a viscous flow of the gas, with drawbacks that much more of the flammable, toxic precursor gasses are required and that sharp transitions are more difficult to control

## Slide 3: Background
SPIRE/Bandwidth Semiconductor used MOCVD to grow single-strained-layer GaAs/GaAsP photocathodes (good)
SVT used MBE to grow strained-superlattice GaAs/GaAsP photocathodes (better)
In this work JLab, ODU and BNL, focus on MOCVD
  Strained Superlattice photocathodes
  Strained Superlattice photocathodes with DBR
We were granted 3 months no-cost extension, project officially ends 12/31/2022

## Slide 4: Project Goals

## Slide 5: Project Conclusion
Stated clearly:
We successfully fabricated both kinds of photocathodes, SSL and SSL with DBR, via MOCVD. Exceptional work by ODU and Rochester Institute of Technology
We achieved our central goal: Polarization > 90% and QE > 1%
Between JLab and BNL, we have nearly 200k$ worth of photocathode material, our photocathode stores now replenished! Enough material for polarimeter cross checks, to support CEBAF and EIC physics programs, and to support polarized source R&D
BNL has a fully functional microMott polarimeter, and this device was essential for project success
JLab’s microMott polarimeter is very close to being operational again
The cross calibration of the two microMott polarimeters will happen
Having both source groups – JLab and BNL – participating in this project has been wonderful, a big selling point (IMHO)

## Slide 6: Budget
FY20 + FY21 loaded budget = 360k$
Support for ODU
Procurements: sample evaluation, Mott apparatus upkeep
Some labor for Matt and Marcy

## Slide 7: Making polarized electron beams with GaAs
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
3
1
1
3
s+
s -
Bulk GaAs – no strain
Maximum Polarization 50%

## Slide 8: Making polarized electron beams with GaAs
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
3
3
s+
s -
Strained GaAs
Maximum Polarization 100%

## Slide 9: Device Structure
Strained Superlattice
Strained Superlattice with Distributed Bragg Reflector
the superlattice - where the polarized electrons come from, many thin layer pairs

## Slide 10: Device Structure
Strained Superlattice
Strained Superlattice with Distributed Bragg Reflector
Highly doped surface layer to reduce surface charge limit (good for EIC)

## Slide 11: Device Structure
Strained Superlattice
Strained Superlattice with Distributed Bragg Reflector
Metamorphic grading: starting with GaAs, ending with GaAsP0.35
to create a relaxed layer upon which thick buffer layer is grown

## Slide 12: Device Structure
Strained Superlattice
Strained Superlattice with Distributed Bragg Reflector
Another complicated superlattice which forms the distributed Bragg reflector (DBR)
Etalon formed between DBR and top surface: stores light, more light absorbed, higher QE

## Slide 13: MOCVD growth parameters
Key Precursors
  Trimethyl Gallium (Ga(CH3)3)
  Arsine (AsH3) and Phosphine (PH3)
  Diethyl Zinc (Zn(CH3CH3)2)
  Carbon Tetrachloride (CCl4)
  Lower diffusivity of carbon in GaAsP should improve lifetime of device surface
Substrate: 2” GaAs wafers with either 0 or 2o offcut in the 110 direction
Growth rate range: 3-8 μm/hr
Temperature: 650-750oC
MOCVD system at Rochester Institute of Technology

## Slide 14: Issues that needed to be resolved
Sample temperature and growth rate for best metamorphic grading
Phosphorus concentration for optimum strain, and polarization
Defect mitigation
Cleave plane orientation, offcut or no offcut

## Slide 15: Tools Used
Telemetry: in-situ measurement
  Pyrometry
  Curvature
  Reflectivity
Temperature
Reflectivity
Curvature

## Slide 16: Tools Used
Nomarski Microscopy : ex-situ measurement
  Differential interference contrast (DIC) microscopy
  Surface topography
Textured photocathode, good, there’s uniform strain
GaAs0.95P0.05
minimal strain so minimal surface features
poorly relaxed growth

## Slide 17: Tools Used
X-ray Diffraction : ex-situ measurement
  Used to measure material strain and composition
  destructive and constructive interference that occurs when X-rays impinge on sample
GaAs/GaAs0.65P0.35 superlattice samples grown on different substrates:
(100) substrate, on-axis
(100) substrate, 2 degree offcut in the (110) direction

## Slide 18: Tools Used
X-ray Diffraction : ex-situ measurement
  Reciprocal phase space mapping
  Shows relaxation of deposited films, key to determining quality of the deposited metamorphic grading
Close to vertical line: more strain
3μm/hr 730oC Growth Temp
Close to diagonal line: less strain
10μm/hr 730oC Growth Temp

## Slide 19: Tools Used
Transmission Electron Microscopy : ex-situ measurement
  TEM micrographs (Images)
  Selected Area Electron Diffraction (SAED)
  Energy Dispersive X-Ray Spectroscopy (EDS)

## Slide 20: Tools Used
Ellipsometry (optical method, layer thickness)
Photoluminescence (PL) mapping (uniformity)
Hall Effect (measure dopant concentration)
Atomic Force Microscopy (surface defects)

## Slide 21: Old Dominion University, Ben Belfore’s first photocathode SSL
Pol ~ 70%
QE ~ 0.3%
lpeak ~ 820 nm
BNL microMott, measurements by Wei Liu

## Slide 22: ODU, Ben’s second photocathode SSL
Pol ~ 80%
QE ~ 0.4%
lpeak ~ 785 nm
BNL microMott, measurements by Wei Liu

## Slide 23: ODU, Ben’s third photocathode, SSL with DBR
Pol ~ 83%
QE ~ 3%
lpeak ~ 785 nm
BNL microMott, measurements by Wei Liu

## Slide 24: ODU, Ben’s fourth photocathode, SSL with DBR
Pol ~ 83%
QE ~ 1.3%
lpeak ~ 775 nm
BNL microMott, measurements by Wei Liu

## Slide 25: Old Dominion University, Adam Masters’ first photocathode, SSL with DBR
Pol ~ 90%
QE ~ 1%
lpeak ~ 785 nm
BNL microMott, measurements by Wei Liu

## Slide 26: Adam’s first photocathode, SSL with DBR
Pol ~ 92%
QE ~ 2.3%
lpeak ~ 785 nm
BNL microMott, measurements by Wei Liu

## Slide 27: ‘microMott’ ‘retarding field’ low voltage polarimeters
BNL
JLab

## Slide 28: Conclusion
Multiple devices grown - superlattice and superlattice samples with distributed Bragg reflector
Successful interaction with “service providers”: North Carolina State University and Rochester Institute of Technology
Problems solved in timely manner: successful doping and compositional calibration of all layers, viable and reliable growth recipes identified
MOCVD is definitively a reliable method for fabricating high polarization photocathodes with good QE
Future Work: arsenic cap layer, hydrogen cleaning, higher polarization and higher QE

## Slide 29: Project Conclusion
Stated clearly:
We successfully fabricated both kinds of photocathodes, SSL and SSL with DBR, via MOCVD. Exceptional work by ODU and Rochester Institute of Technology
We achieved our central goal: Polarization > 90% and QE > 1%
Between JLab and BNL, we have nearly 200k$ worth of photocathode material, our photocathode stores now replenished! Enough material for polarimeter cross checks, to support CEBAF and EIC physics programs, and to support polarized source R&D
BNL has a fully functional microMott polarimeter, and this device was essential for project success
JLab’s microMott polarimeter is very close to being operational again
The cross calibration of the two microMott polarimeters will happen
Having both source groups – JLab and BNL – participating in this project has been wonderful, a big selling point (IMHO)

## Slide 30: Back up slides

## Slide 31: Measurements made at BNL

## Slide 32: MOCVD: Photocathode progress
Dr. Sylvain Marsillac, Old Dominion University
Virginia Center for Photovoltaics
Ben Belfore ODU Graduate Student
The Rochester Institute of Technology III-V EPICenter

## Slide 33: Results: Metamorphic Grading
High-quality strain relaxation of underlying layers is key to getting intended GaAs strain in the emitting region
Necessary because of growing on lattice mismatched substrate
RSM used to characterize extent of relaxation in metamorphic layers
Key parameters changed:
  Growth Rate
  Growth Temperature
  Arsine/Phosphine Ratio

## Slide 34: Results: Metamorphic Grading
Slower Growth Rate resulted in highest strained films (left)
High Temperature with smaller composition change between steps is more promising (right)
3μm/hr 730oC Growth Temp
10μm/hr 650oC lower phosphorous grade

## Slide 35: Results: MOCVD
Graded GaAs to GaAsPx layer growth: Strain in GaAsPx varies with substrate temperature
100 um
Higher temperatures yielded improved surface with moderate relaxation throughout
730°C growth temperature
GaAs
GaAs(0.74)P(0.26)
Optimizing temperatures,
graded layer profile

## Slide 36: Results: Device Continued
Surface quality initially poor but subsequent runs improved surface quality
Refining runs to improve relaxation
Surface completely matted, RSM not performed
3μm/hr 730oC Growth Temp
10μm/hr 650oC Growth Temp
10μm/hr 730oC Growth Temp
PL Map taken on this sample

## Slide 37: MOCVD monitoring: graded layer optimization
Ends at ~34.4 % P
(100) 2° <110>
~10 µm/hr graded layer growth rate
V/III: 20-25
730°C growth temperature
Average ΔP = 4.95%
Higher temperature and higher ΔP steps begins well, levels out to 30% relaxation, and surface degrades during thick 35% buffer

## Slide 38: Making polarized electron beams with GaAs
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
3
1
1
3
s+
s -
Bulk GaAs – no strain
Maximum Polarization 50%
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
3
3
s+
s -
Strained GaAs
Maximum Polarization 100%