## Slide 1: Environmental Applications and first Results from UITF
J. Vennekate

## Slide 2: Outline
Motivation for Environmental Applications of Accelerators
Role of SRF in the Field
Nb3Sn & Cryocoolers
Ongoing R&D Projects at JLab
Irradiation Beamline at UITF
  1st Results

## Slide 3: Motivation
“Environmental Applications for Accelerators”?
environmental remediation techniques which utilize electron beam
main mechanism generation of free radicals in gas/water
flue gas treatment
wastewater treatment
oxidizing
reducing

## Slide 4: Example facilities for Wastewater Treatment
Hangzhou & Chengdu coal power plants in China
  300,000 Nm3/h
  two 800 keV, 320 kW accelerators
  started 1997
Deagu dyeing treatment plant in South Korea
  10,000 m3/h
  1 MeV, 400 kW accelerator
  started 2006
Guanhua Knitting Factory industrial wastewater in China
  30,000 m3/h
  total of 7 accelerators
  started 2020

## Slide 5: Accelerator R&D – Role of SRF
many facilities but irradiation part compact integration in larger facilities
CapEx often driver normal conducting technology
NC vs. SRF
like lightbulb vs LED
SRF solutions gain in advantage at higher beam energy and power 1 MeV, 1 MW
However, maintain compactness!
less efficient but cheap & simple
very efficient but more complex
Cryoplant?

## Slide 6: Recent developments – Key Technology
Nb3Sn
enhance SC capabilities of Nb
102 more efficient @ 4 K
vapor diffusion on bulk Nb
enables cond. cool. operation
develop new coating methods
Cryocoolers
“dry” cryogens
“plug & play” with helium compressor
          significant progress over last 10 years
          now off the shelf as commercial product 2 W @ 4 K (6.5 kW)

## Slide 7: Technology Projects at the Lab I
development and analysis of compact 1 MeV accelerator (2018)
CC single cell prototypes
952 MHz cavity in horizontal cryostat (Ciovati Stewardship)
RF source development magnetron design
2.45 GHz and now 915 MHz target 1 MW (Rimmer & Wang Stewardship)

## Slide 8: Technology Projects at the Lab II
advancement to multi-cell cavity design 10 MeV (Vennekate Stewardship)
novel target/beam exit interfaces UITF as testbed (Subaward ODU)
2.45 GHz multicell prototype
use magnetron for compact low power accelerator

## Slide 9: Irradiation at the UITF I
LDRD project & collaboration with
testbed for irradiation studies – up to 10 MeV, 100 nA (max. 150 nA)
We want/need more!
dose accumulates control irradiation time 0.5 - 20 kGy 1 - 40 min
built a new beamline

## Slide 10: Irradiation at the UITF II
target rail
target container with ~ 60 mL water opti-chromic rods to verify dose

## Slide 11: What is we are “shooting” at?
1,4-dioxane
used as a solvent/solvent stabilizer
ubiquitous in commonly used products such as detergents
often observed in landfill leachate
EPA classification as “probable human carcinogen”
first regulations for drinking water in NY, CA …
resistant to naturally occurring biodegradation processes
removed through hydroxyl radical (*OH) oxidation (non-reactive with ozone)
ebeam irradiation
oxidizing
reducing

## Slide 12: Preliminary Results
different water samples
  DI water (spiked)
  secondary effluent (spiked)
  unspiked water
  GAC, …
first results show significant reduction at ~1 - 2 kGy (96 %)
we also irradiated PFAS …
Stay tuned!
preliminary

## Slide 13: Questions?
J. Vennekate
hannesv@jlab.org
Motivation for Environmental Applications of Accelerators
Role of SRF in the Field
Nb3Sn & Cryocoolers
Ongoing R&D Projects at JLab
Irradiation Beamline at UITF
  1st Results
Many thanks to GA, HRSD, ODU, the UITF team and the SRF R&D department!