## Slide 1: Test of W Foils with 3.5 MeV e‒ Beam at MAMI
Andriy Ushakov
Ce+BAF Design Group Meeting
January 11, 2023

## Slide 2: Target Material Tests at MAMI (3.5 MeV or 180 MeV e‒ Beam)
Radiation damage test of target materials at elevated average temperature 0.215 dpa at 300 °C for tungsten
Fatigue test at expected for JLab e+ injector cycling temperatures Tave ≈ 300 °C and ΔT = 125 °C
MESA
accelerator
& experiments
50 µA @ 3.5 MeV 50 µm RMS
22 µA @ 180 MeV 250 µm RMS

## Slide 3: 180 MeV e‒ Beam and W Target
Thickness of W target: 100 μm
Length of W target: 80 mm
Width of W target: 3 mm
Thickness of Al2O3 ceramic: 1 mm
Beam
W
Al2O3
3D View of ¼ of Target
Al
Temperature, Radiation and Convection
22 μA @ 180 MeV e- beam with 250 μm RMS spot size on target

## Slide 4: 180 MeV e‒ : Heat Power and Target T for Duty Cycles of 0.17
Average P = 25.9 W/mm3
Average Temperature
Ppulse = 152 W/mm3
ΔT = 125 °C
Cycling Temperature for Pulse Length = 34 ms, Pulse Period = 200 ms
Tave = 302 °C

## Slide 5: 180 MeV e‒ Beam: Peak Equivalent Stress (W: 0.1mm x 3mm x 80mm) Pulse Length = 34 ms and Pulse Period = 200 ms
Max σvM (400 °C) = 118 MPa ( Fatigue Strength)

## Slide 6: Radiation Damage by 22 μA @ 180 MeV e‒ Beam with 250 μm RMS Spot Size
Rad. Damage of Tungsten = 1.96E-20 dpa/e-
22 μA → 1.375E+14 e-/s
For cw e- beam
To reach the damage of 0.215 dpa in W:
• 8E+4 seconds of irradiation is needed (22.2 h).
• = 619 °C in W foil (0.1 mm x 10 mm x 80 mm)
Tungsten
Material | Displacement Threshold Energy [eV] | Rad. Damage [dpa/e-]
Ta | 90 | 1.94E-20
W | 90 | 1.96E-20
Re | 60 | 3.37E-20
Cu | 30 | 
W40Cu |  | 5.27E-20

## Slide 7
# | Thickness [μm] | Length x Width | Pulse Length [ms] | Pulse Period [ms] | Tave [°C] | ΔTpulse [°C] | Rad. Damage [dpa] | Number of cycles | Irradiation Time [h] | Total Charge [C]
1 | 100μm | 80mm x 10mm | cw |  | 619 |  | 0.215 | - | 22.16 | 1.75
2 | 100μm | 80mm x 3mm | 34 | 200 | 302 | 125 | 0.001 | 104 | 0.556 | 0.01
Ʃ |  |  |  |  |  |  |  |  | 22.72 | 1.76
# | Thickness [μm] | Length x Width | Pulse Length [ms] | Pulse Period [ms] | Tave [°C] | ΔTpulse [°C] | Rad. Damage [dpa] | Number of cycles | Irradiation Time [h] | Total Charge [C]
1 | 100μm | 80mm x 10mm | cw |  | 619 |  | 0.215 | - | 22.16 | 1.75
2 | 100μm | 80mm x 3mm | 34 | 200 | 302 | 125 | 0.001 | 104 | 0.556 | 
Ʃ |  |  |  |  |  |  |  |  | 22.72 | 1.76
Target #1: test of radiation damage
Target #2: test 10k thermal cycles with expected temperatures at JLab e+ target
Options for Test of W Targets at 180 MeV

## Slide 8: 3.5 MeV e‒ Beam and W Target
Thickness of W target: 100 μm
Length of W target: 80 mm
Width of W target: 3 mm
Beam
W
Al2O3
3D View of ¼ of Target
Al
50 μA @ 3.5 MeV e‒ beam with 50 μm RMS spot size on target
Peak Deposited Power = 8.38 kW/mm3 vs 152 W/mm3 at 180 MeV

## Slide 9: 3.5 MeV e‒ Beam: Heat Power and Target T for Duty Cycles of 0.055
Average P = 461 W/mm3
Cycling Temperature for Pulse Length = 0.15 ms, Pulse Period = 2.73 ms
ΔT ≈ 140 °C
Tave ≈ 300 °C
Average Temperature
Pulse length = 0.15 ms vs 34 ms at 180 MeV
Pulse length is too short

## Slide 10
How pulse length can be increased
keeping
300 °C average temperature (1)
and
120 °C temperature rise per pulse (2)?
Reduce heat path: reduce length of W foil to (0.1 mm x 3 mm x) 42 mm
  Target holder for 42 mm target length was used in the past
Reduce heat density: increase RMS beam size to 100 µm

## Slide 11: W Target 3.5 MeV e‒ Beam with Duty Cycle of 0.107
Thickness of W target: 100 μm
Length of W target: 42 mm
Width of W target: 3 mm
50 μA @ 3.5 MeV e‒ beam with 100 μm RMS spot size on target
Average Power
Average Temperature

## Slide 12: 3.5 MeV e‒ Beam: Heat Power and Thermal Cycle
Pulse Period = 3.74 ms
Pulse Length = 0.4 ms
Deposited Power = 2.18 kW/mm3

## Slide 13: Radiation Damage by 50 μA @ 3.5 MeV e‒ Beam with 50 μm RMS Spot Size
Rad. Damage = 1.02E-19 dpa/e-
vs 1.96E-20 dpa/e- at 180 MeV
50 μA 3.125E+14 e-/s
For cw e- beam
To reach the damage of 0.215 dpa in W:
• 3916 s of irradiation is needed = 1.9 h vs 22.2 h @ 180 MeV
• = ?

## Slide 14: Required Irradiation Time and Maximal Average Temperature for CW and Pulsed 3.5 MeV e‒ Beam with 50 μm RMS Spot Size to reach 0.23 dpa in W target (0.1mm x 10mm x 42mm)

## Slide 15: Summary
Beam focusing system at 3.5 MeV allows to reduce RMS beam size down to 50 µm
Beam current of 50 µA was used in the past. Beam is stable if pulse length is not too short
No activation and long cooling time
Easier to get beam time, lower costs
Targets are in vacuum, no uncertainty connected with cooling by air.
Beam size can be measured precisely
Many millions thermal cycles can be tested: 10M cycles with 0.4 ms pulse length and 3.74 ms pulse period will require 10.4 h irradiation time
Radiation damage in wide temperature range can be tested: 0.23 dpa @ 300 °C will require 9.1 h beam time