## Slide 2
We don’t run beam from the electrostatic center of the cathode/anode
Laser
IN
Electrons
OUT
Ions create QE trough to electrostatic center
Laser spot diameter <1 mm can be moved to different locations on the photocathode (5mm)
Pragmatically Avoiding the “EC”
Here, QE ion damage forms QE trough from four spots to EC.
Gas

## Slide 3
Laser Profile
Photocathode QE
Beam Profile

## Slide 4: Improving Lifetime with Larger Laser Size
J. Grames, et al., Phys. Rev. ST Accel. Beams 14 043501 (2011)
GaAs @ 532nm

## Slide 5: Generation of ions
Most ions created at low energy
Most ions created close to GaAs surface
Beam Current: 2.0 mA
Vacuum: 8.0 × 10-12 Torr

## Slide 6
Low energy ion column for 100 kV gun
Low energy ion column for 200 kV gun
Ion energy
At 200 kV, only 60% of ions are created compared to 100 kV, longer lifetime

## Slide 7
Varying beam voltage
Best vacuum
Electric Fields
Laser Profile
QE Surface
Fixed beam voltage
Good vacuum
Electric & Magnetic Fields
Ion collectors or filters
Beam loss and radiation

## Slide 8
QE x Laser Profiles
=>
Initial
Distribution
Initial Distribution
x Gun + Beamline
=>
Beam Tracking
Ions x Beam x Beamline
=>
Ion Motion
Ion Motion x Gun
=>
Ion Impact Photocathode
Beam Tracking
x Electron Impact Ionization
=>
Ion Generation
Ion Impact x Sputter/Implant
=>
QE modification