## Slide 1: Inverted insulator photoelectron guns at Jefferson Lab
P. Adderley, J. Benesch, B. Bullard, J. Grames, F. Hannon, J. Hansknecht, C. Hernandez-Garcia, R. Kazimi, G. Krafft, M. A. Mamun, M. Poelker, R. Suleiman, M. Tiefenback and S. Zhang
Graduate Students: G. Palacios, Y. Wang, S. Wijiethunga, J. Yoskovitz
Accelerator Seminar, TRIUMF, Vancouver, BC, 21 November 2017

## Slide 2: Outline
Past and present: Polarized electron beam sources at JLab for the high energy nuclear physics program and the high current un-polarized beam for the Free Electron Laser
The way future: Magnetized electron beam generation R&D for high energy electron coolers
The dream: Inverted Insulator electron guns:
  The concept
  The never ending bumpy road to the Super (reliable) Ultra (high vacuum and low emittance) Mega (volts/meter) electron gun
Reality:
  High voltage performance
  Beam production at mA level
  …and ions!

## Slide 3: Key Features of a Polarized Photogun
Photocathode
  High Polarization
  High QE (photoemission yield)
  Long Lifetime at mA level
High Voltage
  No field emission
  Reliable, NO ARCING allowed!
Vacuum
Drive Laser
Notes: Interior Page Design 2

## Slide 4
Polarized electron beam at CEBAF
The endless (?) quest for perfection
1
2
3
4
Lifetime increased from 10s to 100s of Coulombs
Notes: Interior Page Design 1

## Slide 5
Load Lock & Cathode Prep chamber
CEBAF Injector Inverted insulator Gun 130 kV DC
130kV Gun
R28 cable from HVPS to inverted insulator gun
Present configuration
> electron beam to accelerator

## Slide 6
6
Polarized Source Operation Highlights
Photocathode
  Strained Superlattice GaAs/GaAsP photocathode
  Good Polarization 85-87% (measured at Mott)
  Good QE > 1% after activation
Last Spring 2017
  Delivered 20-40 uA to 3 halls at a time (249.5 & 499 MHz)
This Fall 2017 – Winter 2018
  CEBAF restoration starts late November
  12 weeks of running scheduled
  Start simultaneous 4-Hall Operation

## Slide 7: Lifetime Studies at mA Beam Current
Polarized positrons for CEBAF, and on-going discussions with BNL related to high current eRHIC EIC, prompted experiments at CEBAF to characterize lifetime vs. laser spot size using high-polarization photocathodes
CEBAF 130kV polarized “inverted gun” with load lock
Make beam here
Deliver it here
Vary the laser beam size
Monitor vacuum and radiation
1mA
Required laser power, slope proportional to QE decay
Increasing laser size reduces QE decay proportionally
Note:
1 mA 86 C/day
5 mA 432 C/day
10 mA 860 C/day
50 mA 4320 C/day

## Slide 8: Improving Lifetime with Larger Laser Size
J. Grames, et al, Phys. Rev. ST Accel. Beams 14 043501 (2011)
GaAs @ 532nm

## Slide 9: First Results: GaAs/GaAsP at mA Current
  CEBAF charge lifetime improves with spot size, as expected, but eventually beam size becomes “too large”
  Laser diameters greater than ~4 mm (4 sigma) will require properly designed cathode/anode electrodes, to ensure 100% transmission, to maintain excellent vacuum, to minimize ion bombardment
We operate left of this line

## Slide 10
The JLab IR Free Electron Laser (FEL) holds the world’s average power record (2006) @ 14 kW (l=1.06 mm) 8.5 mA CW un-polarized electron beam
in (2005)

## Slide 11: The DC gun consists of electrodes that hold the photocathode inside a vacuum chamber. The electrodes are electrically isolated by ceramic insulators. This design (2005) is an evolution of the 1997 original*
Electrodes
Vacuum chamber
Ceramic insulators
Corona shield
High voltage feed
NEG pumps
RGA, extractor gauge
and leak valve
Photocathode
Photocathode retractor mechanism
33 inches
This is a vent-bake e-gun
*D. Engwall, et al., 1997 Particle Accelerator Conference, Vancouver, B.C. Canada, 2693, (1997). IEEE, Piscataway, NJ, (1998)

## Slide 12: The FEL gun delivered over 7000 Coulombs and over 900 hours of beam time at 1-8.5 mA CW with a single GaAs wafer, with 1/e lifetime of 550C at 5 mA CW.
GaAs wafer 25 mm dia
Active area 16 mm dia
Drive laser 8 mm dia

## Slide 13: Making magnetized e-beam for JLEIC High Energy Electron Cooler R&D
High Energy Electron Cooler
ion beam
cooling solenoid (B>0)
Magnetization flip
cooling solenoid (B<0)
injector
beam dump
linac
fast extraction kicker
fast injection kicker
dechirper
rechirper
circulating bunches
extracted bunches
injected bunches
exchange
septum
vertical
bend
into ERL
vertical
bend
to CCR
ion beam
Circulator Cooler Ring
ERL Ring

## Slide 14: Magnetized Bunched-Beam Electron Cooling
Upon exit of Cathode Solenoid
Upon entering Cooling Solenoid
Electrons born in strong uniform Bz
V
B
V
B
B
V
B
V
Ion beam cooling in presence of magnetic field is much more efficient than cooling in a drift (no magnetic field):
Long cooling solenoid provides desired cooling effect:

## Slide 15: Electron beam suffers an azimuthal kick at entrance of cooling solenoid.
But this kick can be cancelled by an earlier kick at exit of photogun.
That is the purpose of cathode solenoid
Learned that gun solenoid can influence field emission
First trials with gun at high voltage and solenoid ON resulted in new field emission and vacuum activity
But we developed a procedure to energize solenoid without exciting new field emitters
Chart: z, m

## Slide 16: But putting the electron beam into the cooling solenoid represents a challenge!
Bunch length | 60 ps (2 cm)
Repetition rate | 43.3 MHz
Bunch charge | 2.0 nC
Peak current | 33.3 A
Average current | 86.6 mA
Transverse normalized emittance | <19 microns
Cathode spot radius – Flat-top () | 3.14 mm
Solenoid field at cathode (Bz) | 0.5 kG
Bunch length | 60 ps (2 cm)
Repetition rate | 43.3 MHz
Bunch charge | 2.0 nC
Peak current | 33.3 A
Average current | 86.6 mA
Transverse normalized emittance | <19 microns
 | 3.14 mm
Solenoid field at cathode (Bz) | 0.5 kG
Cornell University demonstrated 65 mA and 2 nC, but not at same time, and non-magnetized
Fermilab Magnetized Photoinjector Laboratory:
Pulsed NCRF gun with Cs2Te photocathode and UV laser (λ=263 nm)
Bunch charge: 0.5 nC and bunch length: 3 ps
0.5% duty factor (average current: 7.5 μA)
  Bunch frequency: 3 MHz
  Macropulse duration: 1 ms
  Number of bunches per macropulse: 3000
  Macropulse frequency: 5 Hz

## Slide 17: Taking on the challenge: magnetized Beam in JLab’s Gun Test Stand
Beamline
Gun Solenoid
Photocathode
Preparation
Chamber
Gun HV Chamber
Slit
Viewer Screen
Shield Tube
Viewer 3 Screen
Beam Dump
Use slit and viewscreens to measure mechanical angular momentum:
: solenoid field at photocathode
: laser rms size
φ: rotation (sheering) angle

## Slide 18: Slit and Viewscreen Measurement
0 G at photocathode
1511 G at photocathode
Beamlet observed on downstream viewer

## Slide 19: The Gun Test Stand with 300 kV Inverted Gun and CsK2Sb Photocathode
Slide 19
19
Learning how to use the new photocathode

## Slide 20: Photocathode Preparation Chamber
K2CsSb grown with a mask – limit photocathode active area (3 mm diameter) to reduce beam halo, minimize vacuum excursions and high voltage arcing, prolong photogun operating lifetime
Active area can be offset from electrostatic center
5 mm active area available, Entire photocathode can be activated too
Consistently growing photocathodes with 5-7% QE

## Slide 21: Glassman gas insulated HVPS connected to the inverted insulator gun using epoxy receptacles and 350kV to R30 cable plugs
500kV 5 mA DC HVPS, SF6 at 10 psi
350kV plug, epoxy receptacle in SF6
R30 plug into gun ceramic
R30 inverted ceramic & electrode
Notes: Interior Page Design 2

## Slide 22: Thanks to Naimat Khan at TRIUMF: 350kV plug and epoxy receptacle from Dielectric Sciences
R30
R28

## Slide 23: Inverted Insulator Photoguns
CEBAF 130 kV, used since 2010
350 kV gun for GTS and UITF
Longer “R30” insulator
Spherical electrode
R30
R28

## Slide 24: Building the 350 kV Gun
C. Hernandez-Garcia, M. Poelker, and J. Hansknecht, “High Voltage Studies of Inverted-geometry Ceramic Insulators for a 350kV dc Polarized Electron Gun,” IEEE Transactions on Dielectrics and Electrical Insulation, Vol. 23, No. 1; February 2016
Start with “dummy” electrode (no photocathode) and test different insulators and cathode screening electrodes
R30
R28
R30
R30

## Slide 25: The Reality of HV Breakdown
The first test with R30 pure alumina ceramic suffered breakdown at ~315kV with subsequent puncture at 330kV.
A second test with a new R30 pure alumina suffered breakdown at ~315 kV.
* M. BastaniNejad, A. A. Elmustafa, E. Forman, J. Clark, S. Covert, J. Grames, J. Hansknecht, C. Hernandez-Garcia, M. Poelker and R. Suleiman, “Improving the performance of stainless-steel DC high voltage photoelectron gun cathode electrodes via gas conditioning with helium or krypton,” Nucl. Instr. and Meth. in Phys. Res. A, Vol. 762, pp. 135–141, 2014
Field emission managed via krypton-processing*, i.e., voltage was applied with ~10-5 Torr krypton added to gun chamber

## Slide 26: Careful design of triple-junction-shield
Gradients shown for 350 kV
Simulationsby Y. Wang
Ceramic
HV plug
Design overall shape for low gradient here !!

## Slide 27: Optimizing the Electrode Design
Pure alumina insulator replaced with doped alumina (charge drainage) for higher voltage stand-off and robust operations
Electrode ‘shed’ (triple junction shield) re-designed to lower gradient from 12 MV/m to 10 MV/m at 350kV
Pure alumina insulator
Doped alumina insulator

## Slide 28: Inverted-Insulator Photoguns
with optimized triple point shields and mildly conductive insulators
Both designs, maximum field strength < 10 MV/m
Insulator
NEG array
36 cm
Electron beam
MV/m
at 350kV
COMSOL simulation done at 350kV by student G. Palacios
Notes: Interior Page Design 2

## Slide 29: Ideal electrode geometries become Hand-Polishing Nightmare!
New CEBAF 200 kV Gun

## Slide 30: Centrifugal Barrel Polishing to Rescue
Months to hours !!!
  From machine shop
30 min. plastic cones
30 min. crushed corncob
  Barrel polishing machine at JLab SRF

## Slide 31: Barrel polished electrodes…
Gun electrodes traditionally polished using sand paper and diamond paste
Tedious process, takes about 30 days to complete
Now performed in 1 day using SRF barrel polishing machine
  From machine shop
30 minutes in plastic cones
30 minutes with corncob
C. Hernandez-Garcia, D. Bullard, F. Hannon, Y. Wang, and M. Poelker, “High voltage performance of a dc photoemission electron gun with centrifugal barrel-polished electrodes,” Rev. Sci. Instrum, 88, 093303 (2017)

## Slide 32: Excellent Surface Finish
Diamond paste polishing Ra 30 nm*
* M. BastaniNejad, A. A. Elmustafa, E. Forman, S. Covert, J. Hansknecht, C. Hernandez-Garcia, M. Poelker, L. Das, M. Kelley, P. Williams, “Evaluation of electropolished stainless steel electrodes for use in DC high voltage photoelectron guns,” J. Vac. Sci. Technol. A, Vol. 33, No. 4, Jul/Aug 2015
similar to traditional hand polishing with sand paper and diamond grit

## Slide 33: The ultimate metric of success: High Voltage!
Reached
360 kV in 70 hours
Vacuum and radiation levels indistinguishable from bkgd at 350kV
10 MV/m at 350 kV

## Slide 34: We now have 3 photoguns with barrel polished electrodes
CEBAF 200 kV
Conditioned to 216 kV,
No FE at 200kV, ready for installation
UITF 350 kV
Under assembly
GTS 350 kV
In operation since Nov. 2016 with CsK2Sb photocathode:
4.5 mA beam! Magnetized AND non-magnetized

## Slide 35: 7 hour run at 4.5 mA Magnetized Beam
Delivered 4.5 mA DC magnetized beam for ~7 h, low QE lifetime.
Investigating charge lifetime factors from twenty two 1-hour long runs of 3-4.5 mA beams at 200-300 kV gun HV, and 0-400 A gun solenoid current conditions
Investigating the efficacy and necessity of installed dc ion-clearing electrodes to stop ions in beamline from reaching gun and causing HV arcs
1.5 KGauss @ cathode
8% QE
Only 165 Coulomb 1/e QE lifetime

## Slide 36: With cathode solenoid off, we observe cathode arcing!
4.5mA
Non-magnetized beam current
Active area, CsKSb
mA BEAM!
Cathode damage
Damaged
Active area
Sudden QE drop due to photo-cathode arcing
Sb
GaAs
Ta
Mo
puck
Damaged
Electrostatic center

## Slide 37: No cathode arcing with gun solenoid energized
150 A
3 mA
4% QE
200 A
250 A
300 A
400 A
Cathode solenoid current
Anode current
Anode current and ‘noise’ amplitude decrease as gun solenoid strength is increased

## Slide 38: PRELIMINARY secondary ion mobility study
Check the ion mobility
See if the ions generated outside the extraction can comeback even with solenoids running
Generate H2 ions at least 1 m away from the cathode
Work by:
Cristhian Valerio
Universidad Autonoma de Sinaloa, Mexico

## Slide 39: Secondary electrons in the cathode strike the anode
Yellow line: secondary electrons emitted from cathode.
RED LINE: Secondary ions returning to cathode
0 A
400 A
But magnetic field from solenoid focuses secondary electrons, allowing them to go through the anode.
Ions strike the cathode with high density when solenoid is off
Ion density at the cathode decreases when solenoid is energized
SimIon simulations by Cristhian Valerio

## Slide 40: Finally:500kV Inverted insulator gun…using a cable?
F. E. Hannon, P. Evtishenko, and C. Hernandez-Garcia, “Electrostatic modeling of the Jefferson Laboratory Inverted Ceramic Gun”, Proceedings of the International Particle Accelerator Conference 2010
R30
R28
“350”

## Slide 41: Summary
Jlab has over 20 years experience designing, building and operating 100-350kV DC photo-guns for production of polarized and un-polarized electron beams at mA CW
Demonstrated 4.5 mA magnetized and un-magnetized DC beam for extended periods of time, but cathode arcing needs to be understood and resolved.
K2CsSb Photocathode Preparation Chamber, Gun, Solenoid and Beamline are all operational
Photogun operates reliably at 300 kV with cathode solenoid
Have successfully magnetized electron beam and measured rotation angle, reasonable agreement between measured and predicted but refining the simulation with GPT (3d)
Preparing to install a gain-switched drive laser, to generate mA magnetized beam with RF structure
Then switch to 32 mA 225 kV HV power supply….
…exploring tests for 500kV DC gun using high voltage cable!

## Slide 42: Thanks to all those whom have done all the work
P. Adderley, J. Benesch, B. Bullard, J. Grames, F. Hannon, J. Hansknecht, M. Poelker, M. A. Mamun, R. Suleiman, M. Stutzman, G. Palacios, Y. Wang, S. Wijiethunga, J. Yoskovitz, S. Zhang, C. Valerio*
ODU Graduate Students, Postdoc
*Collaborator at U. of Sinaloa, Mexico
Including the ~70 people team of technicians and engineers that make the Gun Test Stand possible

## Slide 43: Backup Slides

## Slide 44: High Polarization Photocathodes
30 mA/W
Bulk GaAs
1 mA/W
100 nm
Strained GaAs
Strained Superlattice GaAs/GaAsP
6 mA/W
100 nm
14 Layers
Photocathode capability (polarization and QE) has grown significantly.
Pe- 35% 35% 75% 75% 85% 89%
Ie- 30mA 100mA 50mA 100mA 150mA 200mA
1995 1998 1999 2000 2004 2017
with DBR
30 mA/W
Testing at
CEBAF now

## Slide 45: Charge Lifetime of High Current Beam
Chart: Average QE, %
| 5.715676069259496 | 5.825312852859493 | 5.3284289836885 | 5.188527345657496 | 5.045150279998493 | 4.804235696792496 | 4.901609659195 | 5.124999999999995
3 mA | 1085 | 10000 | 377 | 2583 | 512 | 343 | 5000 | 162
4 mA | 183 | 214 | 309 | 167 | 195
4.5 mA | 275 | 210 | 143 | 294 | 164
Chart: Illumination Power, mW
| 122.3386545751785 | 120.0361487808348 | 131.2296968658689 | 134.7681285492275 | 138.5980756753513 | 145.5482545886744 | 142.65683498257 | 136.4386576196589
3 mA | 1085 | 10000 | 377 | 2583 | 512 | 343 | 5000 | 162
4 mA | 183 | 214 | 309 | 167 | 195
4.5 mA | 275 | 210 | 143 | 294 | 164
Chart: Solenoid=300 A
| 3.0 | 4.0 | 4.5
200 kV | 512 | 183 | 210
300 kV | 2583 | 214 | 143
Same laser spot size (0.38 mm rms)
  better lifetime at lower beam current
  Increased lifetime with lower incident laser power
With HV OFF: No QE drop from 22 h illumination at 0.8 W (required for 4.5 mA runs), even at 2 W for 2 h.
Laser spot size↑ and QE↑ ═ LT↑

## Slide 46: Charge Lifetime of High Current Beam
Chart: Gun HV=300 kV
| 0.0 | 200.0 | 300.0 | 400.0
3 mA | 1085 | 162 | 2583 | 343
4 mA | 195 | 167 | 214 | 309
4.5 mA | 294 | 143 | 275
Chart: Run Sequence
| 4.0 | 5.0 | 2.0 | 8.0 | 7.0 | 9.0 | 6.0 | 3.0
3 mA | 1085 | 10000 | 377 | 2583 | 512 | 343 | 5000 | 162
4 mA | 183 | 214 | 309 | 167 | 195
4.5 mA | 275 | 210 | 143 | 294
Chart: Beam Current=3 mA
| 200.0 | 250.0 | 300.0
0 A | 10000 | 10000 | 1085
200 A | 377 | 162
300 A | 512 | 2583
400 A | 343
No apparent Lifetime dependency on gun HV, magnetization effect, or run sequence
Only 3 incidents of QE drop due to arcing, and this happened only with non-magnetized beam
Strong focusing of gun solenoid might help keep ions away from e-beam

## Slide 47: Measuring Electron Beam Magnetization
Use slit and viewscreens to measure mechanical angular momentum:
: solenoid field at photocathode
: laser rms size
φ: rotation (sheering) angle

## Slide 48: New Steel Photocathode Holders
New steel holders (pucks) to enhance field to 2.0 kG at photocathode. Two types:
  Molybdenum and carbon steel hybrid puck
  Carbon steel puck
Molybdenum
Steel
Steel

## Slide 49: Classic voltage induced gas desorption
With every 1 kV increase, gas (mainly Hydrogen) is released from the chamber walls and accelerated by the potential towards the electrode. Upon impact, secondary electrons are released and accelerated to the chamber walls, releasing more gas. The process acts as a plasma, inducing pressure rise and x-rays detected by Geiger-Muller tubes. Since pumping is provided by NEG modules, the cascade process decays in a few minutes.

## Slide 50: The # of secondary electrons striking the anode decreases with solenoid strength
200 A
400 A
The anode register a negative current during operation
It decrease as the big solenoid increase its strength

## Slide 51: Secondary electrons in the cathode
Shifting the beam from the center helps to spread the ion back bombardment in the cathode

## Slide 52: Cathode ion Back bombardment
Beam shift 2mm
Beam center
Solenoid on

## Slide 53: Anode current in the anode
Chart: Anode current
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0 | 9.0 | 10.0 | 11.0 | 12.0 | 13.0 | 14.0 | 15.0 | 16.0 | 17.0 | 18.0 | 19.0 | 20.0 | 21.0 | 22.0 | 23.0 | 24.0 | 25.0 | 26.0 | 27.0 | 28.0 | 29.0 | 30.0 | 31.0 | 32.0 | 33.0
anode sol on | -2.97e-09 | -3.18e-09 | -3.42e-09 | -3.835e-09 | -4.2e-09 | -3.93e-09 | -5.235e-09 | -5.23e-09 | -6.575e-09 | -5.915e-09 | -8.065e-09 | -6.37e-09 | -1.063e-08 | -8.23e-09 | -7.84e-09 | -1.7e-08 | -1.521e-08 | -8.19e-09 | -6.125e-09 | -9.725e-09 | -1.3345e-08 | -2.0545e-08 | -1.5715e-08 | -1.2415e-08 | -1.09e-08 | -9.145e-09 | -8.465e-09 | -7.545e-09 | -1.1025e-08 | -1.349e-08 | -1.896e-08 | -1.6545e-08 | -1.051e-08
The current intensity need to be set correctly but the trends will be the same

## Slide 54: Photocathode Preparation
Co-deposition of alkalis (K and Cs) on Sb layer using an effusion alkali source to grow bialkali photocathode
Deposition chamber was initially baked at 200 °C for >180 h
Vacuum with NEG pumps and an ion pump, Vacuum ~ 10-11 Torr
Sb (99.9999%) , K (99.95%), and Cs (99.9+%)
Working distance: 2 cm, -280 V bias, low power (4 mW) laser (532 nm) and wavelength tunable light source
Substrate temperatures: 120 °C (for Sb), dropping from 120 °C to 80 °C (for alkalis)
Sb heater current supply from 25 A
Temperature kept stable at effusion source and adjusted to control alkali evaporation rate: hot air inlet tube (381-462 ° C), dispensing tube (232 -294 ° C), and reservoir tube (153 -281 ° C)
Chamber pressure: during bialkali deposition, > 1x10-8 Torr and post-deposition to ~10-9-10-10 Torr quickly
H2O partial pressure < 2x10-11 Torr

## Slide 55: New Photoguns for…
CEBAF Injector Full-Energy Upgrade
  Replace 130 kV gun with 200 kV gun
Upgraded Injector Test Facility
  Commission new hardware destined for CEBAF: 200kV gun, HDIce, new quarter cryomodule, etc.,
  R&D: polarized positron source, Bubble Chamber astrophysics experiment, produce polarized targets for physics, etc.,
JLab Electron Ion Collider
  Higher voltage polarized gun for higher bunch charge
  Very high average current un-polarized beams for cooling ions – magnetized cooling
LERF/FEL
  Replace vent/bake gun with load locked gun
  Use alkali-antimonide photocathode instead of GaAs
Notes: Interior Page Design 2

## Slide 56: Upgraded Injector Test Facility - UITF
TEST NEW PHOTOGUNS
COMMISSION NEW QUARTER CRYOMODULE
TEST 200 kV WIEN FILTER
UITF beamline has BPMs, pockels cell tests can happen here…..
TEST HDIce
56